An. F: Printing -process scheme.

- F.1: Colours preparation.

- F.1.1: Reactive colours preparation

- F.1.2: Acid colours preparation

- F.1.3: Cationic colours preparation

- F.1.4: Disperse colours preparation

- F.2: Thickeners preparation.

- F.2.1: Reactive colours thickeners preparation

- F.2.2: Acid colours thickeners preparation

- F.2.3: Cationic colours thickeners preparation

- F.2.4: Disperse colours thickeners preparation

- F.3: Printing paste preparation.

- F.3.1: Reactive printing paste preparation

- F.3.2: Acid printing paste preparation

- F.3.3: Cationic printing paste preparation

- F.3.4: Disperse printing paste preparation

- F.4: Reactive printing.

- F.4.1: Automatic table reactive printing

- F.4.2: Flat table reactive printing

- F.4.3: Electronic table reactive printing

- F.4.4: Rotary machine reactive printing

- F.4.5: Ink-jet reactive printing

- F.5: Acid printing

- F.5..1: Automatic table acid printing

- F.5.2: Flat table acid printing

- F.5.3: Electronic table acid printing

- F.5.4: Rotary machine acid printing

- F.5.5: Ink-jet acid printing

- F.6: Cationic printing

- F.6..1: Automatic table cationic printing

- F.6.2: Flat table cationic printing

- F.6.3: Electronic table cationic printing

- F.6.4: Rotary machine acid printing

- F.7: Disperse printing

- F.7..1: Automatic table disperse printing

- F.7.2: Flat table disperse printing

- F.7.3: Electronic table disperse printing

- F.7.4: Rotary machine disperse printing

- F.8: Printing screen washing

- F.9: Printing squeegees washing

- F.10: Kids washing

- F.11: Tubs washing

F.1: Colours preparation.

F.1.1: Reactive colours preparation

| Department | Printing |
| --- | --- |
| Fabric | COTTON-VISCOSE |
| Process | Reactive colours preparation |
| Equipment | Mixer |
| Item | M1-M2 |
| Run time (h) | - |
| Number of run/yr | 2253-2253 (1) |
| Processed fabric (kg/yr) | 89831-89831 |
| Processed fabric per run (kg) | - |

| Water type W2: 16 l Solubilizing agent (450AA) = 1000 g; Thickening agent (482AA) = 400 g; Reactive colours = 2600 g. Steam type S3 | Mixing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 40 l | Washing |  |  |  |
|  | Discharge |  | Discharge type D2: 40 l T [°C]=17; pH [-]=8,3; Conductivity [mS/cm]=3,06; COD [mg/l]=12000; TSS [mg/l]=2500. |  |

Notes:

For VISCOSE fabric refer to An.D: Production model

(1): Average production per run: 20 kg.

F.1.2: Acid colours preparation

| Department | Printing |
| --- | --- |
| Fabric | SILK-WOOL |
| Process | Acid colours preparation |
| Equipment | Mixer |
| Item | M1-M2 |
| Run time (h) | - |
| Number of run/yr | 1243-1243 (1) |
| Processed fabric (kg/yr) | 49562-49562 |
| Processed fabric per run (kg) | - |

| Water type W2: 16 l Solubilizing agent (450AA) = 500 g; Thickening agent (570AA) = 600 g; pH stabilizer (458AA)= 1200 g; Acid colours = 1700 g. Steam type S3 | Mixing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 40 l | Washing |  |  |  |
|  | Discharge |  | Discharge type D2: 40 l T [°C]=17; pH [-]=8,3; Conductivity [mS/cm]=3,06; COD [mg/l]=12000; TSS [mg/l]=2500. |  |

Notes:

(1): Average production per run: 20 kg.

F.1.3: Cationic colours preparation

| Department | Printing |
| --- | --- |
| Fabric | POLYACRYLIC |
| Process | Cationic colours preparation |
| Equipment | Mixer |
| Item | M1-M2 |
| Run time (h) | - |
| Number of run/yr | 129-129 (1) |
| Processed fabric (kg/yr) | 5163-5163 |
| Processed fabric per run (kg) | - |

| Water type W2: 16 l Solubilizing agent (556AA) = 300 g pH stabilizer (424AA) = 300 g; Cationic colours = 3400 g. Steam type S3 | Mixing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 40 l | Washing |  |  |  |
|  | Discharge |  | Discharge type D2: 40 l T [°C]=17; pH [-]=8,3; Conductivity [mS/cm]=3,06; COD [mg/l]=12000; TSS [mg/l]=2500. |  |

Notes:

(1): Average production per run: 20 kg.

F.1.4: Disperse colours preparation

| Department | Printing |
| --- | --- |
| Fabric | PES-SILK/ACETATE |
| Process | Disperse colours preparation |
| Equipment | Mixer |
| Item | M1-M2 |
| Run time (h) | - |
| Number of run/yr | 1554-1554 (1) |
| Processed fabric (kg/yr) | 61952-61952 |
| Processed fabric per run (kg) | - |

| Water type W2: 16 l Disperse colours = 4000 g. Steam type S3 | Mixing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 40 l | Washing |  |  |  |
|  | Discharge |  | Discharge type D2: 40 l T [°C]=17; pH [-]=8,3; Conductivity [mS/cm]=3,06; COD [mg/l]=12000; TSS [mg/l]=2500. |  |

Notes:

(1): Average production per run: 20 kg.

F.2: Thickeners preparation

F.2.1: Reactive colours thickener preparation.

| Department | Printing |
| --- | --- |
| Fabric | COTTON-VISCOSE |
| Process | Reactive colours thickener preparation |
| Equipment | Mixer |
| Item | M3-M4 |
| Run time (h) | - |
| Number of run/yr | 900-900 (1) |
| Processed fabric (kg/yr) | 89831-89831 |
| Processed fabric per run (kg) | - |

| Water type W2: 200 l Solubilizing agent (450AA) = 15000 g; Thickening agent (539AA) = 5000 g; Thickening agent (478AA) = 15000 g; Antioxidizing agent (482AA) = 15000 g; | Mixing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 400 l | Washing |  |  |  |
|  | Discharge |  | Discharge type D2: 400 l T [°C]=17; pH [-]=8,3; Conductivity [mS/cm]=3,06; COD [mg/l]=12000; TSS [mg/l]=2500. |  |

Notes:

For VISCOSE fabric refer to An.D: Production model

(1): Average production per run: 250 kg.

F.2.2: Acid colours thickener preparation.

| Department | Printing |
| --- | --- |
| Fabric | SILK-WOOL |
| Process | Acid colours thickener preparation |
| Equipment | Mixer |
| Item | M3-M4 |
| Run time (h) | - |
| Number of run/yr | 497-497(1) |
| Processed fabric (kg/yr) | 49562-49562 |
| Processed fabric per run (kg) | - |

| Water type W2: 200 l Thickening agent (470AA) = 45000 g; pH stabilizer (426AA) = 2000 g; pH stabilizer (433AA) = 2000 g; Antifoaming agent (613AL) = 1000g. | Mixing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 400 l | Washing |  |  |  |
|  | Discharge |  | Discharge type D2: 400 l T [°C]=17; pH [-]=8,3; Conductivity [mS/cm]=3,06; COD [mg/l]=12000; TSS [mg/l]=2500. |  |

Notes:

(1): Average production per run: 250 kg.

F.2.3: Cationic colours thickener preparation.

| Department | Printing |
| --- | --- |
| Fabric | POLYACRYLIC |
| Process | Cationic colours thickener preparation |
| Equipment | Mixer |
| Item | M3-M4 |
| Run time (h) | - |
| Number of run/yr | 52-52(1) |
| Processed fabric (kg/yr) | 5163-5163 |
| Processed fabric per run (kg) | - |

| Water type W2: 200 l pH stabilizer (902AA) = 2000 g; Antifoaming agent (613AL) = 3000 g; Thickening agent (520AA) = 41000 g; Anti fermentative agent () = 4000 g. | Mixing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 400 l | Washing |  |  |  |
|  | Discharge |  | Discharge type D2: 400 l T [°C]=17; pH [-]=8,3; Conductivity [mS/cm]=3,06; COD [mg/l]=12000; TSS [mg/l]=2500. |  |

Notes:

(1): Average production per run: 250 kg.

F.2.4: Disperse colours thickener preparation.

| Department | Printing |
| --- | --- |
| Fabric | PES-SILK/ACETATE |
| Process | Disperse colours thickener preparation |
| Equipment | Mixer |
| Item | M3-M4 |
| Run time (h) | - |
| Number of run/yr | 622-622 (1) |
| Processed fabric (kg/yr) | 61952-61952 |
| Processed fabric per run (kg) | - |

| Water type W2: 200 l Thickening agent (539AA) = 43000 g; pH stabilizer (426AA) = 5000 g; Antifoaming agent (613AL) = 2000 g. | Mixing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 400 l | Washing |  |  |  |
|  | Discharge |  | Discharge type D2: 400 l T [°C]=17; pH [-]=8,3; Conductivity [mS/cm]=3,06; COD [mg/l]=12000; TSS [mg/l]=2500. |  |

Notes:

(1): Average production per run: 250 kg.

F.3: Printing paste preparation.

F.3.1: Reactive printing paste preparation

| Department | Printing |
| --- | --- |
| Fabric | COTTON-VISCOSE |
| Process | Reactive printing paste preparation |
| Equipment | TUBS |
| Item | - |
| Run time (h) | - |
| Number of run/yr | 13519 (1) |
| Processed fabric (kg/yr) | 179662 |
| Processed fabric per run (kg) | - |

| Reactive colours Reactive colours thickener (2) | Mixing |  |  |  |
| --- | --- | --- | --- | --- |

Notes:

(1): Average production per run: 40 kg.

(2): Average ratio: 1:5

For VISCOSE fabric refer to An.D: Production model

F.3.2: Acid printing paste preparation

| Department | Printing |
| --- | --- |
| Fabric | SILK-WOOL |
| Process | Acid printing paste preparation |
| Equipment | TUBS |
| Item | - |
| Run time (h) | - |
| Number of run/yr | 7459 (1) |
| Processed fabric (kg/yr) | 99124 |
| Processed fabric per run (kg) | - |

| Acid colours Acid colours thickeners (2) | Mixing |  |  |  |
| --- | --- | --- | --- | --- |

Notes:

(1): Average production per run: 40 kg.

(2): Average ratio: 1:5

F.3.3: Cationic printing paste preparation

| Department | Printing |
| --- | --- |
| Fabric | POLYACRYLIC |
| Process | Cationic printing paste preparation |
| Equipment | TUBS |
| Item | - |
| Run time (h) | - |
| Number of run/yr | 777 (1) |
| Processed fabric (kg/yr) | 10325 |
| Processed fabric per run (kg) | - |

| Cationic colours Cationic colours thickeners (2) | Mixing |  |  |  |
| --- | --- | --- | --- | --- |

Notes:

(1): Average production per run: 40 kg.

(2): Average ratio: 1:5

F.3.4: Disperse printing paste preparation

| Department | Printing |
| --- | --- |
| Fabric | PES-SILK/ACETATE |
| Process | Disperse printing paste preparation |
| Equipment | TUBS |
| Item | - |
| Run time (h) | - |
| Number of run/yr | 9324 (1) |
| Processed fabric (kg/yr) | 123905 |
| Processed fabric per run (kg) | - |

| Disperse colours Disperse colours thickeners (2) | Mixing |  |  |  |
| --- | --- | --- | --- | --- |

Notes:

(1): Average production per run: 40 kg.

(2): Average ratio: 1:5

F.4: Reactive printing.

F.4.1: Automatic table reactive printing

| Department | Printing |
| --- | --- |
| Fabric | COTTON-VISCOSE |
| Process | Automatic table reactive printing |
| Equipment | Automatic repeat table |
| Item | ART1-ART2-ART3 |
| Run time (h) | - |
| Number of run/yr | 507-507-507 |
| Processed fabric (kg/yr) | 3850-3850-3850 |
| Processed fabric per run (kg) | 7,6-7,6-7,6 |

| Reactive printing paste (1) | Squeezing |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Water type W1: 40 l: Soaping agent ()= g/l. | Table washing |  | Discharge type D2: 40 l T [°C]=18; pH [-]=7,38; Conductivity [mS/cm]=0,91; COD [mg/l]=2107; TSS [mg/l]=63. |  |  |
| Water type W1: 30 l: | Table rinsing |  | Discharge type D2: 30 l T [°C]=17; pH [-]=7,66; Conductivity [mS/cm]=0.28; COD [mg/l]=400; TSS [mg/l]=20. |  |  |

Notes:

(1): Average number of colours (squeegees and screens): 8

For VISCOSE fabric refer to An.D: Production model

F.4.2: Flat table reactive printing

| Department | Printing |
| --- | --- |
| Fabric | COTTON-VISCOSE |
| Process | Flat table reactive printing |
| Equipment | Flat table |
| Item | FT1 |
| N° of cycles /yr | 507 |
| Operating hours/yr | 113 |
| Processed fabric (kg/yr) | 3850 |
| Processed fabric per cycle (kg) | 7,6 |

| Reactive printing paste (1) | Squeezing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 450 l/h | Table continuous washing (2) |  | Discharge type D2: 450 l/h T [°C]=18; pH [-]=7,38; Conductivity [mS/cm]=0,91; COD [mg/l]=2561; TSS [mg/l]=63. |  |

Notes:

(1): Average number of colours (squeegees and screens): 8

(2): Washer built onto the machine.

For VISCOSE fabric refer to An.D: Production model

F.4.3: Electronic table reactive printing

| Department | Printing |
| --- | --- |
| Fabric | COTTON-VISCOSE |
| Process | Electronic table reactive printing |
| Equipment | Electronic hand table |
| Item | ET1-ET2 |
| N° of cycles /yr | 143-143 |
| Operating hours/yr | 1073-1073 |
| Processed fabric (kg/yr) | 40756-40756 |
| Processed fabric per run (kg) | 285-285 |

| Reactive printing paste (1) | Squeezing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 2200 l/h | Table continuous washing (2) |  | Discharge type D2: 2200 l/h T [°C]=18; pH [-]=7,64; Conductivity [mS/cm]=2,32; COD [mg/l]=2750; TSS [mg/l]=270. |  |

Notes:

(1): Average number of colours(squeegees and screens): 8

(2): Washer built onto the machine.

For VISCOSE fabric refer to An.D: Production model

F.4.4: Rotary machine reactive printing

| Department | Printing |
| --- | --- |
| Fabric | COTTON-VISCOSE |
| Process | Rotary machine reactive printing |
| Equipment | Rotary machine |
| Item | RM1 |
| N° of cycles /yr | 290 |
| Operating hours/yr | 1089 |
| Processed fabric (kg/yr) | 82750 |
| Processed fabric per cycle (kg) | 285 |

| Reactive printing paste (1) | Squeezing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 2200 l/h | Table and cylinders continuous washing (2) |  | Discharge type D2: 2200 l/h T [°C]=18; pH [-]=7,31; Conductivity [mS/cm]=0,55; COD [mg/l]=903; TSS [mg/l]=10. |  |

Notes:

(1): Average number of colours(cylinders): 8

(2): Washer built onto the machine.

For VISCOSE fabric refer to An.D: Production model

F.4.5: Ink-jet r reactive printing

| Department | Printing |
| --- | --- |
| Fabric | SILK |
| Process | Ink-jet reactive printing |
| Equipment | Ink-jet printer |
| Item | IJP1-IJP2-IJP3 |
| Run time (h) | - |
| N° of run/yr | 109-109-109 |
| Processed fabric (kg/yr) | 827-827-827 |
| Processed fabric per run (kg) | 7,6 |

| Reactive printing paste (1) | Printing |  |
| --- | --- | --- |

Notes:

(1): Average number of colours (cartridges): 8

F.5: Acid printing.

F.5.1: Automatic table acid printing

| Department | Printing |
| --- | --- |
| Fabric | SILK-WOOL |
| Process | Automatic table acid printing |
| Equipment | Automatic repeat table |
| Item | ART1-ART2-ART3 |
| Run time (h) | - |
| Number of run/yr | 279-279-279 |
| Processed fabric (kg/yr) | 2124-2124-2124 |
| Processed fabric per run (kg) | 7,6-7,6-7,6 |

| Acid printing paste (1) | Squeezing |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Water type W1: 40 l: Soaping agent ()= g/l. | Table washing |  | Discharge type D2: 40 l T [°C]=18; pH [-]=7,38; Conductivity [mS/cm]=0,91; COD [mg/l]=2107; TSS [mg/l]=63. |  |  |
| Water type W1: 30 l: | Table rinsing |  | Discharge type D2: 30 l T [°C]=17; pH [-]=7,66; Conductivity [mS/cm]=0.28; COD [mg/l]=400; TSS [mg/l]=20. |  |  |

Notes:

(1): Average number of colours (squeegees and screens): 8

F.5.2: Flat table acid printing

| Department | Printing |
| --- | --- |
| Fabric | SILK-WOOL |
| Process | Flat table acid printing |
| Equipment | Flat table |
| Item | FT1 |
| N° of cycles /yr | 279 |
| Operating hours/yr | 62 |
| Processed fabric (kg/yr) | 2124 |
| Processed fabric per cycle (kg) | 7,6 |

| Reactive printing paste (1) | Squeezing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 450 l/h | Table continuous washing (2) |  | Discharge type D2: 450 l/h T [°C]=18; pH [-]=7,38; Conductivity [mS/cm]=0,91; COD [mg/l]=2561; TSS [mg/l]=63. |  |

Notes:

(1): Average number of colours (squeegees and screens): 8

(2): Washer built onto the machine.

F.5.3: Electronic table acid printing

| Department | Printing |
| --- | --- |
| Fabric | SILK-WOOL |
| Process | Electronic table acid printing |
| Equipment | Electronic hand table |
| Item | ET1-ET2 |
| N° of cycles /yr | 79-79 |
| Operating hours/yr | 592-592 |
| Processed fabric (kg/yr) | 22486-22486 |
| Processed fabric per run (kg) | 285-285 |

| Acid printing paste (1) | Squeezing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 2200 l/h | Table continuous washing (2) |  | Discharge type D2: 2200 l/h T [°C]=18; pH [-]=7,64; Conductivity [mS/cm]=2,32; COD [mg/l]=2750; TSS [mg/l]=270. |  |

Notes:

(1): Average number of colours (squeegees and screens): 8

(2): Washer built onto the machine.

F.5.4: Rotary machine acid printing

| Department | Printing |
| --- | --- |
| Fabric | SILK-WOOL |
| Process | Rotary machine acid printing |
| Equipment | Rotary machine |
| Item | RM1 |
| N° of cycles /yr | 160 |
| Operating hours/yr | 601 |
| Processed fabric (kg/yr) | 45655 |
| Processed fabric per cycle (kg) | 285 |

| Acid printing paste (1) | Squeezing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 2200 l/h | Table and cylinders continuous washing (2) |  | Discharge type D2: 2200 l/h T [°C]=18; pH [-]=7,31; Conductivity [mS/cm]=0,55; COD [mg/l]=903; TSS [mg/l]=10. |  |

Notes:

(1): Average number of colours(cylinders): 8

(2): Washer built onto the machine.

F.5.5: Ink-jet r acid printing

| Department | Printing |
| --- | --- |
| Fabric | SILK |
| Process | Ink-jet reactive printing |
| Equipment | Ink-jet printer |
| Item | IJP1-IJP2-IJP3 |
| Run time (h) | - |
| N° of run/yr | 12-12-12 |
| Processed fabric (kg/yr) | 92-92-92 |
| Processed fabric per run (kg) | 7,6 |

| Acid printing paste (1) | Printing |  |
| --- | --- | --- |

Notes:

(1): Average number of colours (cartridges): 8

F.6: Cationic printing.

F.6.1: Automatic table cationic printing

| Department | Printing |
| --- | --- |
| Fabric | POLYACRYLIC |
| Process | Automatic table cationic printing |
| Equipment | Automatic repeat table |
| Item | ART1-ART2-ART3 |
| Run time (h) | - |
| Number of run/yr | 29-29-29 |
| Processed fabric (kg/yr) | 221-221-221 |
| Processed fabric per run (kg) | 7,6-7,6-7,6 |

| Cationic printing paste (1) | Squeezing |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Water type W1: 40 l: Soaping agent ()= g/l. | Table washing |  | Discharge type D2: 40 l T [°C]=18; pH [-]=7,38; Conductivity [mS/cm]=0,91; COD [mg/l]=2107; TSS [mg/l]=63. |  |  |
| Water type W1: 30 l: | Table rinsing |  | Discharge type D2: 30 l T [°C]=17; pH [-]=7,66; Conductivity [mS/cm]=0.28; COD [mg/l]=400; TSS [mg/l]=20. |  |  |

Notes:

(1): Average number of colours (squeegees and screens): 8

F.6.2: Flat table cationic printing

| Department | Printing |
| --- | --- |
| Fabric | POLYACRYLIC |
| Process | Flat table cationic printing |
| Equipment | Flat table |
| Item | FT1 |
| N° of cycles /yr | 29 |
| Operating hours/yr | 6 |
| Processed fabric (kg/yr) | 221 |
| Processed fabric per cycle (kg) | 7,6 |

| Cationic printing paste (1) | Squeezing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 450 l/h | Table continuous washing (2) |  | Discharge type D2: 450 l/h T [°C]=18; pH [-]=7,38; Conductivity [mS/cm]=0,91; COD [mg/l]=2561; TSS [mg/l]=63. |  |

Notes:

(1): Average number of colours (squeegees and screens): 8

(2): Washer built onto the machine.

F.6.3: Electronic table cationic printing

| Department | Printing |
| --- | --- |
| Fabric | POLYACRYLIC |
| Process | Electronic table cationic printing |
| Equipment | Electronic hand table |
| Item | ET1-ET2 |
| N° of cycles /yr | 8-8 |
| Operating hours/yr | 62-62 |
| Processed fabric (kg/yr) | 2342-2342 |
| Processed fabric per cycle (kg) | 285-285 |

| Cationic printing paste (1) | Squeezing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 2200 l/h | Table continuous washing (2) |  | Discharge type D2: 2200 l/h T [°C]=18; pH [-]=7,64; Conductivity [mS/cm]=2,32; COD [mg/l]=2750; TSS [mg/l]=270. |  |

Notes:

(1): Average number of colours (squeegees and screens): 8

(2): Washer built onto the machine.

F.6.4: Rotary machine cationic printing

| Department | Printing |
| --- | --- |
| Fabric | POLYACRYLIC |
| Process | Rotary machine cationic printing |
| Equipment | Rotary machine |
| Item | RM1 |
| N° of cycles /yr | 17 |
| Operating hours/yr | 63 |
| Processed fabric (kg/yr) | 4756 |
| Processed fabric per cycle (kg) | 285 |

| Cationic printing paste (1) | Squeezing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 2200 l/h | Table and cylinders continuous washing (2) |  | Discharge type D2: 2200 l/h T [°C]=18; pH [-]=7,31; Conductivity [mS/cm]=0,55; COD [mg/l]=903; TSS [mg/l]=10. |  |

Notes:

(1): Average number of colours(cylinders): 8

(2): Washer built onto the machine.

F.7: Disperse printing.

F.7.1: Automatic table disperse printing

| Department | Printing |
| --- | --- |
| Fabric | PES-SILK/ACETATE |
| Process | Automatic table disperse printing |
| Equipment | Automatic repeat table |
| Item | ART1-ART2-ART3 |
| Run time (h) | - |
| Number of run/yr | 349-349-349 |
| Processed fabric (kg/yr) | 2655-2655-2655 |
| Processed fabric per run (kg) | 7,6-7,6-7,6 |

| Disperse printing paste (1) | Squeezing |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Water type W1: 40 l: Soaping agent ()= g/l. | Table washing |  | Discharge type D2: 40 l T [°C]=18; pH [-]=7,38; Conductivity [mS/cm]=0,91; COD [mg/l]=2107; TSS [mg/l]=63. |  |  |
| Water type W1: 30 l: | Table rinsing |  | Discharge type D2: 30 l T [°C]=17; pH [-]=7,66; Conductivity [mS/cm]=0.28; COD [mg/l]=400; TSS [mg/l]=20. |  |  |

Notes:

(1): Average number of colours (squeegees and screens): 8

F.7.2: Flat table disperse printing

| Department | Printing |
| --- | --- |
| Fabric | PES-SILK/ACETATE |
| Process | Flat table disperse printing |
| Equipment | Flat table |
| Item | FT1 |
| N° of cycles /yr | 349 |
| Operating hours/yr | 78 |
| Processed fabric (kg/yr) | 2655 |
| Processed fabric per cycle (kg) | 7,6 |

| Disperse printing paste (1) | Squeezing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 450 l/h | Table continuous washing (2) |  | Discharge type D2: 450 l/h T [°C]=18; pH [-]=7,38; Conductivity [mS/cm]=0,91; COD [mg/l]=2561; TSS [mg/l]=63. |  |

Notes:

(1): Average number of colours (squeegees and screens): 8

(2): Washer built onto the machine.

F.7.3: Electronic table disperse printing

| Department | Printing |
| --- | --- |
| Fabric | PES-SILK/ACETATE |
| Process | Electronic table disperse printing |
| Equipment | Electronic hand table |
| Item | ET1-ET2 |
| N° of cycles /yr | 99-99 |
| Operating hours/yr | 740-740 |
| Processed fabric (kg/yr) | 28108-28108 |
| Processed fabric per cycle (kg) | 285-285 |

| Disperse printing paste (1) | Squeezing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 2200 l/h | Table continuous washing (2) |  | Discharge type D2: 2200 l/h T [°C]=18; pH [-]=7,64; Conductivity [mS/cm]=2,32; COD [mg/l]=2750; TSS [mg/l]=270. |  |

Notes:

(1): Average number of colours (squeegees and screens): 8

(2): Washer built onto the machine.

F.7.4: Rotary machine disperse printing

| Department | Printing |
| --- | --- |
| Fabric | PES-SILK/ACETATE |
| Process | Rotary machine disperse printing |
| Equipment | Rotary machine |
| Item | RM1 |
| N° of cycles /yr | 200 |
| Operating hours/yr | 751 |
| Processed fabric (kg/yr) | 57069 |
| Processed fabric per cycle (kg) | 285 |

| Disperse printing paste (1) | Squeezing |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W1: 2200 l/h | Table and cylinders continuous washing (2) |  | Discharge type D2: 2200 l/h T [°C]=18; pH [-]=7,31; Conductivity [mS/cm]=0,55; COD [mg/l]=903; TSS [mg/l]=10. |  |

Notes:

(1): Average number of colours(cylinders): 8

(2): Washer built onto the machine.

F.8: Printing screen washing.

| Department | Printing |
| --- | --- |
| Fabric | - |
| Process | Printing screen washing |
| Equipment | Screen washer |
| Item | SCW1 |
| Run time (h) | - |
| Number of run/yr | 42524 |
| Processed fabric (kg/yr) | - |
| Processed fabric per run (kg) | - |

| Water type W1: 450 l | Washing (1) | Discharge type D2: 450 l T [°C]= 18; pH [-]= 8,75; Conductivity [mS/cm]= 2,6; COD [mg/l]= 1050; TSS [mg/l]= 406. |
| --- | --- | --- |

Notes:

(1): 1 screen for each run

F.9: Printing squeegees washing.

| Department | Printing |
| --- | --- |
| Fabric | - |
| Process | Printing squeegees washing |
| Equipment | Squeegees washer |
| Item | SQW1 |
| Run time (h) | - |
| Number of run/yr | 10631 |
| Processed fabric (kg/yr) | - |
| Processed fabric per run (kg) | - |

| Water type W1: 450 l | Washing (1) | Discharge type D2: 450 l T [°C]= 18; pH [-]= 7,07; Conductivity [mS/cm]= 2,6; COD [mg/l]= 389; TSS [mg/l]= 947. |
| --- | --- | --- |

Notes:

(1): 2 squeegees for each run

F.10: Kids washing.

| Department | Printing |
| --- | --- |
| Fabric | - |
| Process | Kids washing |
| Equipment | Kids washer |
| Item | KW1 |
| Run time (h) | 1,5 |
| Number of run/yr | 120 |
| Processed fabric (kg/yr) | - |
| Processed fabric per run (kg) | - |

| Water type W1: 700 l |  |  | Washing |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Discharge |  |  | Discharge type D2: 700 l T [°C]= 18; pH [-]= 7,88; Conductivity [mS/cm]= 2,68; COD [mg/l]= 4107; TSS [mg/l]= 2125. |  |  |  |  |
| Water type W1: 700 l |  | Rinsing |  |  |  |  |  |  |  |
|  |  | Discharge |  |  | Discharge type D2: T [°C]= 18; pH [-]= 7,09; Conductivity [mS/cm]= 0,6; COD [mg/l]= 1127; TSS [mg/l]=33. |  |  |  |  |

Notes:

F.11: Tubs washing.

| Department | Printing |
| --- | --- |
| Fabric | - |
| Process | Tubs washing |
| Equipment | Tubs washer |
| Item | TW1 |
| Run time (h) | 0,75 |
| Number of run/yr | 15539 |
| Processed fabric (kg/yr) | - |
| Processed fabric per run (kg) | - |

| Water type W1: 480 l |  |  | Washing (1) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  | Discharge type D2: 480 l T [°C]= 18; pH [-]= 7,17; Conductivity [mS/cm]= 2,33; COD [mg/l]= 3500; TSS [mg/l]= 690. |  |  |  |

Notes:

(1): 2 tubs for each run.