An. H: Fabric washing - process scheme.

- H.1: Rope washing

- H.1.1: Disperse printed washing

- H.1.2: Cationic printed washing

- H.1.3: Acid printed washing

- H.1.4: Reactive printed washing

- H2: Open width washing

- H.2.1: Disperse printed washing

- H.2.2: Acid printed washing

- H.2.3: Reactive printed washing

- H.3: Equipment washing

- H.3.1: Rope washer washing

- H.3.2: Open width washer washing

H.1: Rope washing

H.1.1: Disperse printed washing

| Department | Fabric washing |
| --- | --- |
| Fabric | PES |
| Process | Disperse printed washing |
| Equipment | Rope washer |
| Item | RW1 |
| Number of run/yr | 2174 |
| Run time (h) | 1,00 |
| Processed fabric (kg/yr) | 41302 |
| Processed fabric per run(kg) | 19 |

| Water type W1: 1000 l Soaping agent (646AL) = 1 g/l; Caustic soda (608AL) = 1 g/l; Sodium hydrosulphide (625AL)= 2,5 g/l . Steam type S3 | 1st bath T=100°C; t=10 min |  |  |  |
| --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 90; pH [-]= 12,26; Conductivity [mS/cm]= 10,13; COD [mg/l]= 2324; TSS [mg/l]=66. |  |
| Water type W1: 1000 l | 1st washing |  |  |  |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 23; pH [-]= 11,73; Conductivity [mS/cm]= 3,57; COD [mg/l]= 1987; TSS [mg/l]= 46. |  |
| Water type W1: 1000 l Hydrochloric acid (425AA) = 1 g/l Steam type S3 | 2nd bath T=70°C; t= 10 min (50% of total run) |  |  |  |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 70; pH [-]= 5,43; Conductivity [mS/cm]= 1,63; COD [mg/l]= 295; TSS [mg/l]= 24. |  |
| Water type W1: 1000 l | 2nd washing (50% of total run) |  |  |  |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 18; pH [-]= 6,97; Conductivity [mS/cm]= 0,79; COD [mg/l]= 113; TSS [mg/l]= 30. |  |
| Water type W1: 1000 l | Filling (for fabric discharge) |  |  |  |

Notes:

H.1.2: Cationic printed washing

| Department | Fabric washing |
| --- | --- |
| Fabric | POLYACRYLIC |
| Process | Cationic printed washing |
| Equipment | Rope washer |
| Item | RW1 |
| Number of run/yr | 543 |
| Run time (h) | 1,00 |
| Processed fabric (kg/yr) | 10325 |
| Processed fabric per run(kg) | 19 |

| Water type W1: 1000 l Soaping agent (653AL) = 1 g/l. | 1st bath T=20°C; t=10 min |  |  |  |
| --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 18; pH [-]= 6,83; Conductivity [mS/cm]= 0,96; COD [mg/l]= 3873; TSS [mg/l]=402. |  |
| Water type W1: 1000 l | 1st washing |  |  |  |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 18; pH [-]= 7,08; Conductivity [mS/cm]= 0,65; COD [mg/l]= 568; TSS [mg/l]= 129. |  |
| Water type W1: 1000 l Soaping agent (653AL) = 1 g/l. Antifoaming agent (613AL) = 0,5 g/l. Steam type S3 | 2nd bath T=40°C; t=10 min |  |  |  |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 40; pH [-]= 7,8; Conductivity [mS/cm]= 0,58; COD [mg/l]= 429; TSS [mg/l]= 21. |  |
| Water type W1: 1000 l | 2nd washing |  |  |  |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 18; pH [-]= 8,03; Conductivity [mS/cm]= 0,54; COD [mg/l]= 49; TSS [mg/l]= 13. |  |
| Water type W1: 1000 l | Filling (for fabric discharge) |  |  |  |

Notes:

H.1.3: Acid printed washing

| Department | Fabric washing |
| --- | --- |
| Fabric | WOOL |
| Process | Acid printed washing |
| Equipment | Rope washer |
| Item | RW1 |
| Number of run/yr | 696 |
| Run time (h) | 1,00 |
| Processed fabric (kg/yr) | 13216 |
| Processed fabric per run(kg) | 19 |

| Water type W1: 1000 l Soaping agent (654AL) = 1 g/l. Steam type S3 | 1st bath T=30°C; t=10 min |  |  |  |
| --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 30; pH [-]= 5,33; Conductivity [mS/cm]= 2,33; COD [mg/l]= 398; TSS [mg/l]=271. |  |
| Water type W1: 1000 l | 1st washing |  |  |  |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 18; pH [-]= 6,86; Conductivity [mS/cm]= 1,15; COD [mg/l]= 247; TSS [mg/l]= 89. |  |
| Water type W1: 1000 l Soaping agent (654AL) = 1 g/l. Antifoaming agent (613AL) = 0,5 g/l. Steam type S3 | 2nd bath T=40°C; t=10 min |  |  |  |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 40; pH [-]= 7,3; Conductivity [mS/cm]= 0,86; COD [mg/l]= 73; TSS [mg/l]= 43. |  |
| Water type W1: 1000 l | 2nd washing |  |  |  |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 18; pH [-]= 7,19; Conductivity [mS/cm]= 0,62; COD [mg/l]= 50; TSS [mg/l]= 33. |  |
| Water type W1: 1000 l | Filling (for fabric discharge) |  |  |  |

Notes:

H.1.4: Reactive printed washing

| Department | Fabric washing |
| --- | --- |
| Fabric | VISCOSE |
| Process | Reactive printed washing |
| Equipment | Rope washer |
| Item | RW1 |
| Number of run/yr | 5978 |
| Run time (h) | 1,00 |
| Processed fabric (kg/yr) | 113579 |
| Processed fabric per run(kg) | 19 |

| Water type W1: 1000 l Soaping agent (718AF) = 1 g/l. Steam type S3 | 1st bath T=70°C; t=10 min |  |  |  |
| --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 70; pH [-]= 8,76; Conductivity [mS/cm]= 1,98; COD [mg/l]= 1753; TSS [mg/l]=35. |  |
| Water type W1: 1000 l | 1st washing |  |  |  |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 23; pH [-]= 7,94; Conductivity [mS/cm]= 1,12; COD [mg/l]= 387; TSS [mg/l]= 259. |  |
| Water type W1: 1000 l Soaping agent (718AF) = 1 g/l. Steam type S3 | 2nd bath T=100°C; t=10 min |  |  |  |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 100; pH [-]= 7,99; Conductivity [mS/cm]= 0,73; COD [mg/l]= 495; TSS [mg/l]= 21. |  |
| Water type W1: 1000 l | 2nd washing |  |  |  |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 23; pH [-]= 7,72; Conductivity [mS/cm]= 0,68; COD [mg/l]= 78; TSS [mg/l]= 117. |  |
| Water type W1: 1000 l | Filling (for fabric discharge) |  |  |  |

Notes:

For VISCOSE fabric refer to An.D: Production model

H.2: Open width washing

H.2.1: Disperse printed washing.

| Department | Fabric washing |
| --- | --- |
| Fabric | PES-SILK/ACETATE |
| Process | Disperse printed washing |
| Equipment | Open width washer |
| Item | OWW1 |
| Number of cycles/yr | 435 |
| Cycle time (h) | 2,5 |
| Processed fabric (kg/yr) | 82603 |
| Processed fabric per hour (kg/h) | 76 |

| Water type.W1: 3000 l Water type W2: 76 l/h (reintegration) | 1st washing | Discharge type D2: 3000 l T [°C]= 18; pH [-]= 7,9; Conductivity [mS/cm]= 0,21; COD [mg/l]= 760; TSS [mg/l]=25. |
| --- | --- | --- |
| Water type.W1: 2000 l Water type W2: 76 l/h (reintegration) For PES fabric: Caustic soda (608AL) = 1,5 g/l; Sodium hydrosulphide (625AL) = 1,5 g/l; Soaping agent (646AL) = 1,5 g/l. For ACETATE fabric: Soaping agent (654AL) = 1 g/l. Steam type S3. | 1st bath T= 90°C | Discharge type D2: 2000 l T [°C]= 90; pH [-]= 8,1; Conductivity [mS/cm]= 4,53; COD [mg/l]= 820; TSS [mg/l]= 48. |
| Water type.W1: 2000 l Water type W2: 76 l/h (reintegration) For PES fabric: Caustic soda (608AL) = 1,5 g/l; Sodium hydrosulphide (625AL) = 1,5 g/l; Soaping agent (646AL) = 1,5 g/l. For ACETATE fabric: Soaping agent (654AL) = 1 g/l. Steam type S3. | 2nd bath T= 90°C | Discharge type D2: 2000 l T [°C]= 90; pH [-]= 9,3; Conductivity [mS/cm]= 5,43; COD [mg/l]= 150; TSS [mg/l]=18. |
| Water type.W1: 2000 l Water type W2: 76 l/h (reintegration) For PES fabric: Caustic soda (608AL) = 1,5 g/l; Sodium hydrosulphide (625AL) = 1,5 g/l; Soaping agent (646AL) = 1,5 g/l. For ACETATE fabric: Soaping agent (654AL) = 1 g/l. Steam type S3. | 3rd bath T= 90°C | Discharge type D2: 2000 l T [°C]= 90; pH [-]= 8,5; Conductivity [mS/cm]= 3,87; COD [mg/l]= 200; TSS [mg/l]= 15. |
| Water type.W1: 3000 l Water type W2: 76 l/h (reintegration) | 2nd washing | Discharge type D2: 3000 l T [°C]= 38; pH [-]= 7,8; Conductivity [mS/cm]= 0,23; COD [mg/l]= 20; TSS [mg/l]= 10. |

Notes:

H.2.2: Acid printed washing.

| Department | Fabric washing |
| --- | --- |
| Fabric | SILK-WOOL |
| Process | Acid printed washing |
| Equipment | Open width washer |
| Item | OWW1 |
| Number of cycles/yr | 454 |
| Cycle time (h) | 2,5 |
| Processed fabric (kg/yr) | 86183 |
| Processed fabric per hour (kg/h) | 76 |

| Water type.W1: 3000 l Water type W2: 76 l/h (reintegration) | 1st washing | Discharge type D2: 3000 l T [°C]= 18; pH [-]= 7,9; Conductivity [mS/cm]= 0,24; COD [mg/l]= 835; TSS [mg/l]= 53. |
| --- | --- | --- |
| Water type.W1: 2000 l Water type W2: 76 l/h (reintegration) Soaping agent (654AL) = 1 g/l. | 1st bath T= 20°C | Discharge type D2: 2000 l T [°C]= 20; pH [-]= 7,63; Conductivity [mS/cm]= 0,26; COD [mg/l]= 650; TSS [mg/l]= 42. |
| Water type.W1: 2000 l Water type W2: 76 l/h (reintegration) Soaping agent (654AL) = 1 g/l. | 2nd bath T= 20°C | Discharge type D2: 2000 l T [°C]= 20; pH [-]= 8,3; Conductivity [mS/cm]= 0,27; COD [mg/l]= 530; TSS [mg/l]= 31. |
| Water type.W1: 2000 l Water type W2: 76 l/h (reintegration) Soaping agent (654AL) = 1 g/l. | 3rd bath T= 20°C | Discharge type D2: 2000 l T [°C]= 20; pH [-]= 7,9; Conductivity [mS/cm]= 0,32; COD [mg/l]= 455; TSS [mg/l]= 34. |
| Water type.W1: 2000 l Water type W2: 76 l/h (reintegration) | 2nd washing | Discharge type D2: 3000 l T [°C]= 20; pH [-]= 7,5; Conductivity [mS/cm]= 0,23; COD [mg/l]= 50; TSS [mg/l]= 13. |

Notes:

H.2.3: Reactive printed washing.

| Department | Fabric washing |
| --- | --- |
| Fabric | COTTON-SILK |
| Process | Reactive printed washing |
| Equipment | Open width washer |
| Item | OWW1 |
| Number of cycles/yr | 351 |
| Cycle time (h) | 2,5 |
| Processed fabric (kg/yr) | 68562 |
| Processed fabric per hour (kg/h) | 76 |

| Water type.W1: 3000 l Water type W2: 76 l/h (reintegration) | 1st washing | Discharge type D2: 3000 l T [°C]= 18; pH [-]= 8,66; Conductivity [mS/cm]= 1,6; COD [mg/l]= 250; TSS [mg/l]= 74. |
| --- | --- | --- |
| Water type.W1: 2000 l Water type W2: 76 l/h (reintegration) Soaping agent (718AF) = 1 g/l. Steam type S3. | 1st bath T= 90°C | Discharge type D2: 2000 l T [°C]= 90; pH [-]= 7,79; Conductivity [mS/cm]= 0,62; COD [mg/l]= 200; TSS [mg/l]= 27. |
| Water type.W1: 2000 l Water type W2: 76 l/h (reintegration) Soaping agent (718AF) = 1 g/l. Steam type S3. | 2nd bath T= 90°C | Discharge type D2: 2000 l T [°C]= 90; pH [-]= 7,73; Conductivity [mS/cm]= 0,61; COD [mg/l]= 400; TSS [mg/l]= 11. |
| Water type.W1: 2000 l Water type W2: 76 l/h (reintegration) Soaping agent (718AF) = 1 g/l. Steam type S3. | 3rd bath T= 90°C | Discharge type D2: 2000 l T [°C]= 90; pH [-]= 7,73; Conductivity [mS/cm]= 0,6; COD [mg/l]= 200; TSS [mg/l]= 14. |
| Water type.W1: 3000 l Water type W2: 76 l/h (reintegration) | 2nd washing | Discharge type D2: 3000 l T [°C]= 23; pH [-]= 7,29; Conductivity [mS/cm]= 0,56; COD [mg/l]= 30; TSS [mg/l]=14. |

Notes:

H.3: Equipment washing

H.3.1: Rope washer washing

| Department | Fabric washing |
| --- | --- |
| Fabric | - |
| Process | Rope washer washing |
| Equipment | Rope washer |
| Item | RW1 |
| Number of cycles/yr | 2174 (1) |
| Cycle time (h) | 0,5 |
| Processed fabric (kg/yr) | - |
| Processed fabric per hour (kg/h) | - |

| Water type W1: 1000 l | Washing |  |  |  |
| --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D2: 1000 l T [°C]= 18; pH [-]= 7,9; Conductivity [mS/cm]= 0,31; COD [mg/l]= 200; TSS [mg/l]= 10. |  |

Notes:

(1): Equipment washing after disperse printed washing.

H.3.2: Open width washer washing.

| Department | Fabric washing |
| --- | --- |
| Fabric | - |
| Process | Open width washer washing |
| Equipment | Open width washer |
| Item | OWW1 |
| Number of cycles/yr | 435 (1) |
| Cycle time (h) | 0,5 |
| Processed fabric (kg/yr) | - |
| Processed fabric per hour (kg/h) | - |

| Water type.W1: 3000 l | 1st washing | Discharge type D2: 3000 l T [°C]= 18; pH [-]= 7,9; Conductivity [mS/cm]= 0,27; COD [mg/l]= 50; TSS [mg/l]= 10. |
| --- | --- | --- |
| Water type.W1: 2000 l | 2nd washing | Discharge type D2: 2000 l T [°C]= 18; pH [-]= 7,9; Conductivity [mS/cm]= 0,31; COD [mg/l]= 50; TSS [mg/l]= 10. |
| Water type.W1: 2000 l | 3rd washing | Discharge type D2: 2000 l T [°C]= 18; pH [-]= 7,9; Conductivity [mS/cm]= 0,29; COD [mg/l]= 50; TSS [mg/l]= 10. |
| Water type.W1: 2000 l | 4th washing | Discharge type D2: 2000 l T [°C]= 18; pH [-]= 7,9; Conductivity [mS/cm]= 0,31; COD [mg/l]= 50; TSS [mg/l]= 10. |
| Water type.W1: 2000 l | 5th washing | Discharge type D2: 3000 l T [°C]= 18; pH [-]= 7,9; Conductivity [mS/cm]= 0,31; COD [mg/l]= 50; TSS [mg/l]= 10. |

Notes:

(1): Equipment washing after disperse printed washing.