An. I: Finishing - process scheme.

- I.1: Water finishing.

- I.2: Softener finishing.

I.1: Water  finishing.

| Department | Finishing |
| --- | --- |
| Fabric | COTTON - SILK - WOOL - PES-POLYACRYLATE - VISCOSE - SILK/ACETATE |
| Process | Water finishing |
| Equipment | Rameuse |
| Item | R1 |
| Number of cycles/year | 328 |
| Cycle time (h) | 4 |
| Processed fabric (kg/yr) | 187097 |
| Processed fabric per hour (kg/h) | 143 |

| Water type W2: 143 l/h | Doping Wringing Thermosetting (T=130°C) | Discharge type D2: 100 l/cycle T [°C]= 18; pH [-]= 7,6; Conductivity [mS/cm]= 0,21; COD [mg/l]= 350; TSS [mg/l]= 50. |
| --- | --- | --- |

Notes:

For VISCOSE fabric refer to An.D: Production model

I.2: Softener  finishing.

| Department | Finishing |
| --- | --- |
| Fabric | COTTON - SILK - WOOL - PES-POLYACRYLATE - VISCOSE - SILK/ACETATE |
| Process | Softener finishing |
| Equipment | Rameuse |
| Item | R1 |
| Number of cycles/year | 146 |
| Cycle time (h) | 4 |
| Processed fabric (kg/yr) | 83154 |
| Processed fabric per hour (kg/h) | 143 |

| Water type W2: 143 l/h Softener (708AF) = 10 g/l | Doping Wringing Thermosetting (T=130°C) | Discharge type D2: 100 l/cycle T [°C]= 18; pH [-]= 7,6; Conductivity [mS/cm]= 0,21; COD [mg/l]= 7500; TSS [mg/l]= 150. |
| --- | --- | --- |

Notes:

For VISCOSE fabric refer to An.D: Production model