- An. F: Preparation - Process scheme.

- F.1: Scouring.

- F 1.1 Scouring in Jigger at 50°-90°C

- F 1.2 Scouring in Jigger at 60°C

- F 1.3 Scouring in Torpedo at 80°-90°C

- F 1.4 Scouring with continuos washing at 60°C in Torpedo

- F 1.5 Scouring in Torpedo at 60°C

- F 1.6 Scouring in Overflow at 80°-90°C

- F 1.7 Scouring in Overflow at 60°C

- F.2: Scouring for disperse dyeing.

- F 2.1 Scouring disperse dyeing in Torpedo at 90°C

- F 2.2 Scouring disperse dyeing Overflow at 90°C

- F.3: Desizing.

- F 3.1 Desizing in Jigger at 90°C

- F 3.2 Desizing in Jigger at 70°-90°C

- F 3.3 Desizing in Torpedo at 70°C

- F 3.4 Desizing in Torpedo at 90°C

- F 3.5 Desizing in Overflow at 90°C

- F.4: Double scouring.

- F 4.1 Double scouring with continuos washing in Torpedo at 60°C

- F 4.2 Double scouring in Torpedo at 60°C

- F.5: Special scouring.

- F 5.1 Special scouring in Jigger at 90°C

- F 5.2 Special scouring in Torpedo at 60°C

- F.6: Bleaching.

- F 6.1 Bleaching in Jigger at 90°C

- F 6.2 Bleaching in Torpedo at 80°C

- F.7: Bleaching before dyeing.

- F 7.1 Bleaching before dyeing in Overflow at 90°C

- F.8: Barking.

- F 8.1 Barking in Torpedo at 110°-130°C

- F.1: Scouring.

- F 1.1: Scouring in Jigger at 50° - 90°C

| Department | Preparation |
| --- | --- |
| Fabric | FLAX-PL-CO/PL-FLAX/PL |
| Process | Scouring in Jigger at 50°-90°C |
| Equipment | Jigger |
| Item | J144-J145-C146 |
| Run time (h) | 2,30-4 |
| Number of run/yr | 87-155-2 |
| Processed fabric (kg/yr) | 10014-9496-110 |
| Processed fabric per run (kg) | 115-61-55 |

| Water type W4 :equip volume Non ionic surfactant (1058 - 2057)=4 - 8 g/l Steam type S1 | Bath T=50-90°C t=30 min Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 68; pH [-]= 9,75; Conductivity [mS/cm]=0,45; COD [mg/l]= 7050. TSS [mg/l]= 250 |  |  |
| Water type W3: 1290-2210-1215 l | Continuous washing (1 lysis) |  | Discharge type D1: 1290-2210-1215 T [°C]= 35; pH [-]= 8,3; Conductivity [mS/cm]= 0,23; COD [mg/l]= 1420 TSS [mg/l]= 80 |  |  |
| Water type W4:equip volume T [°C]=40. | Washing (2 lysis) |  |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 32; pH [-]= 7,99; Conductivity [mS/cm]= 0,19; COD [mg/l]= 110. TSS [mg/l]= 25 |  |  |
| Water type W3:equip volume | Filling (for fabric discharge) |  |  |  |  |
|  | Filling discharge (50% of total run) |  | Discharge type D1: equip. volume T [°C]= 18 pH [-]= 7,8 Conductivity [mS/cm]= 0,21 COD [mg/l]= 50 TSS [mg/l]= 5 |  |  |

- Notes:

Scouring at 50°C: 8% of total run.

Scouring at 90°C: 92% of total run.

For   FLAX/PL   Fabric:   see An.D

- F 1.2 Scouring in Jigger at 60°C

| Department | Preparation |
| --- | --- |
| Fabric | FLAX-PL-CO/PL-FLAX/PL |
| Process | Scouring in Jigger at 60°C |
| Equipment | Jigger |
| Item | J144-J145-C146 |
| Run time (h) | 4,00 |
| Number of run/yr | 27-47-2 |
| Processed fabric (kg/yr) | 3108-2879-110 |
| Processed fabric per run (kg) | 115-61-55 |

| Water type W4 :equip volume Non ionic surfactant (2057)=1 g/l; Sequestering agent (1071)=0,5 g/l. Steam type S1 | Bath T=60°C t=40 min Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 52; pH [-]= 8,2; Conductivity [mS/cm]= 1,12; COD [mg/l]=1010. TSS [mg/l]= 110 |  |  |
| Water type W3: 2210-1290-1215 l | Continuous washing (1 lysis) |  | Discharge type D1: 2210-1290-1215 T [°C]= 25; pH [-]= 7,9; Conductivity [mS/cm]= 0,52; COD [mg/l]= 200. TSS [mg/l]= 20 |  |  |
| Water type W4:equip volume | Washing (2 lysis) |  |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 31; pH [-]= 7,8; Conductivity [mS/cm]= 0,21; COD [mg/l]= 70. TSS [mg/l]= 5 |  |  |
| Water type W3 :equip volume | Filling (for fabric discharge) |  |  |  |  |
| Water type W3 :equip volume | Filling disharge (50% of total run) |  | Discharge type D1: equip. volume T [°C]= 19 pH [-]= 7,6 Conductivity [mS/cm]= 0,18 COD [mg/l]= 50 TSS [mg/l]= 5 |  |  |

- Notes:

For   FLAX/PL   Fabric:   see An.D

- F 1.3 Scouring in Torpedo at 80°-90°C

| Department | Preparation |
| --- | --- |
| Fabric | FLAX-PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Scouring in Torpedo at 80°-90°C |
| Equipment | Torpedo |
| Item | T151-T153-T154-T155 |
| Run time (h) | 1,30-2,10 |
| Number of run/yr | 58-16-129-19 |
| Processed fabric (kg/yr) | 8651-1075-5262-1921 |
| Processed fabric per run (kg) | 149-67-41-101 |

| Water type W4:equipment volume Non ionic surfactant (2057)=3-1,5 g/l Steam type S1 | Bath T= 80-90°C t= 30 min Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]=48; pH [-]=9,54; Conductivity [mS/cm]=0,23; COD [mg/l]=1060; TSS [mg/l]=70. |  |  |
| Water type W3:equip volume | Washing |  |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]=19; pH [-]=8,80; Conductivity [mS/cm]=0,19; COD [mg/l]=160; TSS [mg/l]=12 |  |  |

- Notes:

Scouring at 80°C: 50% of total run.

Scouring at 90°C: 50% of total run

For   FLAX/PL   Fabric:   see An.D

.

F 1.4 Scouring with continuos washing in Torpedo at 60° C

| Department | Preparation |
| --- | --- |
| Fabric | FLAX-PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Scouring with continuos washing in Torpedo at 60°C |
| Equipment | Torpedo |
| Item | T151-T153-T154-T155 |
| Run time (h) | 2,40 |
| Number of run/yr | 309-56-89-184 |
| Processed fabric (kg/yr) | 46088-5968-3630-18605 |
| Processed fabric per run (kg) | 149-106-41-101 |

| Water type W4:equip volume Non ionic surfactant (1058)=3 g/l. Steam type S1 | Bath T=60°C t=50 min Indirect heating |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W4: 1500 l | Continuous washing |  | Discharge type D1: 1500 l T [°C]= 53; pH [-]= 8,5; Conductivity [mS/cm]= 1,8; COD [mg/l]= 1250; COD [mg/l]= 510 (for T154); TSS [mg/l]= 115 |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 40; pH [-]= 7,9; Conductivity [mS/cm]= 0,5; COD [mg/l]= 810; COD [mg/l]= 510 (for T154); TSS [mg/l]= 65; |  |
| ; |  |  |  |  |
| Water type W4 :equip volume | Washing |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 31; pH [-]= 7,9; Conductivity [mS/cm]= 0,2; COD [mg/l]= 150 TSS [mg/l]= 12 |  |

Notes:

- For FLAX/PL FABRIC: SEE An.D

- F 1.5 Scouring in Torpedo at 60°C

| Department | Preparation |
| --- | --- |
| Fabric | FLAX-PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Scouring in Torpedo at 60°C |
| Equipment | Torpedo |
| Item | T155 |
| Run time (h) | 3,10 |
| Number of run/yr | 119 |
| Processed fabric (kg/yr) | 12032 |
| Processed fabric per run (kg) | 101 |

| Water type W4: equip volume Non ionic surfactant (1058)=3 g/l. Steam type S1 |  | Bath T=60°C t=50 min Indirect heating |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Discharge |  | Discharge type D1: equip. volume T [°C]= 53; pH [-]= 8,5; Conductivity [mS/cm]= 1,9; COD [mg/l]= 1650; TSS [mg/l]= 80; |  |
| Water type W4:equip volume |  | Washing |  |  |  |
|  |  | Discharge |  | Discharge type D1: equip. volume T [°C]= 38; pH [-]= 7,6; Conductivity [mS/cm]= 0,19; COD [mg/l]= 400; TSS [mg/l]= 15 |  |

- Notes:

Scouring at 80°C: 50% of total run.

Scouring at 90°C: 50% of total run

For   FLAX/PL   Fabric:   see An.D

- F 1.6 Scouring in Overflow at 80°-90°C

| Department | Preparation |
| --- | --- |
| Fabric | FLAX-PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Scouring in Overflow at 80°-90°C |
| Equipment | Overflow |
| Item | O192-O193-O194 |
| Run time (h) | 2,50 |
| Number of run/yr | 34-18-26 |
| Processed fabric (kg/yr) | 1798-834-880 |
| Processed fabric per run (kg) | 53-46-34 |

| Water type W4:equip volume Non ionic surfactant (1058)=2-4 g/l; Lubricating agent (1057)=2 g/l. Steam type S1 | Bath T=80-90°C t=30-60 min Indirect heating |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Water type W4: 500 l | Continuous washing |  |  | Discharge type D1: 500 l T [°C]= 68; pH [-]= 8,2; Conductivity [mS/cm]= 1,3; COD [mg/l]= 2720. COD [mg/l]= 2150 (for O193 O194) TSS [mg/l]= 180 |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 40; pH [-]= 7,6; Conductivity [mS/cm]= 0,19; COD [mg/l]= 2280 COD [mg/l]= 2050 (for O193 O194) TSS [mg/l]= 80 |  |  |  |
| Water type W4: equip. volume |  | Washing |  |  |  |  |  |
|  |  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 28; pH [-]= 7,2; Conductivity [mS/cm]= 0,19; COD [mg/l]= 450. TSS [mg/l]= 25 |  |  |
| Water type W3: equip. volume |  | Filling (for fabric discharge) |  |  |  |  |  |
|  |  | Filling discharge (50% of total run) |  |  | Discharge type D1: equip. volume T [°C]= 19 pH [-]= 7,6 Conductivity [mS/cm]= 0,21 COD [mg/l]= 150 TSS [mg/l]= 12 |  |  |

- Notes:

Scouring at 80°C: 50% of total run;

Scouring at 90°C: 50% of total run.

For   FLAX/PL   Fabric:   see An.D

- F 1.7 Scouring in Overflow at 60°C

| Department | Preparation |
| --- | --- |
| Fabric | FLAX-PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Scouring in Overflow at 60°C |
| Equipment | Overflow |
| Item | O192-O193-O194 |
| Run time (h) | 3,10 |
| Number of run/yr | 2-107-46 |
| Processed fabric (kg/yr) | 106-4958-1557 |
| Processed fabric per run (kg) | 53-46-34 |

| Water type W4:equip volume Non ionic surfactant (1058)=2 g/l; Lubricating agent (1057)=2 g/l. Steam type S1 | Bath T=60°C t=60 min Indirect heating |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]=52; pH [-]=8,86; Conductivity [mS/cm]=0,21; COD [mg/l]=1580; TSS [mg/l]=65. |  |  |  |
| Water type W3: equip. volume |  | Washing |  |  |  |  |  |
|  |  | Discharge |  |  | Discharge type D1: equip. volume T [°C]=17; pH [-]=8,24; Conductivity [mS/cm]=0,17; COD [mg/l]=150; TSS [mg/l]=12. |  |  |
| Water type W3: equip. volume |  | Filling (for fabric discharge) |  |  |  |  |  |

|  | Filling discharge (50% of total run) |  | Discharge type D1: equip. volume T [°C]= 17; pH [-]= 7,6; Conductivity [mS/cm]= 0,21; COD [mg/l]= 50; TSS [mg/l]= 5. |  |
| --- | --- | --- | --- | --- |

- Notes:

For   FLAX/PL   Fabric:   see An.D

- F.2: Scouring for disperse dyeing.

- F 2.1 Scouring for disperse dyeing in Torpedo at 90°C

| Department | Dyeing |
| --- | --- |
| Fabric | PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Scouring for disperse dyeing in torpedo at 90°C |
| Equipment | Torpedo |
| Item | T151-T153-T154-T155 |
| Run time (h) | 4.00-5.30 |
| Number of run/yr | 88-30-122-2 |
| Processed fabric (kg/yr) | 6652-1810-8622-79 |
| Processed fabric per run (kg) | 75-60-71-39 |

| Water type W4:equip volume Non ionic surfactant (2057): 1,5 g/l. Steam type S1 | Bath T=90°C; t=30 min. Indirect heating |  |  |
| --- | --- | --- | --- |
| Water type W3: 1500 l; | Continuous Washing | Discharge type Dl: 1500 l T [°C]= 78; pH [-]= 8,1; Conductivity [mS/cm]=0,6; COD [mg/l]= 1580. TSS [mg/l]= 80 |  |
|  | Discharge | Discharge type D1: equip. volume T [°C]= 43; pH [-]= 7,8; Conductivity [mS/cm]= 0,3; COD [mg/l]= 1020. TSS [mg/l]= 95 |  |

- Notes:

For   FLAX/PL   Fabric:   see An.D

- F 2.2 Scouring for disperse dyeing in Overflow at 90°C

| Department | Dyeing |
| --- | --- |
| Fabric | PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Scouring for disperse dyeing in overflow at 90°C |
| Equipment | Overflow |
| Item | O192-O193-O194 |
| Run time (h) | 5,00-6,00 |
| Number of run/yr | 0-106-63 |
| Processed fabric (kg/yr) | 0-5691-3166 |
| Processed fabric per run (kg) | 0-54-50 |

| Water type W4:equip volume Lubricating agent (1057): 2 g/l; Non ionic surfactant (2057 ): 1,3 g/l Steam type S1 | Bath T=90°C; t=30 min. Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Water type W3: 500 l; | Continuous washing |  | Discharge type Dl: 500 l T [°C]= 50; pH [-]= 8,1; Conductivity [mS/cm]= 1,6; COD [mg/l]= 2630 COD [mg/l]= 2110 (for O193 O194) TSS [mg/l]= 80 |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 50; pH [-]= 7,6; Conductivity [mS/cm]= 0,8; COD [mg/l]= 2150 COD [mg/l]= 2050 (for O193 O194) TSS [mg/l]= 35 |  |  |
| Water type W4: equip. volume | Washing |  |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 38; pH [-]= 7,6; Conductivity [mS/cm]= 0,21; COD [mg/l]= 300. TSS [mg/l]= 18 |  |  |

- Notes:

For   FLAX/PL   Fabric:   see An.D

- F 3: Desizing.

- F 3.1 Desizing in Jigger at 90°C

| Department | Preparation |
| --- | --- |
| Fabric | PL-CO/PL-FLAX/PL |
| Process | Desizing in Jigger at 90°C |
| Equipment | Jigger |
| Item | J144-J145-C146 |
| Run time (h) | 5,00 |
| Number of run/yr | 13-108-0 |
| Processed fabric (kg/yr) | 2557-5975-0 |
| Processed fabric per run (kg) | 197-55-0 |

| Water type W4 :equip volume Non ionic surfactant (2057):8 g/l Steam type S1 | 1st bath T=90°C t=30 min Indirect heating |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 68; pH [-]= 8,5; Conductivity [mS/cm]= 1,9; COD [mg/l]= 9500. TSS [mg/l]= 250 |  |  |  |  |
| Water type W4 :equip volume | 1st Washing (2 lysis) |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 30; pH [-]= 7,6; Conductivity [mS/cm]= 1,8; COD [mg/l]= 8700. TSS [mg/l]= 150 |  |  |  |  |
| Water type W4 :equip volume Non ionic surfactant (2057)=8 g/l. Steam type S1 | 2nd bath T=90°C t=30 min Indirect heating |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 60; pH [-]= 7,6; Conductivity [mS/cm]= 1,8; COD [mg/l]= 7500. TSS [mg/l]= 150 |  |  |  |  |
| Water type W3: 4355-1091-1000 l | Continuous washing (1 lysis) |  |  | Discharge type D1: 4355-1091-1000 l T [°C]= 88; pH [-]= 8,1; Conductivity [mS/cm]= 0,5; COD [mg/l]= 800. TSS [mg/l]= 30 |  |  |  |  |
| Water type W4 :equip volume | 2nd Washing (2 lysis) |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 25; pH [-]= 7,6; Conductivity [mS/cm]= 0,2; COD [mg/l]= 100. TSS [mg/l]= 10 |  |  |  |  |
| Water type W4: equip. volume |  | Filling (for fabric discharge) |  |  |  |  |  |  |
|  |  | Filling discharge (50% of total run) |  |  | Discharge type D1: equip. volume T [°C]= 35; pH [-]= 7,6; Conductivity [mS/cm]= 0,19; COD [mg/l]= 50. TSS [mg/l]= 0 |  |  |  |

- Notes:

For   FLAX/PL   Fabric:   see An.D

- F 3.2 Desizing in Jigger at 70°-90°C

| Department | Preparation |
| --- | --- |
| Fabric | PL-CO/PL-FLAX/PL |
| Process | Desizing in Jigger at 70°-90°C |
| Equipment | Jigger |
| Item | J144-J145-C146 |
| Run time (h) | 5,00 |
| Number of run/yr | 257-25-6 |
| Processed fabric (kg/yr) | 50556-1383-355 |
| Processed fabric per run (kg) | 197-55-59 |

| Water type W4 :equip volume Non ionic surfactant (2057)=7,5 g/l; Sodium Hydrosulphite (1017)=2 g/l. Steam type S1 | 1st bath T=70-90°C t=30 min Indirect heating |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 51; pH [-]= 8,2; Conductivity [mS/cm]= 1,8; COD [mg/l]= 10750 TSS [mg/l]= 185 |  |  |  |  |  |  |
| Water type W4 :equip volume Non ionic surfactant (2057)=7,5 g/l; Sodium Hydrosulphite (1017)=2 g/l. Steam type S1 | 2nd bath T=70-90°C t=30 min Indirect heating |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 56; pH [-]= 8,5; Conductivity [mS/cm]= 2,1; COD [mg/l]= 8600. TSS [mg/l]= 93 |  |  |  |  |  |  |
| Water type W4 :equip volume Sodium Hydrosulphite (1017)=2 g/l; Non ionic surfactant (1058)=2 g/l; Soda Solvay (1016)=0,5 g/l; Surfactant (2057)=7,5 g/l. Steam type S1 | 3rd bath T=70-90°C t=30 min Indirect heating |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 58; pH [-]= 8,3; Conductivity [mS/cm]= 2,5; COD [mg/l]= 8250. TSS [mg/l]= 120 |  |  |  |  |  |  |
| Water type W3 2: 4355-1091-1000 l | Continuous washing (1 lysis) |  |  | Discharge type D1:4355-1091-1000 l T [°C]= 25; pH [-]= 7,8; Conductivity [mS/cm]= 0,31; COD [mg/l]= 950. TSS [mg/l]= 15 |  |  |  |  |  |  |
| Water type W4 :equip volume Steam type S1 | Washing (2 lysis) |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,06; Conductivity [mS/cm]= 0,21; COD [mg/l]= 310. TSS [mg/l]= 20 |  |  |  |  |  |  |
| Water type W4 : equip. volume |  | Filling (for fabric discharge) |  |  |  |  |  |  |  |  |
|  |  | Filling discharge (50% of total run) |  |  | Discharge type D1: equip. volume T [°C]= 38; pH [-]= 7,8; Conductivity [mS/cm]= 0,21; COD [mg/l]= 100. TSS [mg/l]= 10 |  |  |  |  |  |

Notes:

Desizing at 70°C: 60% of total run.

Desizing at 90°C: 40% of total run.

For   FLAX/PL   Fabric:   see An.D

- F 3.3 Desizing in Torpedo at 70°C

| Department | Preparation |
| --- | --- |
| Fabric | PL |
| Process | Desizing in Torpedo at 70°C (DOS09S) |
| Equipment | Torpedo |
| Item | T151-T153-T154-T155 |
| Run time (h) | 6,30 |
| Number of run/yr | 66-0-2-0 |
| Processed fabric (kg/yr) | 9803-0-101-0 |
| Processed fabric per run (kg) | 148-0-50-0 |

| Water type W4:equip volume Non ionic surfactant (1058)=2 g/l; Sodium Hydrosulphite (1017)=2 g/l; Soda Solvay (1016)=0,5 g/l. Steam type S1 | 1st bath T=70°C t=30 min Indirect heating |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W4: 1500 l | 1st continuous washing |  | Discharge type D1: 1500 l T [°C]= 51; pH [-]= 8,01; Conductivity [mS/cm]= 2,01; COD [mg/l]= 2300. COD [mg/l]= 950 (for T154). TSS [mg/l]= 70 |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 50; pH [-]= 7,8; Conductivity [mS/cm]= 1,3; COD [mg/l]= 1460. COD [mg/l]= 950 (For T154). TSS [mg/l]= 40 |  |
| Water type W4:equip volume Non ionic surfactant (1058)=2 g/l; Sodium Hydrosulphite (1017)=2 g/l; Soda Solvay (1016)=0,5 g/l. Steam type S1 | 2nd bath T=70°C t=30 min Indirect heating |  |  |  |
| Water type W4: 1500 l | 2nd continuous washing |  | Discharge type D1: 1500 l T [°C]= 50; pH [-]= 8,03; Conductivity [mS/cm]= 1,8; COD [mg/l]= 2300. COD [mg/l]= 950 (for T154) TSS [mg/l]= 70 |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 48; pH [-]= 7,8; Conductivity [mS/cm]= 0,3; COD [mg/l]= 1460. COD [mg/l]= 950 (for T154) TSS [mg/l]= 75 |  |
| Water type W3 : equip. volume Non ionic surfactant (2057):3 g/l. Steam type S1 | 3rd bath T=60°C; t=40 min Indirect heating |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 40; pH [-]= 7,2; Conductivity [mS/cm]= 0,2; COD [mg/l]= 2260. TSS [mg/l]= 30 |  |
| Water type W3: equip. volume | Washing |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,2; Conductivity [mS/cm]= 0,18; COD [mg/l]= 150. TSS [mg/l]= 0 |  |

- Notes:

- F 3.4 Desizing in Torpedo at 90°C

| Department | Preparation |
| --- | --- |
| Fabric | PL |
| Process | Desizing in Torpedo at 90°C |
| Equipment | Torpedo |
| Item | T151-T153-T154-T155 |
| Run time (h) | 3,30-4,30 |
| Number of run/yr | 38-3-16-1 |
| Processed fabric (kg/yr) | 5644-506-910-66 |
| Processed fabric per run (kg) | 148-169-57-66 |

| Water type W4 :equip volume Non ionic surfactant (1058): 4 g/l; Dispersant agent (2058): 1 g/l; Soda Solvay (1016): 0,5 g/l. Steam type S1 | 1st bath T=90°C t=30 min Indirect heating |  |  |  |
| --- | --- | --- | --- | --- |
| Water type W4 : 1500 l | 1st continuous washing |  | Discharge type D1: 1500 l T [°C]=50; pH [-]=9,64; Conductivity [mS/cm]=0,96; COD [mg/l]=2380; COD [mg/l]=1010 (for T154); TSS [mg/l]=50. |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]=42; pH [-]=9,55; Conductivity [mS/cm]=0,62; COD [mg/l]=1500; COD [mg/l]=1010 (for T154); TSS [mg/l]=30. |  |
| Water type W4 :equip volume Non ionic surfactant (1058): 4 g/l; Dispersant agent (2058): 1 g/l; Soda Solvay (1016): 0,5 g/l. Steam type S1 | 2nd Bath T=90-110°C t=30 min Indirect heating |  |  |  |
| Water type W4 :1500 l | 2nd continuous washing |  | Discharge type D1: 1500 l T [°C]=54; pH [-]=10,37; Conductivity [mS/cm]=1,04; COD [mg/l]=1850; COD [mg/l]=750 (for T154); TSS [mg/l]=50. |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]=42; pH [-]=10,18; Conductivity [mS/cm]=0,66; COD [mg/l]=1200; COD [mg/l]=750 (for T154); TSS [mg/l]=55. |  |
| Water type W3: equip. volume | Washing |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]=16; pH [-]=8,76; Conductivity [mS/cm]=0,21; COD [mg/l]=150; TSS [mg/l]= 10. |  |

- Notes:

- F 3.5 Desizing in Overflow at 90°C

| Department | Preparation |
| --- | --- |
| Fabric | PL |
| Process | Desizing in Overflow at 90°C |
| Equipment | Overflow |
| Item | O192-O193-O194 |
| Run time (h) | 3,50 |
| Number of run/yr | 0-175-19 |
| Processed fabric (kg/yr) | 0-9400-1099 |
| Processed fabric per run (kg) | 0-54-58 |

| Water type W4:equip volume Non ionic surfactant (2057):4 g/l; Lubricating agent (1057):2 g/l. Steam type S1 | 1st Bath T=90°C t=40 min Indirect heating |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Water type W4: 500 l | Continuous washing |  |  |  | Discharge type D1: 500 l T [°C]=56; pH [-]=7,77; Conductivity [mS/cm]=0,22; COD [mg/l]=7050; COD [mg/l]=5720 (for O192 O193); TSS [mg/l]=363. |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]=54; pH [-]=8,04; Conductivity [mS/cm]=0,20; COD [mg/l]=6100; COD [mg/l]=5500 (for O192 O193); TSS [mg/l]=39. |  |  |
| Water type W4: equip. volume | 1st Washing |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]=40; pH [-]=6,83; Conductivity [mS/cm]=0,19; COD [mg/l]=880; TSS [mg/l]=31. |  |  |
| Water type W4:equip volume Non ionic surfactant (2057):1 g/l. Steam type S1 | 2nd bath T=60°C t=30 min Indirect heating |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]=43; pH [-]=7,34; Conductivity [mS/cm]=0,18; COD [mg/l]=1350; TSS [mg/l]=25. |  |  |
| Water type W3 : equip. volume | 2nd washing |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]=22; pH [-]=7,05; Conductivity [mS/cm]=0,18; COD [mg/l]=200; TSS [mg/l]=11. |  |  |
| Water type W3 : equip. volume | Filling (for fabric discharge) |  |  |  |  |  |  |
|  | Filling discharge (50% of total run) |  |  |  | Discharge type D1: equip. volume T [°C]= 17; pH [-]= 7,8; Conductivity [mS/cm]= 0,21; COD [mg/l]= 50; TSS [mg/l]= 0. |  |  |

- Notes:

- F4: Double scouring.

- F 4.1 Double scouring in torpedo with continuos washing at 60°C

| Department | Preparation |
| --- | --- |
| Fabric | F-PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Double scouring in Torpedo with continuos washing at 60°C |
| Equipment | Torpedo |
| Item | T151,T153,T154,T155 |
| Run time (h) | 4,00 |
| Number of run/yr | 303-23-16-0 |
| Processed fabric (kg/yr) | 25000-3675-620-0 |
| Processed fabric per run (kg) | 82-160-39-0 |

| Water type W4:equip. volume Non ionic surfactant (1058)=5 g/l; Sequestering agent (1071)=0,5 g/l. Steam type S1 | 1st bath T=60°C t=50 min Indirect heating |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Water type W3:1500 l | 1st continuous washing |  |  |  | Discharge type D1: 1500 l T [°C]=53; pH [-]=9,79; Conductivity [mS/cm]=0,44; COD [mg/l]=2210; COD [mg/l]=940 (for T154); TSS [mg/l]=70. |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]=40; pH [-]=9,71; Conductivity [mS/cm]=0,37; COD [mg/l]=1450; COD [mg/l]=940 (for T154); TSS [mg/l]=25. |  |  |  |  |  |  |
| Water type W4:equip. volume Non ionic surfactant (2057)=4,5 g/l. Steam type S1 |  | 2nd bath T=60°C t=60 min Indirect heating |  |  |  |  |  |  |  |  |  |
| Water type W4: 1500 l |  | 2nd continuous washing |  |  |  | Discharge type D1: 1500 l T [°C]=55; pH [-]=9,08; Conductivity [mS/cm]=0,22; COD [mg/l]=4600; COD [mg/l]=2000 (for T154); TSS [mg/l]=48. |  |  |  |  |  |
|  |  |  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]=36; pH [-]=8,71; Conductivity [mS/cm]=0,19; COD [mg/l]=2810; COD [mg/l]=2000 (for T154); TSS [mg/l]=35. |  |  |  |  |
| Water type W4:equip volume Acetic acid (2006): 1,3 g/l Steam type S1 | 3rd bath T=30°C t=10 min |  |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]=16; pH [-]=3,86; Conductivity [mS/cm]=0,29; COD [mg/l]=1050; TSS [mg/l]=10. |  |  |  |  |  |  |
| Water type W3:equip volume | Washing |  |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]=12; pH [-]=4,78; Conductivity [mS/cm]=0,18; COD [mg/l]=160; TSS [mg/l]=0. |  |  |  |  |  |  |

- Notes:

For   FLAX/PL   Fabric:   see An.D

- F 4.2 Double scouring in Torpedo at 60°C

| Department | Preparation |
| --- | --- |
| Fabric | F-PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Double scouring in Torpedo at 60°C |
| Equipment | Torpedo |
| Item | T155 |
| Run time (h) | 5,10 |
| Number of run/yr | 282 |
| Processed fabric (kg/yr) | 27303 |
| Processed fabric per run (kg) | 97 |

| Water type W4: equip. volume Non ionic surfactant (1058)=5 g/l; Sequestering agent (1071)=0,5 g/l. Steam type S1 | 1st bath T=60°C t=40 min Indirect heating |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  |  | Discharge type D1: equip volume T [°C]= 59; pH [-]= 9,8; Conductivity [mS/cm]= 0,45; COD [mg/l]= 2650. TSS [mg/l]= 75 |  |  |  |  |  |  |
| Water type W3:equip. volume |  | 1st washing |  |  |  |  |  |  |  |  |  |
|  |  |  | Discharge |  |  |  | Discharge type D1: equip volume T [°C]= 35; pH [-]= 8,7; Conductivity [mS/cm]= 0,21; COD [mg/l]= 2300. TSS [mg/l]= 58 |  |  |  |  |
| Water type W4: equip volume Non ionic surfactant (2057)=4,5 g/l. | 2nd bath T=60°C t=40 min Indirect heating |  |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip volume T [°C]= 50; pH [-]= 9,05; Conductivity [mS/cm]= 0,37; COD [mg/l]= 5250. TSS [mg/l]= 25 |  |  |  |  |  |  |
| Water type W4:equip volume | 2nd washing |  |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip volume T [°C]= 31; pH [-]= 8,6; Conductivity [mS/cm]= 0,25; COD [mg/l]= 2050. TSS [mg/l]= 80 |  |  |  |  |  |  |
| Water type W4 equip volume Acetic acid (2006): 1,3 g/l. | 3rd bath T=40°C t=15 min |  |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip volume T [°C]= 31; pH [-]= 3,8; Conductivity [mS/cm]= 0,19; COD [mg/l]= 980. TSS [mg/l]= 40 |  |  |  |  |  |  |
| Water type W3 equip volume | 3rd washing |  |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip volume T [°C]= 21; pH [-]= 7,06; Conductivity [mS/cm]= 0,19; COD [mg/l]= 200. TSS [mg/l]= 0 |  |  |  |  |  |  |

- Notes:

For   FLAX/PL   Fabric:   see An.D

- F.5: Special scouring

- F 5.1 Special scouring in Jigger at 90°C.

| Department | Preparation |
| --- | --- |
| Fabric | FLAX-PL-CO/PL-FLAX/PL |
| Process | Special scouring in Jigger at 90°C |
| Equipment | Jigger |
| Item | J145 |
| Run time (h) | 2,30 |
| Number of run/yr | 350 |
| Processed fabric (kg/yr) | 32467 |
| Processed fabric per run (kg) | 93 |

| Water type W4:equip. volume Surfactant (1070): 16 g/l: Sequestering agent (1071): 4 g/l; Sodium carbonate (1016): 1 g/l. Steam type S1 | 1st bath T=90°C t=60 min Indirect heating |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Water type W3:2000 l | Continuous washing |  |  |  | Discharge type D1: 2000 l T [°C]= 76; pH [-]= 8,5; Conductivity [mS/cm]= 0,56; COD [mg/l]= 7700. TSS [mg/l]= 85 |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]= 68; pH [-]= 8,3; Conductivity [mS/cm]= 0,31; COD [mg/l]= 3750. TSS [mg/l]= 28 |  |  |  |  |  |  |
| Water type W3:equip. volume |  | Washing |  |  |  |  |  |  |  |  |  |
|  |  |  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]= 28; pH [-]= 7,6; Conductivity [mS/cm]= 0,22; COD [mg/l]= 500. TSS [mg/l]= 15 |  |  |  |  |
| Water type W3 :equip volume | Filling (for fabric discharge) |  |  |  |  |  |  |  |  |  |  |
|  | Filling discharge (50% of total run) |  |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,6; Conductivity [mS/cm]= 0,19; COD [mg/l]= 200. TSS [mg/l]= 0 |  |  |  |  |  |  |

- Notes:

For   FLAX/PL   Fabric:   see An.D

- F 5.2 Special scouring in Torpedo at 70°C

| Department | Preparation |
| --- | --- |
| Fabric | F-PL-CO/PL-FLAX/PL |
| Process | Special scouring in Torpedo at 70°C |
| Equipment | Torpedo |
| Item | T151 |
| Run time (h) | 2,30 |
| Number of run/yr | 18 |
| Processed fabric (kg/yr) | 467 |
| Processed fabric per run (kg) | 26 |

| Water type W4:equip. volume Surfactant (1070): 5 g/l: Soda Solvay (1016): 1,5 g/l; Sequestering agent (1071): 1 g/l. Steam type S1 | 1st bath T=70°C t=60 min Indirect heating |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Water type W3:1500 l T [°C]= 40 | Continuous washing |  |  |  | Discharge type D1: 1500 l T [°C]= 58; pH [-]= 8,5; Conductivity [mS/cm]= 0,56; COD [mg/l]= 3800. TSS [mg/l]= 55 |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]= 51; pH [-]= 8,3; Conductivity [mS/cm]= 0,31; COD [mg/l]= 2420. TSS [mg/l]= 27 |  |  |  |  |  |  |
| Water type W4:equip. volume |  | 1st washing |  |  |  |  |  |  |  |  |  |
|  |  |  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]= 28; pH [-]= 7,6; Conductivity [mS/cm]= 0,22; COD [mg/l]= 500. TSS [mg/l]= 15 |  |  |  |  |
| Water type W4:equip volume Non ionic surfactant (2057): 4 g/l. Steam type S1 | 2nd bath T=60°C t=60 min Indirect heating |  |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]= 41; pH [-]= 8,2; Conductivity [mS/cm]= 0,54; COD [mg/l]= 2150. TSS [mg/l]= 50 |  |  |  |  |  |  |
| Water type W3:equip volume Acetic acid (2006): 1 g/l. | 3rd bath T=10°C t=10 min |  |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 3,8; Conductivity [mS/cm]= 0,21; COD [mg/l]= 980. TSS [mg/l]= 10 |  |  |  |  |  |  |
| Water type W4:equip volume | 2nd washing |  |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]= 21; pH [-]= 7,06; Conductivity [mS/cm]= 0,19; COD [mg/l]= 350. TSS [mg/l]= 10 |  |  |  |  |  |  |

- Notes:

For   FLAX/PL   Fabric:   see An.D

- F.6: Bleaching.

- F 6.1 Bleaching in Jigger at 90°C

| Department | Preparation |
| --- | --- |
| Fabric | F- CO/PL-FLAX/PL-SILK/PL |
| Process | Bleaching in Jigger at 90°C |
| Equipment | Jigger |
| Item | J144,J145,C146 |
| Run time (h) | 4,00 |
| Number of run/yr | 185-82-4 |
| Processed fabric (kg/yr) | 25067-4145-301 |
| Processed fabric per run (kg) | 135-50-75 |

| Water type W4:equip volume Non ionic surfactant (1058):7 g/l. Steam type S1 | 1st bath T=90°C t=30 min Indirect heating |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 68; pH [-]= 8,1; Conductivity [mS/cm]= 0,54; COD [mg/l]= 3810. TSS [mg/l]= 35 |  |  |  |  |
| Water type W4:equip volume Caustic soda (1011):7 g/l; Antifoaming agent (2077):0,5 g/l; Non ionic surfactant (1058):1,5 g/l; Hydrogen peroxide 130 vol (1010): 13 g/l. Steam type S1 | 2nd bath T=98°C t=30 min Indirect heating |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 65; pH [-]= 7,8; Conductivity [mS/cm]= 0,21; COD [mg/l]= 950. TSS [mg/l]= 41 |  |  |  |  |
| Water type W3 2840-1050-1570 l | Continuous washing (1 lysis) |  |  | Discharge type D1: 2830-1050-1570 T [°C]= 40; pH [-]= 7,8; Conductivity [mS/cm]= 0,19; COD [mg/l]= 320. TSS [mg/l]= 27 |  |  |  |  |
| Water type W4 :equip volume | Washing (2 lysis) |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 21; pH [-]= 7,06; Conductivity [mS/cm]= 0,21; COD [mg/l]= 200. TSS [mg/l]= 10 |  |  |  |  |
| Water type W3: equip. volume |  | Filling (for fabric discharge) |  |  |  |  |  |  |
|  |  | Filling discharge (50% of total run) |  |  | Discharge type D1: equip. volume T [°C]= 19; pH [-]= 7,2; Conductivity [mS/cm]= 0,21; COD [mg/l]= 50. TSS [mg/l]= 5 |  |  |  |

Notes:

For   FLAX/PL   Fabric:   see An.D

- F 6.2 Bleaching in Torpedo at 80°C

| Department | Preparation |
| --- | --- |
| Fabric | CO/PL-FLAX/PL-SILK/PL |
| Process | Bleaching in Torpedo at 80°C |
| Equipment | Torpedo |
| Item | T151,T153,T154,T155 |
| Run time (h) | 4,50 |
| Number of run/yr | 9-2-5-0 |
| Processed fabric (kg/yr) | 1221-206-256-0 |
| Processed fabric per run (kg) | 136-103-51-0 |

| Water type W4:equip volume Non ionic surfactant (1058): 5 g/l; Hydrogen peroxide 130 vol (1010): 2 g/l; Antifoaming agent (2077): 0,5 g/l; Caustic soda (1011): 0,5 g/l; Sequestering agent (1071): 1 g/l Steam type S1 | 1st bath T=80°C t=30 min Indirect heating |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Water type W4:1500 l | 1st continuous washing |  |  | Discharge type D1: 1500 l T [°C]= 61; pH [-]= 8,9; Conductivity [mS/cm]= 0,54; COD [mg/l]= 2150. COD [mg/l]= 780 (for T154) TSS [mg/l]= 45 |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 50; pH [-]= 8,1; Conductivity [mS/cm]= 0,25; COD [mg/l]= 1380. COD [mg/l]= 780 (for T154) TSS [mg/l]= 32 |  |  |  |
| Water type W4:equip volume Non ionic surfactant (2057): 4 g/l. Steam type S1 | 2nd bath T=90°C t=30 min Indirect heating |  |  |  |  |  |  |
| Water type W4:1500 l | 2nd continuous washing |  |  | Discharge type D1: 1500 l T [°C]= 65; pH [-]= 8,3; Conductivity [mS/cm]= 0,51; COD [mg/l]= 4500. COD [mg/l]= 1520 (for T154) TSS [mg/l]= 38 |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 61; pH [-]= 7,8; Conductivity [mS/cm]= 0,21; COD [mg/l]= 2950. COD [mg/l]= 1520 (for T154) TSS [mg/l]= 25 |  |  |  |
| Water type W4:equip volume Non ionic surfactant (2057): 2 g/l. Steam type S1 | 3rd bath T=90°C t=30 min Indirect heating |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 61; pH [-]= 8,1; Conductivity [mS/cm]= 0,5; COD [mg/l]= 2800. TSS [mg/l]= 18 |  |  |  |
| Water type W3:equip volume | Washing |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 21; pH [-]= 7,9; Conductivity [mS/cm]= 0,2; COD [mg/l]= 160. TSS [mg/l]= 5 |  |  |  |

- Notes:

For   FLAX/PL   Fabric:   see An.D

- F 7: Bleaching before dyeing

- F 7.1 Bleaching before dyeing in Overflow at 90°C

| Department | Preparation |
| --- | --- |
| Fabric | F- CO/PL-FLAX/PL-SILK/PL |
| Process | Bleaching before dyeing in Overflow at 90°C |
| Equipment | Overflow |
| Item | O192 |
| Run time (h) | 6,00 |
| Number of run/yr | 49 |
| Processed fabric (kg/yr) | 1550 |
| Processed fabric per run (kg) | 32 |

| Water type W4 :equipment volume Antifoaming agent (2077): 0,5 g/l; Non ionic surfactant (1058): 1,5 g/l; Lubricating agent (1057): 2 g/l; Hydrogen peroxide 130 vol (1010): 3,5 g/l; Caustic soda (1011): 3,5 g/l. Steam type S1 | 1st bath T=90°C t=40 min Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Water type W3: 1000 l T [°C]=10. | Continuous washing |  | Discharge type D1: 1000 l T [°C]= 68; pH [-]= 9; Conductivity [mS/cm]= 0,92; COD [mg/l]= 2800. TSS [mg/l]= 60 |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 51; pH [-]= 8,1; Conductivity [mS/cm]= 0,4; COD [mg/l]= 2050. TSS [mg/l]= 25 |  |  |
| Water type W3 2:equip volume T [°C]=20. | Washing |  |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 41; pH [-]= 7,8; Conductivity [mS/cm]= 0,3; COD [mg/l]= 600. TSS [mg/l]= 18 |  |  |
| Water type W4:equip volume Acetic acid (2006): 1 g/l. Steam type S1 | 2nd bath T=60°C t=10 min Indirect heating |  |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 40; pH [-]= 3,86; Conductivity [mS/cm]= 0,21; COD [mg/l]= 1150. TSS [mg/l]= 10 |  |  |
| Water type W3 :equip volume | Filling (for fabric discharge) |  |  |  |  |
|  | Filling discharge (50% of total run) |  | Discharge type D1: equip. volume T [°C]= 19; pH [-]= 6,9; Conductivity [mS/cm]= 0,21; COD [mg/l]= 200. TSS [mg/l]= 5 |  |  |

- Notes:

For   FLAX/PL   Fabric:   see An.D

- F 8: Barking

- F 8.1 Barking in Torpedo at 110°-130°C

| Department | Preparation |
| --- | --- |
| Fabric | PL |
| Process | Barking in Torpedo at 110°-130°C |
| Equipment | Torpedo |
| Item | T151,T153,T154,T155 |
| Run time (h) | 5,00-5,20 |
| Number of run/yr | 46.0-1-0 |
| Processed fabric (kg/yr) | 5283-0-58-0 |
| Processed fabric per run (kg) | 115-0-58-0 |

| Water type W4:equip volume Caustic soda (1011): 7,5 g/l; Steam type S1 | 1st bath T=110-130°C t=20 min Indirect heating |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 71; pH [-]= 11; Conductivity [mS/cm]= 0,51; COD [mg/l] 6800 TSS [mg/l]= 55 |  |  |  |
| Water type W4:equipment volume | 1st washing |  |  |  |  |  |  |  |
|  |  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 31; pH [-]= 8,3; Conductivity [mS/cm]= 0,21; COD [mg/l]= 1750. TSS [mg/l]= 28 |  |  |  |
| Water type W4:equip volume Non ionic surfactant (1058): 1 g/l; Steam type S1 | 2nd bath T=60°C t=20 min Indirect heating |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 48; pH [-]= 7,9; Conductivity [mS/cm]= 0,5; COD [mg/l]= 930. TSS [mg/l]= 12 |  |  |  |  |
| Water type W4:equip volume Oxalic acid (1007): 1 g/l. Steam type S1 | 3rd bath T=80°C t=20 min Indirect heating |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 51; pH [-]= 45; Conductivity [mS/cm]= 0,3; COD [mg/l]=450 TSS [mg/l]= 10 |  |  |  |  |
| Water type W3:equip volume | 2nd washing |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 40; pH [-]= 7,02; Conductivity [mS/cm]= 0,2; COD [mg/l]= 180. TSS [mg/l]= 0 |  |  |  |  |

- Notes:

Barking at 110°C: 44% of total run.

Barking at 130°C: 56% of total run.

For   FLAX/PL   Fabric:   see An.D