- An.g: Dyeing - Process scheme.

- G.1:Light disperse dyeing.

- G 1.1 Light disperse dyeing in Torpedo

- G 1.2 Light disperse dyeing in Overflow

- G.2:Medium disperse dyeing.

- G 2.1 Medium disperse dyeing in Torpedo

- G.2.2 Medium disperse dyeing in Overflow

- G.3:Dark disperse dyeing.

- G 3.1 Dark disperse dyeing in Torpedo

- G.4:Light disperse + indanthrene dyeing.

- G 4.1 Light disperse + indanthrene dyeing

- G.5:Light direct dyeing.

- G 5.1 Light direct dyeing in Jigger

- G 5.2 Light direct dyeing in Overflow

- G.6:Dark direct dyeing.

- G 6.1 Dark direct dyeing in Jigger

- G 6.2 Dark direct dyeing in Overflow

- G.7:Light reactive dyeing.

- G 7.1 Light reactive dyeing in Jigger

- G 7.2 Light reactive dyeing in Overflow

- G.8:Dark reactive dyeing.

- G 8.1 Dark reactive dyeing in jigger

- G 8.2 Dark reactive dyeing in Overflow

- G.9:Printed washing.

- G 9.1 Printed washing in Jigger

- G 9.2 Printede washing in Overflow

- G.10:Printed triple washing.

- G 10.1 Printed triple washing in Overflow

- G.11:Printed triple washing + stripping.

- G 11.1 Printed triple washing + shipping in Overflow

- G.12:Devorè printed washing.

- G 12.1 Devorè printed washing in Overflow

- G.13:Washing for printing panels fabric..

- G 13.1 Washing for printing panels in Overflow

- G.14:Equipment washing

- G 14.1 Equipment washing – Jigger

- G 14.2 Equipment washing – Torpedo

- G 14.3 Equipment washing - Overflow

- G.1:Light disperse dyeing.

- G 1.1 Light disperse dyeing in Torpedo

| Department | Dyeing |
| --- | --- |
| Fabric | PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Light disperse dyeing in torpedo |
| Equipment | Torpedo |
| Item | T151-T153-T154-T155 |
| Run time (h) | 4.00-5.30 |
| Number of run/yr | 137-43-271-0 |
| Processed fabric (kg/yr) | 12330-3783-14555-0 |
| Processed fabric per run (kg) | 90-88-54-0 |

| Water type W4:equip volume Acetic acid (2006)= 1 g/l; Carrier (2036)= 1 g/l; Disperse dyestuffs<0,05% Steam type S1 | Bath T=110-120-130°C; t=30 min. Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 71; pH [-]= 3,69; Conductivity [mS/cm]= 0,91; COD [mg/l]= 1500. TSS [mg/l]= 35 |  |  |
| Water type W3: equip. volume | Washing |  |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 22; pH [-]= 4,82; Conductivity [mS/cm]= 0,28; COD [mg/l]= 450. TSS [mg/l]= 10 |  |  |

- Notes:

Light disperse dyeing at 110°C: 47% of total run.

Light disperse dyeing at 120°C: 8% of total run.

Light disperse dyeing at 130°C: 45% of total run.

For FLAX-PES fabric: see An.D

G 1.2 Light disperse dyeing in overflow

| Department | Dyeing |
| --- | --- |
| Fabric | PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Light disperse dyeing in overflow |
| Equipment | Overflow |
| Item | O192-O193-O194 |
| Run time (h) | 5,00-6,00 |
| Number of run/yr | 0-163-91 |
| Processed fabric (kg/yr) | 0-8781-455 |
| Processed fabric per run (kg) | 0-54-5 |

| Water type W4:equip volume Lubricating agent (1057)=2,5 g/l; Acetic acid (2006)= 1 g/l; Carrier (2068)= 1 g/l. Disperse dyestuffs < 0,05% Steam type S1 |  | Bath T=100-110-130°C; t=30-40 min. Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Water type W3: 500 l; |  | Continuous washing |  | Discharge type Dl: 500 l T [°C]= 56; pH [-]= 6,11; Conductivity [mS/cm]= 0,23; COD [mg/l]= 3050. TSS [mg/l]= 58 |  |  |
|  |  | Discharge |  | Discharge type D1: equip. volume T [°C]= 50; pH [-]= 3,9; Conductivity [mS/cm]= 0,23; COD [mg/l]= 2200. TSS [mg/l]= 31 |  |  |
| Water type W3: equip. volume |  | Washing |  |  |  |  |
|  |  | Discharge |  | Discharge type D1: equip. volume T [°C]= 21; pH [-]= 6,7; Conductivity [mS/cm]= 0,17; COD [mg/l]= 200. TSS [mg/l]= 10 |  |  |
| Water type W3: equip. volume |  |  | Filling (for fabric discharge) |  |  |  |
|  |  |  | Filling discharge (30% of total run) |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,3; Conductivity [mS/cm]= 0,17; COD [mg/l]= 80; TSS [mg/l]= 0. |  |

- Notes:

Light disperse dyeing at 100°C: 12% of total run.

Light disperse dyeing at 110°C: 67% of total run.

Light disperse dyeing at 130°C: 21% of total run.

- For FLAX-PES fabric: see An.D

- G.2: Medium disperse dyeing.

- G 2.1 Medium disperse dyeing in torpedo

| Department | Dyeing |
| --- | --- |
| Fabric | PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Medium disperse dyeing in torpedo |
| Equipment | Torpedo |
| Item | T151-T153-T154-T155 |
| Run time (h) | 4,30-5,30 |
| Number of run/yr | 106-63-141-3 |
| Processed fabric (kg/yr) | 7642-3856-7583-113 |
| Processed fabric per run (kg) | 72-61-56-38 |

| Water type W4:equip volume Acetic acid (2006)=1 g/l; Carrier (2068)=1 g/l; 0,05%<Disperse dyestuffs<1% Reducing agent (2067)= 3 g/l. Steam type S1 | Bath T=110-130°C; t=30 min. Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 70; pH [-]= 4,07; Conductivity [mS/cm]= 0,76; COD [mg/l]= 1830. TSS [mg/l]= 75 |  |  |
| Water type W3: equip. volume | Washing |  |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 17; pH [-]= 5,95; Conductivity [mS/cm]= 0,19; COD [mg/l]= 800. TSS [mg/l]= 25 |  |  |

- Notes:

- For FLAX-PES fabric: see An.D

- G 2.2 Medium disperse dyeing in overflow

| Department | Dyeing |
| --- | --- |
| Fabric | PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Medium disperse dyeing in overflow (DOS 23F) |
| Equipment | Overflow |
| Item | O192-O193-O194 |
| Run time (h) | 5,00 |
| Number of run/yr | 0-23-13 |
| Processed fabric (kg/yr) | 0-1216-663 |
| Processed fabric per run (kg) | 0-53-51 |

| Water type W4:equip volume Acetic acid (2006)=1 g/l; Carrier (2068)=1 g/l; Carrier (2033) = 0,22 g/l 0,05%<Disperse dyestuffs<1% Reducing agent (2067)= 3 g/l. Steam type S1 | Bath T=110°C; t=40 min. Indirect heating |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 68; pH [-]= 6,5; Conductivity [mS/cm]= 2,1; COD [mg/l]= 2020. TSS [mg/l]= 80 |  |  |  |  |
| Water type W4: equip. volume | Washing |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 48; pH [-]= 7,1; Conductivity [mS/cm]= 1,3; COD [mg/l]= 510. TSS [mg/l]= 30 |  |  |  |  |
| Water type W3: equip. volume |  | Filling (for fabric discharge) |  |  |  |  |  |  |
|  |  | Filling discharge (30% of total run) |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,3; Conductivity [mS/cm]= 0,17; COD [mg/l]= 150; TSS [mg/l]= 0. |  |  |  |

- Notes:

Medium disperse dyeing at 110°C: 30% of total run.

Medium disperse dyeing at 130°C: 70% of total run.

- For FLAX-PES fabric: see An.D

- G.3: Dark disperse dyeing.

- G 3.1 Dark disperse dyeing in torpedo

| Department | Dyeing |
| --- | --- |
| Fabric | PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Dark disperse dyeing in torpedo (DOS22S) |
| Equipment | Torpedo |
| Item | T151-T153-T154-T155 |
| Run time (h) | 4,30-5,30 |
| Number of run/yr | 31-0-33-0 |
| Processed fabric (kg/yr) | 2340-0-1757-0 |
| Processed fabric per run (kg) | 75-0-53-0 |

| Water type W4:equip volume Acetic acid (2006)=1 g/l; Carrier (2068)=1 g/l; Disperse dyestuffs>1% Reducing agent (2067)= 3 g/l. Steam type S1 | Bath T=110°C; t=30 min. Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 75; pH [-]= 7,3; Conductivity [mS/cm]= 2,3; COD [mg/l]= 1750. TSS [mg/l]= 85 |  |  |
| Water type W3: equip. volume | Washing |  |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 68; pH [-]= 7,3; Conductivity [mS/cm]= 1,8; COD [mg/l]= 400. TSS [mg/l]= 10 |  |  |

- Notes:

- For FLAX-PES fabric: see An.D

- G.4: Light disperse + indanthrene dyeing.

- G 4.1 Light disperse + indanthrene dyeing in  torpedo

| Department | Dyeing |
| --- | --- |
| Fabric | PL |
| Process | Light disperse + indanthrene dyeing in torpedo (DOS63S) |
| Equipment | Torpedo |
| Item | T151 |
| Run time (h) | 5,30 |
| Number of run/yr | 27 |
| Processed fabric (kg/yr) | 2854 |
| Processed fabric per run (kg) | 106 |

| Water type W4:equip volume Sequestering agent (1071) = 1 g/l Acetic acid (2006) = 1 g/l Dispersant agent (1043) = 1 g/l Disp dyest + indanthrene< 0,05% Caustic Soda (1011) = 20 g/l Sodium Hydrousulphide = 10 g/l Equalizing agent (2030) = 1 g/l Steam type S1 | 1st bath T=130°C; t=30 min. Indirect heating |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Water type W3: 7000 l; | 1st continuous washing |  |  | Discharge type Dl: 7000 l T [°C]= 74; pH [-]= 8,3; Conductivity [mS/cm]= 1,8; COD [mg/l]= 1140. TSS [mg/l]= 80 |  |  |  |  |
| Oxidating agent (2071) = 5 g/l Detergent (2026) = 1 g/l Steam type S1 | 2nd bath T=98°C; t=20 min. Indirect heating |  |  |  |  |  |  |  |
| Water type W3: 1500 l | 2nd continuous washing |  |  | Discharge type Dl: 1500 l T [°C]= 69; pH [-]= 7,9; Conductivity [mS/cm]= 1,9; COD [mg/l]= 1480. TSS [mg/l]= 75 |  |  |  |  |
|  |  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 65; pH [-]= 7,6; Conductivity [mS/cm]= 1,5; COD [mg/l]= 510. TSS [mg/l]= 15 |  |  |  |
| Water type W3: equip. volume | Washing |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 60; pH [-]= 7,6; Conductivity [mS/cm]= 0,5; COD [mg/l]= 520. TSS [mg/l]= 12 |  |  |  |  |

- Notes:

- G.5:Light direct dyeing.

- G 5.1 Light direct dyeing in Jigger

| Department | Dyeing |
| --- | --- |
| Fabric | FLAX-CO/PL-FLAX/PL |
| Process | Light direct dyeing in jigger (51J) |
| Equipment | Jigger |
| Item | J144-J145-C146 |
| Run time (h) | 4,00 |
| Number of run/yr | 26-32-16 |
| Processed fabric (kg/yr) | 2933-1992-1115 |
| Processed fabric per run (kg) | 113-62-70 |

| Water type W4:equip volume Sodium sulphate (2008) = 1 g/l Direct dyestuffs < 0,05% Steam type S1 | 1st bath T=90°C; t=60 min. Indirect heating |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 61; pH [-]= 3,48; Conductivity [mS/cm]= 0,52; COD [mg/l]= 370. TSS [mg/l]= 50 |  |  |  |  |
| Water type W3: 2120-1180-1320 l | Continuous washing (1 lysis) |  |  | Discharge type Dl: 2120-1180-1320 l T [°C]= 40; pH [-]= 6,62; Conductivity [mS/cm]= 0,31; COD [mg/l]= 150. TSS [mg/l]= 25 |  |  |  |  |
| Water type W4: equip. volume | Washing (2 lysis) |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 16; pH [-]= 7,1; Conductivity [mS/cm]= 0,18; COD [mg/l]= 80. TSS [mg/l]= 12 |  |  |  |  |
| Water type W4: equip. volume | Filling (for fabric discharge) |  |  |  |  |  |  |  |
|  |  | Filling discharge (50% of total run) |  |  | Discharge type D1: equip. volume T [°C]= 38; pH [-]= 7,3; Conductivity [mS/cm]= 0,17; COD [mg/l]= 50; TSS [mg/l]= 0. |  |  |  |

- Notes:

- For FLAX-PES fabric: see An.D

- G 5.2 Light direct dyeing in overflow

| Department | Dyeing |
| --- | --- |
| Fabric | FLAX-CO/PL-FLAX/PL-SILK/PL |
| Process | Light direct dyeing in overflow (DOS49F) |
| Equipment | Overflow |
| Item | O192-O193-O194 |
| Run time (h) | 6,30 |
| Number of run/yr | 33-0-0 |
| Processed fabric (kg/yr) | 977-0-0 |
| Processed fabric per run (kg) | 30-0-0 |

| Water type W4:equip volume Sodium Sulphate (2008) = 0,5 g/l Direct dyestuffs < 0,05% Steam type S1 | Bath T=90°C; t=30 min. Indirect heating |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 78; pH [-]= 8,2; Conductivity [mS/cm]= 2,9; COD [mg/l]= 370 TSS [mg/l]= 10 |  |  |  |  |
| Water type W4: equip. volume | Washing |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 61; pH [-]= 7,6; Conductivity [mS/cm]= 1,8; COD [mg/l]= 150. TSS [mg/l]= 0 |  |  |  |  |
| Water type W3: equip. volume |  | Filling (for fabric discharge) |  |  |  |  |  |  |
|  |  | Filling discharge (50% of total run) |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,3; Conductivity [mS/cm]= 0,17; COD [mg/l]= 50; TSS [mg/l]= 0. |  |  |  |

- Notes:

- For FLAX-PES fabric: see An.D

- G 6.1 Dark direct dyeing in Jigger

| Department | Dyeing |
| --- | --- |
| Fabric | FLAX-CO/PL-FLAX/PL |
| Process | Dark direct dyeing in jigger (51J) |
| Equipment | Jigger |
| Item | J144-J145-C146 |
| Run time (h) | 4,00 |
| Number of run/yr | 17-21-10 |
| Processed fabric (kg/yr) | 1955-1328-743 |
| Processed fabric per run (kg) | 115-63-74 |

| Water type W4:equip volume Sodium sulphate (2008) = 1 g/l Direct dyestuffs > 0,05% Steam type S1 | 1st bath T=90°C; t=60 min. Indirect heating |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 61; pH [-]= 3,48; Conductivity [mS/cm]= 0,52; COD [mg/l]= 370. TSS [mg/l]= 50 |  |  |  |  |
| Water type W3: 2210-1320-1550 l | Continuous washing (1 lysis) |  |  | Discharge type Dl: 2210-1320-1550 l T [°C]= 40; pH [-]= 6,62; Conductivity [mS/cm]= 0,31; COD [mg/l]= 150. TSS [mg/l]= 25 |  |  |  |  |
| Water type W4: equip. volume | Washing (2 lysis) |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 16; pH [-]= 7,1; Conductivity [mS/cm]= 0,18; COD [mg/l]= 80. TSS [mg/l]= 12 |  |  |  |  |
| Water type W4: equip. volume Fixing agent (2019):1 g/l | Filling (for fabric discharge) |  |  |  |  |  |  |  |
|  |  | Filling discharge |  |  | Discharge type D1: equip. volume T [°C]= 41; pH [-]= 7,3; Conductivity [mS/cm]= 0,17; COD [mg/l]= 50; TSS [mg/l]= 0. |  |  |  |

- Notes:

- For FLAX-PES fabric: see An.D

- G 6.2 Dark direct dyeing in Overflow

| Department | Dyeing |
| --- | --- |
| Fabric | FLAX-CO/PL-FLAX/PL-SILK/PL |
| Process | Dark direct dyeing in overflow (DOS49F) |
| Equipment | Overflow |
| Item | O192-O193-O194 |
| Run time (h) | 6,30 |
| Number of run/yr | 22-0-0 |
| Processed fabric (kg/yr) | 651-0-0 |
| Processed fabric per run (kg) | 30-0-0 |

| Water type W4:equip volume Sodium Sulphate (2008) = 0,5 g/l Direct dyestuffs > 0,05% Steam type S1 | Bath T=90°C; t=30 min. Indirect heating |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 78; pH [-]= 8,2; Conductivity [mS/cm]= 2,9; COD [mg/l]= 370 TSS [mg/l]= 10 |  |  |  |  |
| Water type W3: equip. volume | Washing |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 61; pH [-]= 7,6; Conductivity [mS/cm]= 1,8; COD [mg/l]= 150. TSS [mg/l]= 0 |  |  |  |  |
| Water type W3: equip. volume |  | Filling (for fabric discharge) |  |  |  |  |  |  |
|  |  | Filling discharge (50% of total run) |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,3; Conductivity [mS/cm]= 0,17; COD [mg/l]= 80; TSS [mg/l]= 0. |  |  |  |

- Notes:

- For FLAX-PES fabric: see An.D

- G.7: Light reactive dyeing.

- G 7.1 Light reactive dyeing in Jigger

| Department | Dyeing |
| --- | --- |
| Fabric | FLAX-CO/PL-FLAX/PL |
| Process | Light reactive dyeing in jigger (91J) |
| Equipment | Jigger |
| Item | J144-J145-C146 |
| Run time (h) | 7,00 |
| Number of run/yr | 3-4-57 |
| Processed fabric (kg/yr) | 357-222-3051 |
| Processed fabric per run (kg) | 119-55-53 |

| Water type W4:equip volume Detergent (2046)= 1 g/l; Dispersant agent (2058)= 1 g/l; Sodium sulphate (2008)= 50 g/l; Soda Solvay (1016)= 3 g/l; Reactive dyestuffs<0,05%; Steam type S1 | 1st bath T=60°C; t=90 min. Indirect heating |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 54; pH [-]= 9; Conductivity [mS/cm]= 3,5; COD [mg/l]= 930. TSS [mg/l]= 25 |  |  |  |  |
| Water type W3: 2500-1150-1110 l | 1st Continuous washing (1 lysis) |  |  | Discharge type Dl: 2500-1150-1110 l T [°C]= 41; pH [-]= 7,8; Conductivity [mS/cm]= 1,7; COD [mg/l]= 170. TSS [mg/l]= 12 |  |  |  |  |
| Water type W4: equip. volume | 1st Washing |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 40; pH [-]= 7,6; Conductivity [mS/cm]= 0,34; COD [mg/l]= 130. TSS [mg/l]= 10 |  |  |  |  |
| Water type W4:equip volume Acetic acid (2006)= 1 g/l. | 2nd bath T=40°C; t=10 min. |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 38; pH [-]= 3,86; Conductivity [mS/cm]= 0,21; COD [mg/l]= 1050. TSS [mg/l]= 21 |  |  |  |  |
| Water type W4:equip volume Detergent (2048)= 4 g/l. Steam type S1 | 3rd bath T=80°C; t=60 min. Indirect heating |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 50; pH [-]= 8,1; Conductivity [mS/cm]= 0,19; COD [mg/l]= 1850. TSS [mg/l]= 50 |  |  |  |  |
| Water type W3: 2500-1150-1110 l | 2nd Continuous washing (1 lysis) |  |  | Discharge type Dl: 2500-1150-1110 l T [°C]= 38; pH [-]= 7,6; Conductivity [mS/cm]= 0,20; COD [mg/l]= 500. TSS [mg/l]= 21 |  |  |  |  |
| Water type W4: equip. volume | 2nd Washing |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 40; pH [-]= 7,6; Conductivity [mS/cm]= 0,21; COD [mg/l]= 220. TSS [mg/l]= 10 |  |  |  |  |
| Water type W3:equip volume | Filling (for fabric discharge) |  |  |  |  |  |  |  |
|  |  | Filling discharge (50% of total run) |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,3; Conductivity [mS/cm]= 0,17; COD [mg/l]= 80; TSS [mg/l]= 0. |  |  |  |

- Notes:

- For FLAX-PES fabric: see An.D

- G 7.2 Light reactive dyeing in overflow

| Department | Dyeing |
| --- | --- |
| Fabric | FLAX-CO/PL-FLAX/PL-SILK/PL |
| Process | Light reactive dyeing in overflow (52F-DOS52F-MOD52F) |
| Equipment | Overflow |
| Item | O192-O193-O194 |
| Run time (h) | 6,50 |
| Number of run/yr | 79-47-27 |
| Processed fabric (kg/yr) | 3314-2546-1039 |
| Processed fabric per run (kg) | 42-54-38 |

| Water type W4:equip volume Sodium solphate (2008) = 50 g/l Soda solvay (1016) = 3 g/l Detergent (2046) = 0,5 g/l Dispersant agent (2058) = 0,5 g/l Lubricating agent (1057) = 2 g/l Reactive dyestuffs<0,05% Steam type S1 | 1st bath T=60°C; t=90 min. Indirect heating |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]= 51; pH [-]= 7,4; Conductivity [mS/cm]= 1,8; COD [mg/l]= 750. TSS [mg/l]= 21 |  |  |  |  |  |  |
| Water type W4:equip volume Acetic acid (2006) = 1 g/l Steam type S1 | 2nd bath T=50°C; t=10 min. Indirect heating |  |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]= 43; pH [-]= 3,6; Conductivity [mS/cm]= 0,18; COD [mg/l]= 1050. TSS [mg/l]= 12 |  |  |  |  |  |  |
| Water type W4:equip volume Lubricating agent (1057) = 2 g/l Detergent (2048) = 2 g/l Steam type S1 | 3rd bath T=80°C; t=25 min. Indirect heating |  |  |  |  |  |  |  |  |  |  |
| Water type W3: 1000 l | Continuous washing |  |  |  | Discharge type Dl: 1000 l T [°C]= 72; pH [-]= 7,8; Conductivity [mS/cm]= 1,5; COD [mg/l]= 2650; COD [mg/l]= 2140 (for O193,O194); TSS [mg/l]= 25 |  |  |  |  |  |  |
|  |  |  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]= 6,8; pH [-]= 7,2; Conductivity [mS/cm]= 0,96; COD [mg/l]= 1950. COD [mg/l]= 1450 (for O193,O194); TSS [mg/l]= 15 |  |  |  |  |
| Water type W3: equip. volume | Washing |  |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]= 43; pH [-]= 7,6; Conductivity [mS/cm]= 0,25; COD [mg/l]= 300. TSS [mg/l]= 10 |  |  |  |  |  |  |
| Water type W3: equip. volume |  | Filling (for fabric discharge) |  |  |  |  |  |  |  |  |  |
|  |  | Filling discharge (50% of total run) |  |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,3; Conductivity [mS/cm]= 0,17; COD [mg/l]= 100; TSS [mg/l]= 0. |  |  |  |  |  |

- Notes:

- For FLAX-PES fabric: see An.D

- G 8.1 Dark  reactive dyeing in Jigger

| Department | Dyeing |
| --- | --- |
| Fabric | FLAX-CO/PL-FLAX/PL |
| Process | Dark reactive dyeing in jigger (91J) |
| Equipment | Jigger |
| Item | J144-J145-C146 |
| Run time (h) | 7,00 |
| Number of run/yr | 3-4-57 |
| Processed fabric (kg/yr) | 357-222-3051 |
| Processed fabric per run (kg) | 119-55-53 |

| Water type W4:equip volume Detergent (2046)= 1 g/l; Dispersant agent (2058)= 1 g/l; Sodium sulphate (2008)= 50 g/l; Soda Solvay (1016)= 3 g/l; Reactive dyestuffs>0,05%. Steam type S1 | 1st bath T=60°C; t=90 min. Indirect heating |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 54; pH [-]= 9; Conductivity [mS/cm]= 3,5; COD [mg/l]= 1100. TSS [mg/l]= 51 |  |  |  |  |
| Water type W3: 2500-1150-1110 l | 1st Continuous washing (1 lysis) |  |  | Discharge type Dl: 2500-1150-1110 l T [°C]= 41; pH [-]= 7,8; Conductivity [mS/cm]= 1,7; COD [mg/l]= 450. TSS [mg/l]= 15 |  |  |  |  |
| Water type W4: equip. volume | 1st Washing |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 40; pH [-]= 7,6; Conductivity [mS/cm]= 0,34; COD [mg/l]= 150. TSS [mg/l]= 0 |  |  |  |  |
| Water type W4:equip volume Acetic acid (2006)= 1 g/l. | 2nd bath T=40°C; t=10 min. |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 38; pH [-]= 3,86; Conductivity [mS/cm]= 0,21; COD [mg/l]= 1050. TSS [mg/l]= 35 |  |  |  |  |
| Water type W4:equip volume Detergent (2048)= 4 g/l. Steam type S1 | 3rd bath T=80°C; t=60 min. Indirect heating |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 50; pH [-]= 8,1; Conductivity [mS/cm]= 0,19; COD [mg/l]= 1850. TSS [mg/l]= 15 |  |  |  |  |
| Water type W3: 2500-1150-1110 l | 2nd Continuous washing (1 lysis) |  |  | Discharge type Dl: 2500-1150-1110 l T [°C]= 38; pH [-]= 7,6; Conductivity [mS/cm]= 0,20; COD [mg/l]= 500. TSS [mg/l]= 10 |  |  |  |  |
| Water type W4: equip. volume | 2nd Washing |  |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 40; pH [-]= 7,6; Conductivity [mS/cm]= 0,21; COD [mg/l]= 220. TSS [mg/l]= 3 |  |  |  |  |
| Water type W3:equip volume | Filling (for fabric discharge) |  |  |  |  |  |  |  |
|  |  | Filling discharge (50% of total run) |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,3; Conductivity [mS/cm]= 0,17; COD [mg/l]= 80; TSS [mg/l]= 0. |  |  |  |

- Notes:

- For FLAX-PES fabric: see An.D

- G 8.2 Dark reactive dyeing in overflow

| Department | Dyeing |
| --- | --- |
| Fabric | FLAX-CO/PL-FLAX/PL-SILK/PL |
| Process | Dark reactive dyeing in overflow (52F-DOS52F-MOD52F) |
| Equipment | Overflow |
| Item | O192-O193-O194 |
| Run time (h) | 6,50 |
| Number of run/yr | 79-47-27 |
| Processed fabric (kg/yr) | 3314-2546-1039 |
| Processed fabric per run (kg) | 42-54-38 |

| Water type W4:equip volume Sodium sulphate (2008) = 50 g/l Soda solvay (1016) = 3 g/l Detergent (2046) = 0,5 g/l Dispersant agent (2058) = 0,5 g/l Lubricating agent (1057) = 2 g/l Reactive dyestuffs>0,05%. Steam type S1 | 1st bath T=60°C; t=90 min. Indirect heating |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]= 51; pH [-]= 7,4; Conductivity [mS/cm]= 1,8; COD [mg/l]= 870. TSS [mg/l]= 12 |  |  |  |  |  |  |
| Water type W4:equip volume Acetic acid (2006) = 1 g/l Steam type S1 | 2nd bath T=50°C; t=10 min. Indirect heating |  |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]= 43; pH [-]= 3,6; Conductivity [mS/cm]= 0,18; COD [mg/l]= 1050. TSS [mg/l]= 55 |  |  |  |  |  |  |
| Water type W4:equip volume Lubricating agent (1057) = 2 g/l Detergent (2048) = 2 g/l Steam type S1 | 3rd bath T=80°C; t=25 min. Indirect heating |  |  |  |  |  |  |  |  |  |  |
| Water type W3: 1000 l; | Continuous washing |  |  |  | Discharge type Dl: 1000 l T [°C]= 72; pH [-]= 7,8; Conductivity [mS/cm]= 1,5; COD [mg/l]= 2700. COD [mg/l]= 2140 (for O193,O194); TSS [mg/l]= 38 |  |  |  |  |  |  |
|  |  |  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]= 6,8; pH [-]= 7,2; Conductivity [mS/cm]= 0,96; COD [mg/l]= 2000. COD [mg/l]= 1450 (for O193,O194); TSS [mg/l]= 23 |  |  |  |  |
| Water type W3: equip. volume | Washing |  |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  |  | Discharge type D1: equip. volume T [°C]= 43; pH [-]= 7,6; Conductivity [mS/cm]= 0,25; COD [mg/l]= 300. TSS [mg/l]= 80 |  |  |  |  |  |  |
| Water type W3: equip. volume |  | Filling (for fabric discharge) |  |  |  |  |  |  |  |  |  |
|  |  | Filling discharge (50% of total run) |  |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,3; Conductivity [mS/cm]= 0,17; COD [mg/l]= 100; TSS [mg/l]= 0. |  |  |  |  |  |

- Notes:

- For FLAX-PES fabric: see An.D

- G.9:Printed washing.

- G 9.1 Printed washing in Jigger

| Department | Dyeing |
| --- | --- |
| Fabric | CO/PL |
| Process | Printed washing in jigger (DOS07J) |
| Equipment | Jigger |
| Item | J144-J145-C146 |
| Run time (h) | 4,00 |
| Number of run/yr | 34-5-0 |
| Processed fabric (kg/yr) | 2809-407-0 |
| Processed fabric per run (kg) | 83-81-0 |

| Water type W3: 1700-1700-1000 l | 1st continuous washing (2 lysis) |  |  | Discharge type D1: 1700-1700-1000 l T [°C]= 18; pH [-]= 7,2; Conductivity [mS/cm]= 0,19; COD [mg/l]= 3150. TSS [mg/l]= 50 |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Water type W3:equip volume | 1st washing (2 lysis) |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,2; Conductivity [mS/cm]= 0,19; COD [mg/l]= 2100. TSS [mg/l]= 21 |  |  |
| Water type W3:equip volume Detergent (2048) = 0,4 g/l Steam type S1 | 2nd bath T=40°C t= 20 min Indirect heating |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 35; pH [-]= 7,9; Conductivity [mS/cm]= 0,21; COD [mg/l]= 800. TSS [mg/l]= 18 |  |  |
| Water type W3: 1700-1700-1000 l | 2nd continuous washing (1 lysis) |  |  | Discharge type D1: 1700-1700-1000 l T [°C]= 18; pH [-]= 7,2; Conductivity [mS/cm]= 0,19; COD [mg/l]= 650. TSS [mg/l]= 20 |  |  |
| Water type W3:equip volume | 2nd washing |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,2; Conductivity [mS/cm]= 0,19; COD [mg/l]= 350. TSS [mg/l]= 10 |  |  |
| Water type W3:equip volume | Filling (for fabric discharge) |  |  |  |  |  |
|  |  | Filling discharge (50% of total run) |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,3; Conductivity [mS/cm]= 0,17; COD [mg/l]= 150; TSS [mg/l]= 0. |  |

- Notes:

- For FLAX-PES fabric: see An.D

- G 9.2 Printed washing in overflow

| Department | Dyeing |
| --- | --- |
| Fabric | CO/PL |
| Process | Printed washing in overflow (DOS90F) |
| Equipment | Overflow |
| Item | O192-O193-O194 |
| Run time (h) | 3,30 |
| Number of run/yr | 43-0-18 |
| Processed fabric (kg/yr) | 2302-0-822 |
| Processed fabric per run (kg) | 53-0-46 |

| Water type W4:equipment volume | 1st washing |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 35; pH [-]= 7,2; Conductivity [mS/cm]= 0,19; COD [mg/l]= 3700. TSS [mg/l]= 75 |  |  |  |  |
| Water type W4: equip. volume Detergent (2048) = 1 g/l |  | 1st bath T=40°C t= 15 min |  |  |  |  |  |  |
|  |  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 38; pH [-]= 7,8; Conductivity [mS/cm]= 0,20; COD [mg/l]= 1150. TSS [mg/l]= 31 |  |  |  |
| Water type W4: equip. volume Hydrogen peroxide 130 vol (1010) = 3 g/l Soda solvay (1016) = 0,25 g/l Antifoaming agent (2077) = 0,25 g/l Non ionic surfactant (1058) = 0,75 g/l Steam type S1 |  | 2nd bath T=90°C t= 20 min Indirect heating |  |  |  |  |  |  |
| Water type W3: 500 l | Continuous Washing |  |  | Discharge type Dl: 500 l T [°C]= 78; pH [-]= 7,2; Conductivity [mS/cm]= 0,21; COD [mg/l] 650=. TSS [mg/l]= 12 |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 63; pH [-]= 7,2; Conductivity [mS/cm]= 300; COD [mg/l]= 500. TSS [mg/l]= 10 |  |  |  |  |
| Water type W3: equip. volume |  | Filling (for fabric discharge) |  |  |  |  |  |  |
|  |  | Filling discharge (50% of total run) |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,3; Conductivity [mS/cm]= 0,17; COD [mg/l]= 150; TSS [mg/l]= 0. |  |  |  |

- Notes:

- G.10: Printed triple washing.

- G 10.1 Printed triple washing in overflow

| Department | Dyeing |
| --- | --- |
| Fabric | CO/PL |
| Process | Triple printed washing in overflow |
| Equipment | Overflow |
| Item | O192-O193-O194 |
| Run time (h) | 5,30 |
| Number of run/yr | 51-4-11 |
| Processed fabric (kg/yr) | 2789-240-424 |
| Processed fabric per run (kg) | 55-60-38 |

| Water type W4:equipment volume | 1st washing |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Water type W3: 4000 l | Continuous washing |  |  |  |  | Discharge type Dl: 4000 l T [°C]= 48; pH [-]= 7,6; Conductivity [mS/cm]= 0,19; COD [mg/l]= 3050. COD [mg/l]= 1850 (for O193,O194) TSS [mg/l]= 35 |  |  |  |  |  |  |  |  |  |
|  | Discharge |  |  |  |  | Discharge type D1: equip. volume T [°C]= 43; pH [-]= 7,5; Conductivity [mS/cm]= 0,19; COD [mg/l]= 3050. COD [mg/l]= 1850 (for O193,O194) TSS [mg/l]= 35 |  |  |  |  |  |  |  |  |  |
| Water type W4: equip. volume |  | 2nd washing |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | Discharge |  |  |  |  | Discharge type D1: equip. volume T [°C]= 43; pH [-]= 7,6; Conductivity [mS/cm]= 0,19; COD [mg/l]= 1350. TSS [mg/l]= 20 |  |  |  |  |  |  |  |  |
| Water type W4: equip. volume Detergent (2048) = 2,5 g/l Lubricating. agent (1057) = 1 g/l Acetic acid (2006) = 1 g/l Steam type S1 |  | 1st bath T=60°C t=20 min Indirect heating |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | Discharge |  |  |  |  | Discharge type D1: equip. volume T [°C]= 51; pH [-]= 6,8; Conductivity [mS/cm]= 0,19; COD [mg/l]= 2400. TSS [mg/l]= 20 |  |  |  |  |  |  |  |  |
| Water type W4: equip. volume Detergent (2048) = 2,5 g/l Lubricating agent (1057) = 1 g/l Acetic acid (2006) = 1 g/l Steam type S1 |  | 2nd bath T=60°C t=30 min Indirect heating |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | Discharge |  |  |  |  | Discharge type D1: equip. volume T [°C]= 51; pH [-]= 7,2; Conductivity [mS/cm]= 0,19; COD [mg/l]= 2250. TSS [mg/l]= 18 |  |  |  |  |  |  |  |  |
| Water type W4: equip. volume Detergent (2048) = 2 g/l Steam type S1 |  |  | 3rd bath T=60°C t=30 min Indirect heating |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  | Discharge |  |  |  |  | Discharge type D1: equip. volume T [°C]= 53; pH [-]= 7,2; Conductivity [mS/cm]= 0,21; COD [mg/l]= 850. TSS [mg/l]= 5 |  |  |  |  |  |  |
| Water type W4: equip. volume |  | 3rd washing |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | Discharge |  |  |  |  | Discharge type D1: equip. volume T [°C]= 48; pH [-]= 7,2; Conductivity [mS/cm]= 0,21; COD [mg/l]= 300. TSS [mg/l]= 3 |  |  |  |  |  |  |  |  |
| Water type W3: equip. volume | Filling (for fabric discharge) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | Filling discharge (50% of total run) |  |  |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,3; Conductivity [mS/cm]= 0,17; COD [mg/l]= 100; TSS [mg/l]= 0. |  |  |  |  |  |  |  |  |

- Notes:

- G.11: Printed triple washing + stripping.

- G 11.1 Printed triple washing + stripping in overflow

| Department | Dyeing |
| --- | --- |
| Fabric | PL-CO/PL |
| Process | Triple printed washing + stripping in overflow |
| Equipment | Overflow |
| Item | O192-O193-O194 |
| Run time (h) | 4,10 |
| Number of run/yr | 81-8-26 |
| Processed fabric (kg/yr) | 4386-336-1394 |
| Processed fabric per run (kg) | 54-42-54 |

| Water type W4:equipment volume Reducing agent (2067) = 1 g/l | 1st bath T=50°C t=10 min |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 38; pH [-]= 7,9; Conductivity [mS/cm]= 1,7; COD [mg/l]= 3050. COD [mg/l]= 1950 (for O193,O194) TSS [mg/l]= 75 |  |  |  |  |
| Water type W4: equip. volume |  | 1st washing |  |  |  |  |  |  |
|  |  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 43; pH [-]= 8,1; Conductivity [mS/cm]= 1,4; COD [mg/l]= 3050. COD [mg/l]= 1950 (for O193,O194) TSS [mg/l]= 61 |  |  |  |
| Water type W4: equip. volume Caustic Soda (1011) = 1 g/l Sodium Hydrosulphite (1017) = 1 g/l Detergent (2048) = 1 g/l Lubricating agent (1057) 1 g/l Steam type S1 |  | 2nd bath T=60°C t=20 min Indirect heating |  |  |  |  |  |  |
|  |  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 51; pH [-]= 7,6; Conductivity [mS/cm]= 1,4; COD [mg/l]= 950. TSS [mg/l]= 28 |  |  |  |
| Water type W4: equip. volume . Caustic Soda (1011) = 1,5 g/l Sodium Hydrosulphite (1017) = 1,5 g/l Detergent (2048) = 1,5 g/l Lubricating agent. (1057) 1 g/l Steam type S1 |  | 3rd bath T=80°C t=20 min Indirect heating |  |  |  |  |  |  |
| Water type W3: 500 l | Continuous washing |  |  | Discharge type D l: 500 l T [°C]= 57; pH [-]= 7,3; Conductivity [mS/cm]= 0,38; COD [mg/l]= 1200. COD [mg/l]= 940 (for O193,O194) TSS [mg/l]= 15 |  |  |  |  |
|  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 53; pH [-]= 7,1; Conductivity [mS/cm]= 0,27; COD [mg/l]= 900. COD [mg/l]= 1040 (for O193,O194) TSS [mg/l]= 10 |  |  |  |  |
| Water type W4: equip. volume |  | 2nd washing |  |  |  |  |  |  |
|  |  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 33; pH [-]= 7,2; Conductivity [mS/cm]= 0,21; COD [mg/l]= 450. TSS [mg/l]= 5 |  |  |  |
| Water type W3: equip. volume |  | Filling (for fabric discharge) |  |  |  |  |  |  |
|  |  | Filling discharge (50% of total run) |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,3; Conductivity [mS/cm]= 0,17; COD [mg/l]= 150; TSS [mg/l]= 0. |  |  |  |

- Notes:

- G.12:Devorè printed washing.

- G.12.1 Devorè printed washing in overflow

| Department | Dyeing |
| --- | --- |
| Fabric | CO/PL |
| Process | Devorè printed washing in overflow |
| Equipment | Overflow |
| Item | O192-O193-O194 |
| Run time (h) | 3,10 |
| Number of run/yr | 206-12-66 |
| Processed fabric (kg/yr) | 11113-491-3511 |
| Processed fabric per run (kg) | 54-41-53 |

| Water type W4:equipment volume |  | 1st washing |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 43; pH [-]= 7,6; Conductivity [mS/cm]= 1,5; COD [mg/l]= 4010. TSS [mg/l]= 81 |  |  |  |  |
| Water type W4: equip. volume Detergent (2048) = 2 g/l |  |  | 1st bath T=50°C T=10 min |  |  |  |  |  |  |
|  |  |  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 48; pH [-]= 7,4; Conductivity [mS/cm]= 0,6; COD [mg/l]= 1800. TSS [mg/l]= 51 |  |  |  |
| Water type W4: equip. volume |  |  | 2nd washing |  |  |  |  |  |  |
|  |  |  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 48; pH [-]= 7,2; Conductivity [mS/cm]= 0,4; COD [mg/l]= 1050. TSS [mg/l]= 25 |  |  |  |
| Water type W4: equip. volume Detergent (2048) = 2 g/l Acetic Acid (2006) = 1 g/l Lubricating Agent (1057) = 2 g/l Steam type S1 |  |  | 2nd bath T=60°C t=20 min Indirect heating |  |  |  |  |  |  |
|  |  |  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 35; pH [-]= 6,8; Conductivity [mS/cm]= 0,8; COD [mg/l]= 1500. TSS [mg/l]= 18 |  |  |  |
| Water type W4: equip. volume Detergent (2048) = 2 g/l Acetic Acid (2006) = 1 g/l Lubricating Agent (1057) = 2 g/l Steam type S1 |  | 3rd bath T=80°C t=20 min Indirect heating |  |  |  |  |  |  |  |
| Water type W3: 1000 l |  | Continuous washing |  |  | Discharge type D1: 1000 l T [°C]= 35; pH [-]= 7,2; Conductivity [mS/cm]= 1,8; COD [mg/l]= 1150. TSS [mg/l]= 21 |  |  |  |  |
|  |  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 27; pH [-]= 7,2; Conductivity [mS/cm]= 1,4; COD [mg/l]= 650. TSS [mg/l]= 15 |  |  |  |  |
| Water type W3: equip. volume |  |  | 3rd washing |  |  |  |  |  |  |
|  |  |  | Discharge |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,1; Conductivity [mS/cm]= 0,8; COD [mg/l]= 350. TSS [mg/l]= 12 |  |  |  |
| Water type W3: equip. volume |  |  | Filling (for fabric discharge) |  |  |  |  |  |  |
|  |  |  | Filling discharge (30% of total run) |  |  | Discharge type D1: equip. volume T [°C]= 18; pH [-]= 7,3; Conductivity [mS/cm]= 0,17; COD [mg/l]= 100; TSS [mg/l]= 0. |  |  |  |

- Notes:

- G.13:Washing for printing  panels fabrics.

- G 13.1 Washing for printing  panel fabric in torpedo

| Department | Dyeing |
| --- | --- |
| Fabric | PL |
| Process | Washing for printing panel fabric in torpedo |
| Equipment | Torpedo |
| Item | T151-T153-T154-T155 |
| Run time (h) | 4,00 |
| Number of run/yr | 1-17-2-0 |
| Processed fabric (kg/yr) | 483-7710-216-0 |
| Processed fabric per run (kg) | 483-453-108-0 |

| Water type W4:equipment volume Caustic Soda (1011) = 1 g/l Non ionic surfactant (2057) = 3 g/l Steam type S1 | 1st bath T= 80°C t= 30 min Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 73; pH [-]= 8,2; Conductivity [mS/cm]= 0,23; COD [mg/l]= 4550; TSS [mg/l]= 55 |  |  |
| Water type W4:equip volume Steam type S1 | 2nd bath T= 60°C t= 20 min Indirect heating |  |  |  |  |
| Water type W4: 4000 l | Continuous Washing |  | Discharge type Dl: 4000 l T [°C]= 48; pH [-]= 7,8; Conductivity [mS/cm]= 0,18; COD [mg/l]= 625. TSS [mg/l]= 10 |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 31; pH [-]= 7,6; Conductivity [mS/cm]= 0,21; COD [mg/l]= 500. TSS [mg/l]= 10 |  |  |
| Water type W4:equip volume Oxalic Acid (1007) = 0,5 g/l Carrier (2068) = 1 g/l Solvent (0011) = 0,03 g/l Steam type S1 | 3rd bath T=90°C t=20 min Indirect heating |  |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 68; pH [-]= 4,8; Conductivity [mS/cm]= 1,3; COD [mg/l]= 1800. TSS [mg/l]= 21 |  |  |
| Water type W4:equip volume Acetic Acid (2006) = 1 g/l Steam type S1 | 4th bath T=90°C t=20 min Indirect heating |  |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 65; pH [-]= 3,6; Conductivity [mS/cm]= 0,6; COD [mg/l]= 105. TSS [mg/l]= 5 |  |  |
| Water type W3: equip. volume | Washing |  |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 41; pH [-]= 6,8; Conductivity [mS/cm]= 0,3; COD [mg/l]= 400. TSS [mg/l]= 0 |  |  |

- Notes:

- G.14: Equipment washing.

- G 14.1: Equipment washing- jigger

| Department | Dyeing |
| --- | --- |
| Fabric | - |
| Process | Equipment washing-jigger |
| Equipment | jigger |
| Item | J144-J145-C146 |
| Run time (h) | 4,00 |
| Number of run/yr | 44-44-44 |
| Processed fabric (kg/yr) | - |
| Processed fabric per run (kg) | - |

| Water type W4:equipment volume Sodium Hydrosulphite (1017) = 2,5 g/l Soda Solvay (1016) = 2 g/l Steam type S1 | 1st bath T= 110°C t= 30 min Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 77; pH [-]= 8,7; Conductivity [mS/cm]= 2,1; COD [mg/l]= 300; TSS [mg/l]= 15 |  |  |
| Water type W3: equip. volume | Washing |  |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 54; pH [-]= 7,9; Conductivity [mS/cm]= 1,5; COD [mg/l]= 50. TSS [mg/l]= 5 |  |  |

- G 14.2: Equipment washing- torpedo

| Department | Dyeing |
| --- | --- |
| Fabric | - |
| Process | Equipment washing-torpedo |
| Equipment | Torpedo |
| Item | T151-T153-T154-T155 |
| Run time (h) | 4,00 |
| Number of run/yr | 44-44-44-44 |
| Processed fabric (kg/yr) | - |
| Processed fabric per run (kg) | - |

| Water type W4:equipment volume Sodium Hydrosulphite (1017) = 6 g/l Caustic Soda (1011) = 4,5 g/l Steam type S1 | 1st bath T= 130°C t= 30 min Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Dispersant agent (2024) = 1,5 g/l Carrier (2023) = 0,8 g/l | Discharge |  | Discharge type D1: equip. volume T [°C]= 78; pH [-]= 8,1; Conductivity [mS/cm]= 2,5; COD [mg/l]= 1350; TSS [mg/l]= 57 |  |  |
| Water type W3: equip. volume | Washing |  |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 53; pH [-]= 7,9; Conductivity [mS/cm]= 1,7; COD [mg/l]= 150. TSS [mg/l]= 18 |  |  |

- G 14.3: Equipment washing- overflow

| Department | Dyeing |
| --- | --- |
| Fabric | - |
| Process | Equipment washing-overflow |
| Equipment | Overflow |
| Item | O192-O193-O194 |
| Run time (h) | 4,00 |
| Number of run/yr | 44-44-44 |
| Processed fabric (kg/yr) | - |
| Processed fabric per run (kg) | - |

| Water type W4:equipment volume Sodium Hydrosulphite (1017) = 2,5 g/l Soda Solvay (1016) = 2 g/l Steam type S1 | 1st bath T= 110°C t= 30 min Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 77; pH [-]= 8,7; Conductivity [mS/cm]= 2,1; COD [mg/l]= 300; TSS [mg/l]= 15 |  |  |
| Water type W3: equip. volume | Washing |  |  |  |  |
|  | Discharge |  | Discharge type D1: equip. volume T [°C]= 54; pH [-]= 7,9; Conductivity [mS/cm]= 1,5; COD [mg/l]= 50. TSS [mg/l]=5 |  |  |