An. H: Finishing- Process scheme.

- H1: Softener finishing;

- H 1.1: Softener finishing (Perlamina);

- H1.2: Softener finishing (Infasil);

- H1.3: Softener finishing (Solusoft).

- H2: Water finishing;

- H3: Non slip  finishing;

- H4: Antistatic finishing;

- H5: Fixing colour  finishing.

H1:Softener finishing

H1.1:Softener finishing (Perlamina):

| Department | Finishing |
| --- | --- |
| Fabric | FLAX-PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Softener finishing (Perlamina) |
| Equipment | Rameuse |
| Item | R161-R163 |
| Operating | Continuous |
| Number of cycles/year | 158-158 |
| Cycle time (h) | 2 |
| Processed fabric (yarn) (kg/yr) | 26974-26974 |
| Processed fabric (yarn) per hour (kg/h) | 85 |

| Water type W3: 85 l/h. Softener (3014):40 g/l | Doping Wringing Thermosetting (T=140°C) | Discharge type D1: 70 l/cycle T [°C]=18; pH [-]=7,6; Conductivity [mS/cm]=0,21; COD [mg/l]=16000; TSS [mg/l]=200. |
| --- | --- | --- |

Notes:

For FLAX-PL fabric:see An.D.

H1.2:Softener finishing (Infasil).

| Department | Finishing |
| --- | --- |
| Fabric (Yarn, …) | FLAX-PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Softener finishing (Infasil) |
| Equipment | Rameuse |
| Item | R161-R163 |
| Operating | Continuous |
| Number of cycles/year | 166-166 |
| Cycle time (h) | 1,7 |
| Processed fabric (yarn) (kg/yr) | 24230-24230 |
| Processed fabric (yarn) per hour (kg/h) | 85 |

| Water type W3: 85 l/h. Antistatic agent (3045): 15 g/l Softener (3003):20 g/l | Doping Wringing Thermosetting (T=140°C) | Discharge type D1: 70 l/cycle T [°C]=19; pH [-]=6,9; Conductivity [mS/cm]=0,17; COD [mg/l]=18220 TSS [mg/l]=200. |
| --- | --- | --- |

Notes:

For FLAX-PL fabric:see An.D.

H3:Softener finishing (Solusoft)

| Department | Finishing |
| --- | --- |
| Fabric | FLAX-PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Softener finishing (Solusoft) |
| Equipment | Rameuse |
| Item | R161-R163 |
| Operating | Continuous |
| Number of cycles/year | 49-49 |
| Cycle time (h) | 1,7 |
| Processed fabric (yarn) (kg/yr) | 7152-7152 |
| Processed fabric (yarn) per hour (kg/h) | 85 |

| Water type W3: 85 l/h. Softener (3094): 30 g/l | Doping Wringing Thermosetting (T=140°C) | Discharge type D1: 70 l/cycle T [°C]=19; pH [-]=7,2; Conductivity [mS/cm]=0,19; COD [mg/l]=11880; TSS [mg/l]=200. |
| --- | --- | --- |

Notes:

For FLAX-PL fabric:see An.D.

H2:Water finishing

| Department | Finishing |
| --- | --- |
| Fabric | FLAX-PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Water finishing |
| Equipment | Rameuse |
| Item | R161-R163 |
| Operating | Continuous |
| Number of cycles/year | 511-511 |
| Cycle time (h) | 1,7 |
| Processed fabric (yarn) (kg/yr) | 74728-74728 |
| Processed fabric (yarn) per hour (kg/h) | 85 |

| Water type W3: 85 l/h. | Doping Wringing Thermosetting (T=120°C) | Discharge type D1: 70 l/cycle T [°C]=19; pH [-]=6,9; Conductivity [mS/cm]=0,17; COD [mg/l]=140 TSS [mg/l]=10. |
| --- | --- | --- |

Notes:

For FLAX-PL fabric:see An.D.

H3:Non slip finishing

| Department | Finishing |
| --- | --- |
| Fabric | FLAX-PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Non slip finishing |
| Equipment | Rameuse |
| Item | R161-R163 |
| Operating | Continuous |
| Number of cycles/year | 102-102 |
| Cycle time (h) | 1,7 |
| Processed fabric (yarn) (kg/yr) | 14824-14824 |
| Processed fabric (yarn) per hour (kg/h) | 85 |

| Water type W3: 85 l/h. Antistatic agent (3045): 10 g/l Non slip agent (3017): 25 g/l \ | Doping Wringing Thermosetting (T=140°C) | Discharge type D1: 70 l/cycle T [°C]=19; pH [-]=6,9; Conductivity [mS/cm]=0,17; COD [mg/l]=17000; TSS [mg/l]=200. |
| --- | --- | --- |

Notes:

For FLAX-PL fabric:see An.D.

H4:Antistatic finishing

| Department | Finishing |
| --- | --- |
| Fabric | FLAX-PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Antistatic finishing |
| Equipment | Rameuse |
| Item | R161-R163 |
| Operating | Continuous |
| Number of cycles/year | 566-566 |
| Cycle time (h) | 1,7 |
| Processed fabric (yarn) (kg/yr) | 82729-82729 |
| Processed fabric (yarn) per hour (kg/h) | 85 |

| Water type W3: 85 l/h. Antistatic agent (3045): 10 g/l | Doping Wringing Thermosetting (T=140°C) | Discharge type D1: 70 l/cycle T [°C]=19; pH [-]=6,9; Conductivity [mS/cm]=0,17; COD [mg/l]=14650; TSS [mg/l]=200. |
| --- | --- | --- |

Notes:

For FLAX-PL fabric:see An.D.

H5: Fixing colour finishing

| Department | Finishing |
| --- | --- |
| Fabric | FLAX-PL-CO/PL-FLAX/PL-SILK/PL |
| Process | Fixing colour finishing |
| Equipment | Rameuse |
| Item | R161-R163 |
| Operating | Continuous |
| Number of cycles/year | 101-101 |
| Cycle time (h) | 3,3 |
| Processed fabric (yarn) (kg/yr) | 28243-28243 |
| Processed fabric (yarn) per hour (kg/h) | 85 |

| Water type W3: 85 l/h. Fixing agent (3116): 20 g/l | Doping Wringing Thermosetting (T=140°C) | Discharge type D1: 70 l/cycle T [°C]=19; pH [-]=6,9; Conductivity [mS/cm]=0,17; COD [mg/l]=15000; TSS [mg/l]=200. |
| --- | --- | --- |

Notes:

For FLAX-PL fabric:see An.D.