An.F: Preparation - Process scheme.

- F.1: Yarn scouring.

- F 1.1:Silk yarn light scouring

- F.1.2: Nylon-PES-Acetate yarn light scouring

- F 1.3: HT scouring

- F 1.4: SHAPPE scouring

- F 1.5: TUSSAH scouring

- F 1.6: SCHANTUNG scouring

- F 1.7: SILK YARN  degumming

- F.2: Polymer charge

- F.3:  Fabric scouring

- F.3.1: silk FABRIC degumming

- F.3.2: Mezzera continuous scouring

- F.3.3: Stella scouring

F.1: Yarn Scouring.

F 1.1: Silk yarn light scouring.

| Department | Preparation |
| --- | --- |
| Yarn | SILK |
| Process | Light scouring |
| Equipment | Autoclave |
| Item | A-B-C/ 31-32-33-34/ 102-103-104-105-106-107/ 203-204/ 301-302 /601 |
| Run time (h) | 0,5 |
| Number of run/yr | 67/ 21/ 194/ 716/ 442/ 119 |
| Processed yarn (kg/yr) | 669/ 502/ 17426/ 143223/ 132620/ 71496 |
| Processed yarn per run (kg) | 10/24/90/200/300/600 |

| Water type W5 :equip volume Anionic-non ionic surfactant (10232)= 5 g/l Steam type S1 | Bath T=60°C t= 30 min Indirect heating |  |  |
| --- | --- | --- | --- |
|  | Discharge | Discharge type D2: equip. volume T [°C]=60; pH [-]= 6,6; Conductivity [mS/cm]=0,34; COD [mg/l]=3480; TSS [mg/l]=120. |  |

Notes:

F 1.2: Nylon-PES-Acetate yarn light scouring.

| Department | Preparation |
| --- | --- |
| Yarn | NYLON-PES-ACETATE |
| Process | Light scouring |
| Equipment | Autoclave |
| Item | 31-32-33-34/ 51-52/ 102-103-104-105-106-107/ 203-204 |
| Run time (h) | 0,75 |
| Number of run/yr | 62/ 206/ 29/ 3 |
| Processed yarn (kg/yr) | 1482/ 8233/ 2634/ 659 |
| Processed yarn per run (kg) | 24/ 40/ 90/ 200 |

| Water type W5 :equip volume Emulsifying agent (10438)= 2 g/l ; Sequestering agent (10433)= 1 g/l; Sodium carbonate (10175)= 0,5 g/l. Steam type S1 | Bath T=60°C t=30 min Indirect heating |  |  |
| --- | --- | --- | --- |
|  | Discharge | Discharge type D2: equip. volume. T [°C]= 60; pH [-]=7,15 ; Conductivity [mS/cm]=0,3; COD [mg/l]=4200; TSS [mg/l]=160 |  |
| Water type W5 :equip volume Steam type S1 | Warm washing T=50°C t=10 min Indirect heating |  |  |
|  | Discharge | Discharge type D2: equip. volume. T [°C]= 50; pH [-]= 7,2; Conductivity [mS/cm]= 0,21; COD [mg/l]=1050; TSS [mg/l]=80. |  |
| Water type W4 :equip volume | Washing |  |  |
|  | Discharge | Discharge type D5: equip. volume. T [°C]=30; pH [-]= 7,6; Conductivity [mS/cm]= 0,19; COD [mg/l]= 450; TSS [mg/l]= 20. |  |

Notes:

F 1.3: HT scouring.

| Department | Preparation |
| --- | --- |
| Yarn | SILK |
| Process | HT scouring |
| Equipment | Autoclave |
| Item | 102-103-104-105-106-107/ 203-204/ 301-302/ 601 |
| Run time (h) | 1,10 |
| Number of run/yr | 127/ 552/ 277/ 70 |
| Processed yarn (kg/yr) | 11443/ 110397/ 83024/ 41738 |
| Processed yarn per run (kg) | 90/ 200/ 300/ 600 |

| Water type W5 :equip volume Solubilizing agent (10389)= 5 g/l; Sequestering agent (10433)= 2 g/l. Steam type S1 | 1st bath T=130°C t=40 min Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D3: equip. volume T [°C]=110; pH [-]=7,26; Conductivity [mS/cm]=0,88; COD [mg/l]=18785; TSS [mg/l]=. |  |  |
| Water type W5 :equip volume Sequestering -dispersant agent (10299)= 2 g/l; Steam type S1 | 2nd bath T=98°C t=20 min Indirect heating |  |  |  |  |
|  | Discharge |  | Discharge type D2: equip. volume T [°C]=95; pH [-]=7,79; Conductivity [mS/cm]= 0,39; COD [mg/l]= 2900; TSS [mg/l]=25 |  |  |
| Water type W5 :equip volume Steam type S1 | Warm washing T=50°C t=10 min Indirect heating |  |  |  |  |
|  | Discharge |  | Discharge type D2: equip. volume T [°C]=50 ; pH [-]= 7,62; Conductivity [mS/cm]=0,21; COD [mg/l]= 720; TSS [mg/l]= 15. |  |  |
| Water type W4 :equip volume | Washing |  |  |  |  |
|  | Discharge |  | Discharge type D5: equip. volume T [°C]=24 pH [-]= 6,95; Conductivity [mS/cm]= 0,2; COD [mg/l]= 220; TSS [mg/l]= 25. |  |  |

Notes:

F 1.4: SHAPPE scouring

| Department | Preparation |
| --- | --- |
| Yarn | SILK |
| Process | SHAPPE scouring |
| Equipment | Autoclave |
| Item | A-B-C/ 31-32-33-34/ |
| Run time (h) | 1,34 |
| Number of run/yr | 67/ 21 |
| Processed yarn (kg/yr) | 669/ 502 |
| Processed fabric per run (kg) | 10/ 24 |

| Water type W5: equipment volume Emulsifying agent (10232)= 2 g/l; Sequestering agent (10382)= 2 g/l; Sequestering agent (10433)= 1 g/l. Steam type S1 | 1st Bath T= 60°C t= 30 min Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D2: equip. volume T [°C]=60; pH [-]=7,43; Conductivity [mess/cm]=0,3; COD [mg/l]=2360; TSS [mg/l]=30. |  |  |
| Water type W5: equipment volume Hydrogen peroxide (10182)= 2 g/l; Stabilizer (10196)= 0,5 g/l; Softener (10252)= 0,5 g/l; Detergent (10437)= 1 g/l. Steam type S1 | 2nd Bath T= 80°C t= 40 min Indirect heating |  |  |  |  |
|  | Discharge |  | Discharge type D2: equip. volume T [°C]=80; pH [-]=7,65; Conductivity [mS/cm]= 0,3; COD [mg/l]=2200; TSS [mg/l]=70. |  |  |
| Water type W5 :equip volume Steam type S1 | 1st warm washing T= 60°C t= 8 min Indirect heating |  |  |  |  |
|  | Discharge |  | Discharge type D2: equip. volume T [°C]=60; pH [-]= 7,89; Conductivity [mS/cm]= 0,18; COD [mg/l]= 750; TSS [mg/l]= 10. |  |  |
| Water type W5 :equip volume Steam type S1 | 2nd warm washing T= 60°C t= 8 min Indirect heating |  |  |  |  |
|  | Discharge |  | Discharge type D2: equip. volume T [°C]= 60; pH [-]= 7,9; Conductivity [mS/cm]= 0,17; COD [mg/l]= 170; TSS [mg/l]= 10. |  |  |
| Water type W5 :equip volume | Washing |  |  |  |  |
|  | Discharge |  | Discharge type D5: equip. volume T [°C]= 22; pH [-]= 7,6; Conductivity [mS/cm]= 0,17; COD [mg/l]= 80; TSS [mg/l]= 5. |  |  |

Notes:

.

F 1.5: TUSSAH scouring

| Department | Preparation |
| --- | --- |
| Yarn | SILK |
| Process | TUSSAH scouring |
| Equipment | Autoclave |
| Item | 102-103-104-105-106-107/ 203-204 |
| Run time (h) | 2,30 |
| Number of run/yr | 7/ 1 |
| Processed fabric (kg/yr) | 602/ 201 |
| Processed fabric per run (kg) | 90/ 200 |

| Water type W5:equip volume Detergent (10300)= 5 g/l; Sequestering agent (10046)= 1 g/l. Steam type S1 | 1st Bath T=90°C t=40 min Indirect heating |  |  |  |
| --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D2: equip. volume T [°C]= 80; pH [-]= 7,8; Conductivity [mS/cm]= 0,23; COD [mg/l]= 3500; TSS [mg/l]= 130.. |  |
| Water type W5:equip volume Enzyme (10191)= 2 g/l; Detergent (10437)= 0,5 g/l; Sodium carbonate (10175)= 0,2 g/l. Steam type S1 | 2nd Bath T=60°C t=60 min Indirect heating |  |  |  |
|  | Discharge |  | Discharge type D2: equip. volume T [°C]=60; pH [-]=7,35; Conductivity [mS/cm]= 0,72; COD [mg/l]= 5900; TSS [mg/l]= 100. |  |
| Water type W4:equip volume | 1st washing |  |  |  |
|  | Discharge |  | Discharge type D5: equip. volume T [°C]= 32; pH [-]= 6,93; Conductivity [mS/cm]= 0,3; COD [mg/l]=1160; TSS [mg/l]= 53. |  |
| Water type W4:equip volume | 2nd washing |  |  |  |
|  | Discharge |  | Discharge type D5: equip. volume T [°C]= 26; pH [-]= 6,97; Conductivity [mS/cm]= 0,19; COD [mg/l]=445; TSS [mg/l]= 30. |  |
| Water type W5:equip volume Reducing agent (10281)= 10 g/l. Steam type S1 | 3rd bath T=90°C t=40 min Indirect heating |  |  |  |
|  | Discharge |  | Discharge type D2: equip. volume T [°C]= 90; pH [-]=6,15; Conductivity [mS/cm]= 7,75; COD [mg/l]= 2030; TSS [mg/l]= 25. |  |
| Water type W5 :equip volume Steam type S1 | Warm washing T= 60°C t= 10 min Indirect heating |  |  |  |
|  | Discharge |  | Discharge type D2: equip. volume T [°C]= 60; pH [-]= 6,84; Conductivity [mS/cm]= 1,9; COD [mg/l]= 530; TSS [mg/l]= 5. |  |
| Water type W4:equip volume | 3rd washing |  |  |  |
|  | Discharge |  | Discharge type D5: equip. volume T [°C]= 33; pH [-]= 7,17; Conductivity [mS/cm]= 0,61; COD [mg/l]= 90; TSS [mg/l]= 10. |  |
| Water type W4:equip volume | 4th washing |  |  |  |
|  | Discharge |  | Discharge type D5: equip. volume T [°C]= 24; pH [-]= 7,09; Conductivity [mS/cm]= 0,29; COD [mg/l]=30; TSS [mg/l]= 5. |  |

Notes:

F 1.6: SHANTUNG scouring

| Department | Preparation |
| --- | --- |
| Yarn | SILK |
| Process | SHANTUNG scouring |
| Equipment | Autoclave |
| Item | 102-103-104-105-106-107/ 201-202 |
| Run time (h) | 2,00 |
| Number of run/yr | 30/ 40 |
| Processed fabric (kg/yr) | 2676/ 8029 |
| Processed fabric per run (kg) | 90/ 200 |

| Water type W5: equip volume Solubilizing agent (10389)= 5 g/l; Sequestering agent (10433)= 1 g/l; Steam type S1 |  | 1st Bath T=130°C t=40 min Indirect heating |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Discharge |  | Discharge type D2: equip. volume T [°C]= 90; pH [-]= 7,3; Conductivity [mS/cm]= 0,7; COD [mg/l]= 9300; TSS [mg/l]= 600. |  |
| Water type W4: equip volume |  | 1st washing |  |  |  |
|  |  | Discharge |  | Discharge type D5: equip. volume T [°C]= 85; pH [-]= 7,6; Conductivity [mS/cm]= 0,3; COD [mg/l]= 3500; TSS [mg/l]= 200. |  |
| Water type W5: equip volume Enzyme (10191)= 2 g/l; Detergent (10437)= 0,5 g/l; Sodium carbonate (10175)= 0,2 g/l. Steam type S1 |  | 2nd Bath T=60°C t=60 min Indirect heating |  |  |  |
|  |  | Discharge |  | Discharge type D2: equip. volume T [°C]= 60; pH [-]= 7,35; Conductivity [mS/cm]= 0,72; COD [mg/l]= 5900; TSS [mg/l]= 100. |  |
| Water type W4 :equip volume |  | 2nd washing |  |  |  |
|  |  | Discharge |  | Discharge type D5: equip. volume T [°C]= 40; pH [-]= 7,2; Conductivity [mS/cm]= 0,21; COD [mg/l]=750; TSS [mg/l]= 120. |  |
| Water type W5: equip volume Hydrogen peroxide (10182)= 10 g/l; Stabilizer (10196)= 0,5 g/l; Softener (10252)= 0,5 g/l. Steam type S1 |  | 3rd bath T=80°C t=30 min Indirect heating |  |  |  |
|  |  | Discharge |  | Discharge type D2: equip. volume T [°C]= 80; pH [-]= 8,02; Conductivity [mS/cm]= 0,2; COD [mg/l]=1800; TSS [mg/l]= 650. |  |
| Water type W5: equip volume Steam type S1 |  | Warm washing T=60°C t=6 min Indirect heating |  |  |  |
|  |  | Discharge |  | Discharge type D2: equip. volume T [°C]= 60; pH [-]= 7,9; Conductivity [mS/cm]= 0,18; COD [mg/l]= 650; TSS [mg/l]= 10. |  |
| Water type W4 :equip volume |  | 3rd washing |  |  |  |
|  |  | Discharge |  | Discharge type D5: equip. volume T [°C]= 32; pH [-]= 7,08; Conductivity [mS/cm]= 0,19; COD [mg/l]= 105; TSS [mg/l]= 30. |  |

Notes:

F 1.7: SILK YARN degumming

| Department | Preparation |
| --- | --- |
| Yarn | SILK |
| Process | SILK YARN degumming |
| Equipment | Autoclave |
| Item | 203-204/ 601 |
| Run time (h) | 2,00 |
| Number of run/yr | 19/ 13 |
| Processed yarn (kg/yr) | 3754/ 7508 |
| Processed yarn per run (kg) | 90/ 200 |

| Water type W5:equip volume Emulsifying agent (10232)= 5 g/l; Sequestering agent (10046)= 1 g/l, Steam type S1 | 1st Bath T=55°C t=60 min Indirect heating |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Discharge |  |  | Discharge type D2: equip. volume T [°C]=55 ; pH [-]= 6,95; Conductivity [mS/cm]= 0,39; COD [mg/l]= 3200; TSS [mg/l]= 300. |  |  |  |
| Water type W4: equip. volume |  | 1st washing |  |  |  |  |  |
|  |  | Discharge |  |  | Discharge type D5: equip. volume T [°C]=35; pH [-]= 7,6; Conductivity [mS/cm]= 0,23; COD [mg/l]= 1017; TSS [mg/l]= 60. |  |  |
| Water type W4: equip. volume |  | 2nd washing |  |  |  |  |  |
|  |  | Discharge |  |  | Discharge type D5: equip. volume T [°C]=20; pH [-]=7,33; Conductivity [mS/cm]= 0,18; COD [mg/l]= 200; TSS [mg/l]= 20. |  |  |
| Water type W5: equip volume Hydrogen peroxide (10182)= 10 g/l; Stabilizer (10196)= 0,5 g/l; Softener (10252)= 0,5 g/l. Steam type S1 | 2nd Bath T=55°C t=40 min Indirect heating |  |  |  |  |  |  |
|  | Discharge |  |  | Discharge type D2: equip. volume T [°C]= 40; pH [-]= 8,02; Conductivity [mS/cm]= 0,2; COD [mg/l]= 1800; TSS [mg/l]= 50. |  |  |  |
| Water type W5: equip. volume |  | 1st warm washing T=60°C t=10 min Indirect heating |  |  |  |  |  |
|  |  | Discharge |  |  | Discharge type D2: equip. volume T [°C]=60; pH [-]= 7,9; Conductivity [mS/cm]= 0,18; COD [mg/l]= 750; TSS [mg/l]= 35. |  |  |
| Water type W5: equip. volume |  | 2nd warm washing T=60°C t=10 min Indirect heating |  |  |  |  |  |
|  |  | Discharge |  |  | Discharge type D2: equip. volume T [°C]=60; pH [-]= 7,9; Conductivity [mS/cm]= 0,18; COD [mg/l]= 600; TSS [mg/l]= 10. |  |  |
| Water type W4: equip. volume |  | 3rd washing |  |  |  |  |  |
|  |  | Discharge |  |  | Discharge type D5: equip. volume T [°C]= 35; pH [-]= 7,9; Conductivity [mS/cm]= 0,18; COD [mg/l]= 400; TSS [mg/l]= 15. |  |  |
| Water type W4: equip. volume |  | 4th washing |  |  |  |  |  |
|  |  | Discharge |  |  | Discharge type D5: equip. volume T [°C]= 21; pH [-]= 7,9; Conductivity [mS/cm]= 0,18; COD [mg/l]= 250; TSS [mg/l]=10. |  |  |

Notes:

F.2. Polymer charge

| Department | Preparation |
| --- | --- |
| Yarn | SILK |
| Process | Polymer charge |
| Equipment | Autoclave |
| Item | 102-103-104-105-106-107/ 203-204/ 301-302/ 601 |
| Run time (h) | 2,25 |
| Number of run/yr | 37/ 124/ 165/ 50 |
| Processed yarn(kg/yr) | 3306/ 24798/ 49597/ 29758 |
| Processed yarn per run (kg) | 90/ 200/ 300/ 600 |

| Water type W5:equip volume Metacrylamide (10073)= 80.%; Ammonium sulphate (10012)=8 %; Formic acid (10005) = 5 g/l. Steam type S1 | Bath T=70°C; t=120 min. Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D2: equip. volume T [°C]= 69; pH [-]= 2,68; Conductivity [mS/cm]= 4,83; COD [mg/l]= 20384; TSS [mg/l]=100. |  |  |
| Water type W5:equip volume Steam type S1 | 1st warm washing T=80°C t=15 min Indirect heating |  |  |  |  |
|  | Discharge |  | Discharge type D2: equip. volume T [°C]= 78; pH [-]= 2,92; Conductivity [mS/cm]= 1,46; COD [mg/l]= 4782; TSS [mg/l]= 46. |  |  |
| Water type W5:equip volume Steam type S1 | 2nd warm washing T=60°C t= 10 min Indirect heating |  |  |  |  |
|  | Discharge |  | Discharge type D2: equip. volume T [°C]= 57; pH [-]= 3,44; Conductivity [mS/cm]= 0,325; COD [mg/l]= 850; TSS [mg/l]= 15. |  |  |

Notes:

F.3. Fabric scouring

F.3.1: SILK FABRIC degumming

| Department | Preparation |
| --- | --- |
| Fabric | SILK |
| Process | SILK FABRIC degumming |
| Equipment | Jigger |
| Item | JG01-JG03-JG05-JG09 |
| Run time (h) | 1,00 |
| Number of run/yr | 121 |
| Processed fabric (kg/yr) | 3256 |
| Processed fabric per run (kg) | 27 |

| Water type W5:equip volume Sequestering agent (10382) = 2 g/l ; Sequestering agent (10433) = 1 g/l ; Detergent ( 10347) = 1 g/l. Steam type S1 | Bath T=60°C; t=40 min. Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D2: equip. volume T [°C]=60; pH [-]= 6,95; Conductivity [mS/cm]=0,39; COD [mg/l]=3225; TSS [mg/l]= 300. |  |  |
| Water type W5: 600 l | 1st continuous washing |  | Discharge type D2: 600 l T [°C]=60; pH [-]= 7,59; Conductivity [mS/cm]= 0,23; COD [mg/l]= 1020; TSS [mg/l]= 60. |  |  |
| Water type W4: 600 l | 2nd continuous washing |  | Discharge type D5 600 l T [°C]=20; pH [-]= 7,33; Conductivity [mS/cm]= 0,18; COD [mg/l]= 90; TSS [mg/l]= 5. |  |  |

f.3.2: Mezzera continuous scouring

| Department | Preparation |
| --- | --- |
| Fabric | SILK-SILK/OTHER |
| Process | Mezzera continuous scouring |
| Equipment | Mezzera |
| Item | VBM1 |
| Number of cycles/yr | 22 |
| Cycle time (h) | 158 |
| Processed fabric (kg/yr) | 65130 |
| Processed fabric per hour (kg/h) | 19 |

| Water type W5: equip. volume + 3000 l (reintegration) Detergent (10070) = 3 g/l: Detergent (10452) = 1 g/l; Sodium carbonate (10175) = 0,5 g/l. Steam type S1 Water type W5: 4500 l/h . Sequestering-dispersant agent (10299) = 3 g/l. Water type W6.: 4500 l/h | Bath T= 98°C; Indirect heating Neutralization Washing Wringing | Discharge type D2: equip. volume T [°C]= 92; pH [-]= 8,5; Conductivity [mS/cm]= 7,89; COD [mg/l]= 21450; TSS [mg/l]= 60. Discharge type.D2: 4500 l/h T [°C]= 70; pH [-]= 7,6; Conductivity [mS/cm]= 0,75; COD [mg/l]= 395; TSS [mg/l]= 5. Discharge type.D4: 4500 l/h T [°C]= 20; pH [-]= 7,9; Conductivity [mS/cm]= 0,19; COD [mg/l]= 50; TSS [mg/l]= 5. Discharge type D4:.3000 l T [°C]= 20; pH [-]= 7,9; Conductivity [mS/cm]= 0,19; COD [mg/l]= 50; TSS [mg/l]= 5. |  |
| --- | --- | --- | --- |

Notes:

F.3.3. Stella scouring

| Department | Preparation |
| --- | --- |
| Fabric | SILK-SILK/OTHER |
| Process | Stella scouring |
| Equipment | Stella |
| Item | STP1-STP2/ STM1-STM2/ STG1 |
| Run time (h) |  |
| Number of run/yr | 772/ 270/ 594 |
| Processed fabric (kg/yr) | 8105/ 10131/ 44578 |
| Processed fabric per run (kg) | 10/ 37/ 75 |

| Water type W5:equip volume Detergent (10070) = 20 g/l; Steam type S1 | Bath T=90°C; t=120 min. Indirect heating |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Discharge |  | Discharge type D2: equip. volume T [°C]= 95; pH [-]= 9,75; Conductivity [mS/cm]= 1,22; COD [mg/l]= 27850; TSS [mg/l]= 430. |  |  |
| Water type W5:equip volume Sequestering-dispersant agent (10299) = 4 g/l. | 1st washing |  |  |  |  |
|  | Discharge |  | Discharge type D2: equip. volume T [°C]= 70; pH [-]= 9,78; Conductivity [mS/cm]= 0,68; COD [mg/l]= 2100; TSS [mg/l]= 25. |  |  |
| Water type W4:equip volume | 2nd washing |  |  |  |  |
|  | Discharge |  | Discharge type D5: equip. volume T [°C]= 40; pH [-]= 8,1; Conductivity [mS/cm]= 0,35; COD [mg/l]= 1200; TSS [mg/l]= 12. |  |  |
| Water type W4:equip volume | 3rd washing |  |  |  |  |
|  | Discharge |  | Discharge type D5: equip. volume T [°C]= 27; pH [-]= 7,9; Conductivity [mS/cm]= 0,25; COD [mg/l]= 500; TSS [mg/l]= 10. |  |  |

Notes: