An.H: Finishing- Process scheme.

- H1: Yarn softener finishing;

- H 1.1: Softener finishing (Morbidol®)

- H1.2: Softener finishing (Rucofil®)

- H1.3: Softener finishing (Destofil®)

- H1.4: Softener finishing (Ceranina®)

- H2: Antistatic finishing.

- H3: Fabric softener finishing(Recolsoft®)

- H4: Fabric water finishing

H1:Yarn softener finishing

H1.1:Softener finishing (Morbidol®)

| Department | Finishing |
| --- | --- |
| Yarn | SILK |
| Process | Softener finishing (Morbidol®) |
| Equipment | Autoclave |
| Item | A-B-C/ 31-32-33-34/ 51-52/ 102-103-104-105-106-107/ 203-204/ 301-302 |
| Number of run/year | 881/ 275/ 286/ 99/ 168/ 53/36 |
| Run time (h) | 0,75 |
| Processed yarn (kg/yr) | 8811/ 6609/ 33043/ 8927/ 33515/ 16000/ 21723 |
| Processed yarn per run (kg) | 10/ 24/ 40/ 90/ 200/ 300/ 600 |

| Water type W5: equipment volume Softener (10344) = 3%; Acetic acid (10002)= 2 g/l. Steam type S1 | Bath T=30°C t=30 min Indirect heating |  |  |
| --- | --- | --- | --- |
|  | Discharge | Discharge type D5: equip. volume T [°C]=30 ; pH [-]= 5,4; Conductivity [mS/cm]= 0,31; COD [mg/l]= 1200; TSS [mg/l]= 30. |  |

|  | Centrifugation |  |
| --- | --- | --- |

|  | Drying |  |
| --- | --- | --- |

Notes:

H1.2:Softener finishing (Rucofil®)

| Department | Finishing |
| --- | --- |
| Fabric | SILK |
| Process | Softener finishing (Rucofil®) |
| Equipment | Autoclave |
| Item | A-B-C/ 31-32-33-34/ 51-52/ 102-103-104-105-106-107/ 203-204/ 301-302 |
| Number of cycles/year | 706/ 392/ 817/ 96/ 124/ 39/ 17 |
| Run time (h) | 0,75 |
| Processed yarn (kg/yr) | 7062/ 9401/ 32678/ 8605/ 24705/ 11770/ 10402 |
| Processed yarn per run (kg) | 10/ 24/ 40/ 90/ 200/ 300/ 600 |

| Water type W5: equipment volume Softener (10455) = 1,5%; Acetic acid (10002)= 3 g/l. Steam type S1 | Bath T=30°C t=30 min Indirect heating |  |  |
| --- | --- | --- | --- |
|  | Discharge | Discharge type D5: equip. volume T [°C]= 30; pH [-]= 3,06; Conductivity [mS/cm]= 0,63; COD [mg/l]= 1436; TSS [mg/l]= 27. |  |

|  | Centrifugation |  |
| --- | --- | --- |

|  | Drying |  |
| --- | --- | --- |

Notes:

H1.3:Softener finishing (Destofil®)

| Department | Finishing |
| --- | --- |
| Yarn | SILK |
| Process | Softener finishing (Destofil®) |
| Equipment | Autoclave |
| Item | A-B-C/ 31-32-33-34/ 51-52/ 102-103-104-105-106-107/ 203-204/ 301-302 |
| Number of cycles/year | 628/ 196/ 589/ 72/ 100/ 40/ 18 |
| Run time (h) | 0,75 |
| Processed yarn (kg/yr) | 6282/ 4712/ 23558/ 6448/ 20087/ 11903/ 10911 |
| Processed yarn per run (kg) | 10/ 24/ 40/ 90/ 200/ 300/ 600 |

| Water type W5: equipment volume Softener (10302) = 2%; Acetic acid (10002)= 3 g/l. Steam type S1 | Bath T=30°C t=30 min Indirect heating |  |  |
| --- | --- | --- | --- |
|  | Discharge | Discharge type D5: equip. volume T [°C]= 30; pH [-]= 3,7; Conductivity [mS/cm]= 0,32; COD [mg/l]= 1745; TSS [mg/l]= 24. |  |

|  | Centrifugation |  |
| --- | --- | --- |

|  | Drying |  |
| --- | --- | --- |

Notes:

H1.4:Softener finishing (Ceranina®)

| Department | Finishing |
| --- | --- |
| Yarn | ACETATE |
| Process | Softener finishing (Ceranina®) |
| Equipment | Autoclave |
| Item | 51-52/ 102-103-104-105-106-107 |
| Number of run/year | 132/ 5 |
| Run time (h) | 0,75 |
| Processed yarn (kg/yr) | 5269/ 439 |
| Processed yarn per run (kg) | 40/ 90 |

| Water type W5: equipment volume Softener (10092) = 0,8%; Acetic acid (10002)= 1 g/l. Steam type S1 | Bath T=30°C t=30 min Indirect heating |  |  |
| --- | --- | --- | --- |
|  | Discharge | Discharge type D5: equip. volume T [°C]= 30; pH [-]= 4,8; Conductivity [mS/cm]= 0,45; COD [mg/l]= 1005; TSS [mg/l]= 30 . |  |

|  | Centrifugation |  |
| --- | --- | --- |

|  | Drying |  |
| --- | --- | --- |

Notes:

H2: Yarn antistatic finishing

| Department | Finishing |
| --- | --- |
| Yarn | Nylon |
| Process | Antistatic finishing |
| Equipment | Autoclave |
| Item | 102-103-104-105-106-107/ 203-204 |
| Number of run/year | 22/ 3 |
| Run time (h) | 0,75 |
| Processed yarn (kg/yr) | 1976/ 659 |
| Processed yarn per run (kg) | 90/ 200 |

| Water type W5: equipment volume Antistatic agent (10360)= 1%; Acetic acid (10002)= 1 g/l. Steam type S1 | Bath T=30°C t=30 min Indirect heating |  |  |
| --- | --- | --- | --- |
|  | Discharge | Discharge type D5: equip. volume T [°C]= 30; pH [-]= 4,5; Conductivity [mS/cm]= 0,32; COD [mg/l]= 1625; TSS [mg/l]= 50. |  |

|  | Centrifugation |  |
| --- | --- | --- |

|  | Drying |  |
| --- | --- | --- |

Notes:

H.3:Fabric softener finishing

| Department | Finishing |
| --- | --- |
| Fabric | SILK-SILK/OTHER |
| Process | Softener finishing (Recolsoft®) |
| Equipment | Rameuse |
| Item | FM01-FM02 |
| Number of cycles/year | 96-96 |
| Cycle time (h) | 14,5 |
| Processed fabric (kg/yr) | 57893-57893 |
| Processed fabric per hour (kg/h) | 41,6-41,6 |

| Water type W4: 58 l/h. Softener (10431) = 20 g/l | Doping Wringing Thermosetting (T=130°C) | Discharge type D5: 100 l/cycle T [°C]= 18; pH [-]= 7,83; Conductivity [mS/cm]= 0,35; COD [mg/l]= 8000; TSS [mg/l]= 150. |
| --- | --- | --- |

Notes:

H.3:Fabric softener finishing

| Department | Finishing |
| --- | --- |
| Fabric | SILK-SILK/OTHER |
| Process | Water finishing |
| Equipment | Rameuse |
| Item | FM01-FM02 |
| Number of cycles/year | 145-145 |
| Cycle time (h) | 14,5 |
| Processed fabric (kg/yr) | 86840-86840 |
| Processed fabric per hour (kg/h) | 41,6-41,6 |

| Water type W4: 87 l/h. | Doping Wringing Thermosetting (T=130°C) | Discharge type D5: 100 l/cycle T [°C]= 20; pH [-]= 7,98; Conductivity [mS/cm]= 0,22; COD [mg/l]= 313; TSS [mg/l]= 15. |
| --- | --- | --- |