An.1: Material flow chart

An.2: Energetic flow chart

An.3: Water flow chart

An.5.b: Continuous process scheme

| Department | piece dyeing |
| --- | --- |
| Fabric | CO |
| Process | pretreatment: boiling, desizing, bleaching |
| Equipment | pretreatment line |
| Item | PT1 |
| Operating | continuous |
| Number of cycles/yr |  |
| Cycle time (h) |  |
| Processed fabric (kg/yr) | 5 796 000 |
| Processed fabric per hour (kg/h) | 1500 |

On the pretreatment line 2 types of treatment are done:

boiling and desizing

desizing and bleaching

The water use depends on the weight of textile treated, the water use is set at 8 l/kg. The heavier the textile material, the more water is used.

| Desizing/boiling: 30% of production on PT1 Water (desizing): 1 l/kg (100% uptake) enzyme: 3 ml/l complex-binding agent: 3 ml/l wetting agent: 3 ml/l Water (boiling): 0.6 l/kg (60% uptake) alkali dispersing agent detergent Water: 8 l/kg detergent: 2 ml/kg wetting agent: 2 ml/kg Desizing/bleaching: 70% of production on PT1 Water (desizing): 1 l/kg (100% uptake) enzyme: 3 ml/l complex-binding agent: 3 ml/l wetting agent: 3 ml/l Water (bleaching): 0.6 l/kg (60% uptake) H2O2 (50%): 35 ml/kg NaOH (30%): 45 ml/kg stabilising agent: 6 ml/kg dispersing agent: 3 ml/kg Water: 8 l/kg detergent: 2 ml/kg wetting agent: 2 ml/kg | combined desizing and boiling (products dosed in 2 separate padders) rinsing combined desizing and bleaching (products dosed in 2 separate padders) rinsing | Discharge of a concentrated solution Analysis of mixed stream (concentrated streams and rinsing water): T [°C]= 70-95 pH [-]= 11 Conductivity [mS/cm]=2.65 COD [mg/l]=19 300 BOD [mg/l]=6 180 SST [mg/l]=1 590 Discharge of a concentrated solution Analysis of mixed stream (concentrated streams and rinsing water): 3 sets of data (different fabric quality) T [°C]=70-95 pH [-]=11.8 Conductivity [mS/cm]=6.72 COD [mg/l]=15 300 BOD [mg/l]=4 870 SST [mg/l]= 437 T [°C]=70-95 pH [-]=11.6 Conductivity [mS/cm]=6.09 COD [mg/l]=11 000 BOD [mg/l]=4 590 SST [mg/l]= 1 410 T [°C]=70-95 pH [-]=11.9 Conductivity [mS/cm]=7.33 COD [mg/l]=14 300 BOD [mg/l]=178 SST [mg/l]= 1 100 |  |
| --- | --- | --- | --- |

An.5.b: Continuous process scheme

| Department | piece dyeing |
| --- | --- |
| Fabric | CO |
| Process | dyeing / topping (vat dyes, sulphur dyes, direct dyes) followed by a rinsing step |
| Equipment | pad-steam |
| Item | PS1 |
| Operating | continuous |
| Number of cycles/yr |  |
| Cycle time (h) |  |
| Processed fabric (kg/yr) | 7 507 000 |
| Processed fabric per hour (kg/h) | 1 700 |

Some of the fabrics (ecru status, which means that they aren't dyed yet) are dyed and afterwards rinsed on the pad-steam.

Other fabrics (dyed status) have already been dyed as a yarn and are topped (which means dyed again) and rinsed on the pad-steam.

| Sulphur dyeing: 60% of production on PS1 Water: 0.7 l/kg (70% uptake) sulphur dyes: 0-250 g/l reducing agent: 5 ml/l wetting agent: 3 ml/l defoaming agent: 0.25 ml/l water: 0.6 l/kg (60% uptake) NaOH:(30%): 30 ml/l glucose monohydrate: 40 g/l NaCl: 50 g/l complexing agent: 5 ml/l water: 10 l/kg water: 0.6 l/kg (60% uptake) oxidising agent: 5 g/l acetic acid: 4 g/l Vat dyeing: 25% of production on PS1 Water: only for the preparation of the dyebath: 0.7 l/kg (70% uptake) vat dyes: 0-50 g/l anti-migration agent: 10 ml/l wetting agent: 3 ml/l defoaming agent: 0.25 ml/l water: 0.6 l/kg (60% uptake) NaOH:(30%): 100 ml/l sodiumhydrosulfite: 50 g/l complexing agent: 5 ml/l water: 10 l/kg water: 0.6 l/kg (60% uptake) oxidising agent: 5 g/l Direct dyeing: 15% of production on PS1 Water: 0.7 l/kg (70% uptake) direct dyes: 0-50 g/l wetting agent: 3 ml/l water: 0.6 l/kg (60% uptake) salt: 100 g/l complexing agent: 5 ml/l water: 10 l/kg |  | dyed / topped reduction rinsing oxidation dyed / topped reduction rinsing oxidation dyed / topped addition of salt rinsing | Discharge of padder liquor containing a concentrated solution of auxiliaries and dyestuff T [°C]=20 pH [-]=12.24 (after 20x dilution with demiwater, pH 6.8) Conductivity [mS/cm]=6.23 (after 40x dilution with demiwater, cond. 0) COD [mg/l]= 122 320 SST [mg/l]= >2800 dark color: black T [°C]=50 pH [-]= 3.6 Conductivity [mS/cm]=5.81 COD [mg/l]=4 360 BOD [mg/l]=2 780 light color: brownish T [°C]=50 pH [-]= 4.0 Conductivity [mS/cm]=4.11 COD [mg/l]=4 570 BOD [mg/l]=171 Discharge of padder liquor containing a concentrated solution of auxiliaries Discharge of padder liquor containing a concentrated solution of auxiliaries and dyestuff T [°C]=50 pH [-]=11 COD [mg/l]=1 800 BOD [mg/l]=280 Discharge of padder liquor containing a concentrated solution of auxiliaries Discharge of padder liquor containing a concentrated solution of auxiliaries and dyestuff Discharge of padder liquor containing a concentrated solution of auxiliaries T [°C]=40 pH [-]=8 COD [mg/l]=8 120 SST [mg/l]=150 |  |
| --- | --- | --- | --- | --- |

An.5.b: Continuous process scheme

| Department | piece dyeing |
| --- | --- |
| Fabric | CO |
| Process | finishing |
| Equipment | sanfor |
| Item | SF1-2 |
| Operating | continuous |
| Number of cycles/yr |  |
| Cycle time (h) |  |
| Processed fabric (kg/yr) | 7 507 000 (SF1) + 9 270 000 (SF2) |
| Processed fabric per hour (kg/h) | 1700 (on each of the sanfors) |

The most important finish is softening and to make the fabric unshrinkable.

| Water use: max. 5 m³/h used for the preparation of finishing bath, to cool the rubber band, to sprinkle on the fabric (to make unshrinkable) and to clean the machinery afterwards finishing products | finishing | Discharge of concentrated solutions and rinsing of machinery: very low flow rate, very much varying in quantity and quality |  |
| --- | --- | --- | --- |

(*):refer to An.9

An.5.b: Continuous process scheme

| Department | yarn dyeing |
| --- | --- |
| Fabric | CO |
| Process | dyeing (indigo, vat dyes, sulphur dyes) and rinsing |
| Equipment | warp dyeing line |
| Item | WDL1-4 |
| Operating | continuous |
| Number of cycles/yr |  |
| Cycle time (h) |  |
| Processed fabric (kg/yr) | 9 480 000 (for all 4) |
| Processed fabric per hour (kg/h) | 350 |

| vat dyeing: 15% of production on WDL1-4 vat dyestuff: 0-50 g/l water: 1 l/kg (100% uptake) wetting agent: 2 ml/l complexing agent:2 g/l defoaming agent: 0.25 ml/l water: 0.2 l/kg (20% uptake) NaOH (30°Bé): 65 ml/l sodiumhydrosulfite: 20 g/l antrachinone: 1.5 g/l water: 4 m³/h oxidising agent: 5 g/l | dyeing reduction rinsing oxidation | Discharge of padder liquor containing a concentrated solution of auxiliaries and dyestuff Discharge of padder liquor containing a concentrated solution of auxiliaries Discharge type: 4 m³/h T [°C]=20 pH [-]=11.92 Conductivity [mS/cm]=14.11 COD [mg/l]=5463 SST [mg/l]=272 Discharge of padder liquor containing a concentrated solution of auxiliaries |
| --- | --- | --- |

| dyeing of indigo: 50% of production on WDL1-4 water for wetting: groundwater: 1 l/kg (100% uptake) water for rinsing: recuperated from rinsing section after dyeing wetting agent: 2 ml/l complexing agent: 7.5 ml/l indigo dyestuff: 5.5 g/l water: 0.25 l/kg (25% uptake) NaOH (30°Bé): 25 ml/kg stabilising agent: 20 g/kg indigo dyestuff: 9.5 g/l water: 0.25 l/kg (25% uptake) NaOH (30°Bé): 25 ml/kg stabilising agent: 20 g/kg water: 3 m³/h water: 0.6 l/kg (60% uptake) oxidising agent: 5 g/l acetic acid |  | wetting/rinsing dyeing OR dyeing rinsing oxidation (only for dark shades, i.e. 10% of indigo dyeing) |  | sample taken from rinsing section after wetting T [°C]=20 pH [-]=9.96 Conductivity [mS/cm]=10.88 COD [mg/l]=4611 SST [mg/l]=1246 Discharge of padder liquor containing a concentrated solution of auxiliaries and dyestuff T [°C]=20 pH [-]= 10.88 (after 40x dilution with demiwater, pH 6.8) Conductivity [mS/cm]= 2.75 (after 40x dilution with demiwater, cond. 0) COD [mg/l]= 12300 SST [mg/l]= >3000 Discharge of padder liquor containing a concentrated solution of auxiliaries and dyestuff T [°C]=20 pH [-]= 11.38 (after 20x dilution with demiwater, pH 6.8) Conductivity [mS/cm]= 4.63 (after 20x dilution with demiwater, cond. 0) COD [mg/l]= 36440 SST [mg/l]= >2700 rinsing water is recuperated for rinsing after wetting or alkali treatment) Discharge type: 3 m³/h T [°C]=20 pH [-]=10.82 Conductivity [mS/cm]=13.15 COD [mg/l]=3205 SST [mg/l]=1423 Discharge of padder liquor containing a concentrated solution of auxiliaries T [°C]=36 pH [-]=5 COD [mg/l]=5500 SST [mg/l]=<20 |
| --- | --- | --- | --- | --- |

| sulphur dyeing: 35% of production on WDL1-4 water for wetting: groundwater: 1 l/kg (100% uptake) water for rinsing: recuperated from rinsing section after dyeing wetting agent: 2 ml/l complexing agent: 7.5 ml/l water for alkali treatment: groundwater: 1 l/kg (100% uptake) water for rinsing: recuperated water from rinsing section after dyeing NaOH (10°Bé or 20°Bé: depending on the depth of the colour): 460 ml/m wetting agent: 2 ml/l complexing agent: 10 ml/l sulphur dyestuff:: 0-250 g/l water: 1 l/kg (100% uptake) NaHS 30%: 5 ml/l wetting agent: 2 ml/l complexing agent:2 g/l defoaming agent: 0.25 ml/l water: 4 m³/h water: 0.6 l/kg (60% uptake) oxidising agent: 5 g/l acetic acid: 4 g/l water: 0.6 l/kg (60% uptake) cationic fixation agent: 20 l/h | wetting/rinsing or alkali treatment/rinsing (only for black) dyeing (in many cases, wetting is combined with dyeing) rinsing oxidation cationic fixation: only 20% of sulphur dyeing on WDL1-4 | sample taken from rinsing section after wetting T [°C]= pH [-]=11.35 Conductivity [mS/cm]=9.64 COD [mg/l]=3888 SST [mg/l]= 356 sample taken from rinsing section after alkali treatment T [°C]= pH [-]= 13.65 Conductivity [mS/cm]= 117.1 COD [mg/l]= 38 160 SST [mg/l]= 136 Discharge of padder liquor containing a concentrated solution of auxiliaries and dyestuff: sample of dark shade (black colour) T [°C]= 20 pH [-]= Conductivity [mS/cm]= COD [mg/l]= 122 320 SST [mg/l]= rinsing water is recuperated for rinsing after wetting or alkali treatment Discharge type: 4 m³/h T [°C]=20 pH [-]=12.53 Conductivity [mS/cm]=21.1 COD [mg/l]=6326 SST [mg/l]=1007 Discharge of padder liquor containing a concentrated solution of auxiliaries Discharge of padder liquor containing a concentrated solution of auxiliaries |
| --- | --- | --- |