An.1: Material flow chart

An.2: Energetic flow chart

An. 3: Water flow chart

An.5a: Batch process scheme.

| Department | yarn dyeing |
| --- | --- |
| Yarn | CO |
| Process | reactive or vat dyeing of cotton yarn |
| Equipment | bobine autoclaves |
| Item | AU1-11 |
| Run time (h) |  |
| Number of run/yr | 3113 |
| Processed yarn (kg/yr) | 1 463 200 |
| Processed yarn per run (kg) | 470 |

No sampling possible on this machinery.

Reactive dyeing: 50% of production on AU1-11

| Water: 3300 l reactive dyestuff wetting agent: 0.2 g/l anti-reduction agent salt levelling agent: 0.03g/l thickener alkali | reactive dyeing |  | Discharge: 3300 l – uptake by yarn |  |
| --- | --- | --- | --- | --- |
| Water: 3300 l | rinsing |  | Discharge : 3300 l |  |
| Water: 3300 l detergent: 0.18 g/l | soaping |  | Discharge : 3300 l |  |
| Water: 3300 l fixation agent: 0.04 g/l | fixation |  | Discharge : 3300 l |  |
| Water: 3300 l softening agent: 0.87 g/l | softening |  | Discharge : 3300 l |  |

Vat dyeing: 50% of production on AU1-11

| Water: 3300 l vat dyestuff wetting agent: 0.2 g/l NaHSO3 levelling agent: 0.02 g/l thickener dispersing agent: 0.11 g/l | vat dyeing |  | Discharge: 3300 l – uptake by yarn |  |
| --- | --- | --- | --- | --- |
| Water: 3300 l | rinsing |  | Discharge: 3300 l |  |
| Water: 3300 l | oxidation |  | Discharge: 3300 l |  |
| Water: 3300 l detergent: 0.18 g/l | soaping |  | Discharge: 3300 l |  |
| Water: 3300 l softening agent: 0.87 g/l | softening |  | Discharge: 3300 l |  |

An.5.b: Continuous process scheme

| Department | pretreatment |
| --- | --- |
| Fabric | CO |
| Process | combined desizing and bleaching |
| Equipment | pretreatment line |
| Item | PT1 |
| Operating | continuous |
| Number of cycles/yr |  |
| Cycle time (h) |  |
| Processed fabric (kg/yr) | 5 852 800 |
| Processed fabric per hour (kg/h) | 2400 |

| Water: 130 l/min recuperated water from last rinsing section NaOH NaCO3 H2O2 sodiumsilicate stabilisers for H2O2 based on polyacrylates 0.14 g/l water: 30 l/min hypochlorite water: 140 l/min fresh water + 130 l/min recuperated water from last rinsing section water: 30 l/min H2O2 water: 260 l/min fresh water | desizing/rinsing bleaching steamer rinsing bleaching steamer rinsing drying | no discharge: this water is led to the ultrafiltration unit for recuperation of size and water pH [-]=5.5 Conductivity [mS/cm]=14.08 COD [mg/l]=37400 no discharge Discharge type: 270 l/min pH [-]=9.3 Conductivity [mS/cm]=3.94 COD [mg/l]=1670 SST [mg/l]= 54 no discharge no discharge since this water is recuperated first compartment T [°C]=80 pH [-]=10 Conductivity [mS/cm]=2.87 COD [mg/l]=2320 SST [mg/l]=153 third compartment T [°C]=60-80 pH [-]=6.9 Conductivity [mS/cm]=1.25 COD [mg/l]=636 SST [mg/l]=12 last compartment T [°C]=60 pH [-]=7.6 Conductivity [mS/cm]=1.19 COD [mg/l]=123 SST [mg/l]=21 |  |
| --- | --- | --- | --- |

An.5.b: Continuous process scheme

| Department | piece dyeing |
| --- | --- |
| Fabric | cotton |
| Process | reactive or vat dyeing of cotton |
| Equipment | pad-steam |
| Item | PS1 |
| Operating | continuous |
| Number of cycles/yr |  |
| Cycle time (h) |  |
| Processed fabric (kg/yr) | 4 791 231 |
| Processed fabric per hour (kg/h) | 2700 |

Water use is optimised on this line: effluent of one compartment flows over in another. Re-use scheme is process dependent.

Reactive dyeing: 57% of production on PS1

| Water reactive dyestuff wetting agent: 0.19 g/l anti-reduction agent salt levelling agent: 0.02g/l thickener alkali water: 100-250 l/min (depending on the weight of the fabric) water (l/min): 115 water: 60 l/min detergent: 0.18 g/l water: 140 l/min (of which 60 l/min comes from fixation compartment) water: 60 l/min fixation agent: 0.04g/l softening agent: 0.87 g/l | reactive dyeing steamer water seal rinsing soaping rinsing fixation softening | padder liquid is discharged (150 l) T [°C]=40 pH [-]=9.5 Conductivity [mS/cm]=13 COD [mg/l]=196 SST [mg/l]=<20 T [°C]=30 pH [-]=6.6 Conductivity [mS/cm]=4.37 COD [mg/l]=1120 SST [mg/l]=<20 T [°C]=95 pH [-]=8.4 Conductivity [mS/cm]=1.47 COD [mg/l]=1180 SST [mg/l]=<20 T [°C]=60-70 pH [-]=8.4 Conductivity [mS/cm]=1.19 COD [mg/l]=202 SST [mg/l]=<20 T [°C]=40 pH [-]=8.1 Conductivity [mS/cm]=1.51 COD [mg/l]=624 SST [mg/l]= <20 |  |
| --- | --- | --- | --- |

Vat dyeing: 43% of production on PS1

| Water vat dyestuff wetting agent: 0.2 g/l levelling agent: 0.02 g/l thickener NaHSO3 dispersing agent: 0.11 g/l water: 100-250 l/min (depending on the weight of the fabric) water: 120 l/min water: 40 l/min H2O2 water: 40 l/min detergent: 0.18 g/l water: 100 l/min softening agent: 0.87 g/l | vat dyeing steamer water seal rinsing oxidising soaping rinsing softening | padder liquid is discharged (150 l) T [°C]=40 pH [-]=10.8 Conductivity [mS/cm]=8.66 COD [mg/l]=989 SST [mg/l]= <20 T [°C]=30 pH [-]=10 Conductivity [mS/cm]=3.36 COD [mg/l]=352 SST [mg/l]= <20 T [°C]=60 pH [-]=8.5 Conductivity [mS/cm]=1.15 COD [mg/l]=240 SST [mg/l]= <20 T [°C]=95 pH [-]=8.6 Conductivity [mS/cm]=1.17 COD [mg/l]=364 SST [mg/l]= <20 T [°C]=60 pH [-]=8.0 Conductivity [mS/cm]=1.22 COD [mg/l]=37 SST [mg/l]= <20 |
| --- | --- | --- |