An.1: Material flow chart

An.2: Energetic flow chart

An.3: Water flow chart

An.5.b: Continuous process scheme

| Department | pretreatment |
| --- | --- |
| Fabric | all kind (mostly CO) |
| Process | bleaching bleaching and oxidative desizing enzymatic desizing |
| Equipment | pad-batch |
| Item | PB1 |
| Operating | semi-continuous |
| Number of cycles/yr |  |
| Cycle time (h) |  |
| Processed fabric (kg/yr) | 4158109 |
| Processed fabric per hour (kg/h) | 3462 |

The 3 mentioned processes are not done after each other: it is always 1 of the 3.

| Bleaching: 18% of production on PB1 - water - NaOH - H2O2 - stabilising agent - detergent Bleaching+oxidative desizing: 64% of production on PB1 - water - NaOH - H2O2 - stabilising agent - detergent - persulphate Enzymatic desizing (heavy fabrics): 18% of production on PB1 - water - detergent - enzymes | bleaching = padding the cold solution on the fabric on the PB1 OR bleaching and desizing = padding the cold solution on the fabric on the PB1 OR enzymatic desizing = padding the hot solution on the fabric on the PB1 AND dwelling the padded rolls to let the solution react with the fabric | Discharge type : discharge of padder solution Bleaching T [°C]= ambient temp. pH [-]=13.22 Conductivity [mS/cm]=130.3 COD [mg/l]=18 700 BOD [mg/l]= <10 SST [mg/l]= 160 Bleaching+oxidative desizing T [°C]= ambient temp pH [-]=12.93 Conductivity [mS/cm]=160.1 COD [mg/l]=19 300 BOD [mg/l]= <10 SST [mg/l]= 108 Enzymatic desizing (heavy fabrics) T [°C]= 70°C pH [-]=7.27 Conductivity [mS/cm]=20.3 COD [mg/l]=36 280 BOD [mg/l]= 21 970 SST [mg/l]= 544 |  |
| --- | --- | --- | --- |

An.5.b: Continuous process scheme

| Department | pretreatment |
| --- | --- |
| Fabric | all kind |
| Process | bleaching (and desizing) followed by rinsing |
| Equipment | rakojet |
| Item | RJ1 |
| Operating | continuous |
| Number of cycles/yr |  |
| Cycle time (h) |  |
| Processed fabric (kg/yr) | 5696040 |
| Processed fabric per hour (kg/h) | 1502 |

Everything treated on PB1 goes also through RJ1.

90% of PES/CO is only pre-treated on the RJ1.

| Water: 3 l/kg water NaOH (50%): 12 ml/kg H2O2 (200 vol%): 15 ml/kg stabilising agent: 3 ml/kg detergent: 7 ml/kg water: 5 l/kg water: 1 l/kg formic acid | rinsing of 100% CO (already bleached on PB1) 14% of production on RJ1 rakojet + steamer (bleaching) rinsing neutralising | Discharge type : counter current stream over 3 compartments T [°C]=90°C pH [-]=11.5 Conductivity [mS/cm]=3.91 COD [mg/l]=3120 BOD [mg/l]=854 SST [mg/l]= 47 Discharge type: counter current stream over 4 compartments T [°C]=90 pH [-]=11.8 Conductivity [mS/cm]=4.22 COD [mg/l]=1850 BOD [mg/l]=<10 SST [mg/l]= <20 1 compartment |  |
| --- | --- | --- | --- |

| Water: 3 l/kg water NaOH (50%): 12 ml/kg H2O2 (200 vol%): 15 ml/kg stabilising agent: 3 ml/kg detergent: 7 ml/kg water: 5 l/kg water: 1 l/kg formic acid | rinsing of 100% CO (already bleached and oxidative desized on PB1) 28% of production on RJ1 rakojet + steamer (bleaching) rinsing neutralising | Discharge type : counter current stream over 3 compartments, T [°C]=90 pH [-]=12.6 Conductivity [mS/cm]=2.07 COD [mg/l]=8660 BOD [mg/l]=3230 SST [mg/l]= 114 Discharge type: counter current stream over 4 compartments T [°C]=90 pH [-]=11.6 Conductivity [mS/cm]=4.9 COD [mg/l]=1920 BOD [mg/l]=<10 SST [mg/l]= 23 1 compartment |
| --- | --- | --- |

| Water : 3 l/kg water NaOH (50%): 40 ml/kg H2O2 (200 vol%): 50 ml/kg stabilising agent: 10 ml/kg detergent: 20 ml/kg water: 5 l/kg water: 1 l/kg formic acid | rinsing of 100% CO (already enzymatic desized on PB1) 5% of production on RJ1 rakojet + steamer rinsing neutralising | Discharge type : counter current stream over 3 compartments, T [°C]=90 pH [-]=7.9 Conductivity [mS/cm]=3.91 COD [mg/l]=10 900 BOD [mg/l]=4 020 SST [mg/l]= 189 Discharge type: counter current stream over 4 compartments T [°C]=90 pH [-]=12.4 Conductivity [mS/cm]=13.4 COD [mg/l]=4 910 BOD [mg/l]=<10 SST [mg/l]= 59 1 compartment |
| --- | --- | --- |
| Water: 3 l/kg water NaOH (50%): 40 ml/kg H2O2 (200 vol%): 50 ml/kg stabilising agent: 10 ml/kg detergent: 20 ml/kg water: 5 l/kg water: 1 l/kg formic acid | wetting of not sized fabric (PES/CO) 30% of production on RJ1 rakojet + steamer (bleaching) rinsing neutralising | Discharge type : counter current stream over 3 compartments, T [°C]=90 pH [-]=8.7 Conductivity [mS/cm]=2.35 COD [mg/l]=1930 BOD [mg/l]=934 SST [mg/l]= 26 Discharge type: counter current stream over 4 compartments T [°C]=90 pH [-]=12.1 Conductivity [mS/cm]=8.01 COD [mg/l]=4770 BOD [mg/l]=<10 SST [mg/l]=20 1 compartment |

| Water: 3 l/kg water NaOH (50%): 40 ml/kg H2O2 (200 vol%): 50 ml/kg stabilising agent: 10 ml/kg detergent: 20 ml/kg water: 5 l/kg water: 1 l/kg formic acid | wetting of sized fabric (PES/CO) 23% of production on RJ1 rakojet + steamer (bleaching) rinsing neutralising | Discharge type : counter current stream over 3 compartments, T [°C]=90 pH [-]=7.5 Conductivity [mS/cm]=3.68 COD [mg/l]=7 900 BOD [mg/l]=3 250 SST [mg/l]=89 Discharge type: counter current stream over 4 compartments T [°C]=90 pH [-]=12 Conductivity [mS/cm]=8.44 COD [mg/l]=4 870 BOD [mg/l]=<10 SST [mg/l]=43 1 compartment |
| --- | --- | --- |

An.5.b: Continuous process scheme

| Department | pre-treatment |
| --- | --- |
| Fabric | all kind (mostly CO and PES/CO) |
| Process | mercerising |
| Equipment | mercerising line |
| Item | ML1 |
| Operating | continuous |
| Number of cycles/yr |  |
| Cycle time (h) |  |
| Processed fabric (kg/yr) | 4756500 |
| Processed fabric per hour (kg/h) | 1360 |

| Water NaOH (24°Baumé): dosed continuously water water formic acid (to get pH 4 on the fabric) | mercerising 100% CO 50% of production on ML1 rinsing 100% CO neutralising 100% CO |  | Discharge: 5 m³/h T [°C]= 85 This stream contains high concentrations of NaOH. A recuperation unit is present to recuperate both the water and the NaOH (in a more concentrated form) neutralising is done in counter current (fabric and water) and all the water is discharged in compartment 1 (ie 6.5 m³/h) compartment 1: discharge: 6.5 m³/h T [°C]=85 pH [-]=3.8 Conductivity [mS/cm]=4.91 COD [mg/l]=1 480 BOD [mg/l]=307 SST [mg/l]=<20 compartment 2: water flows in compartment 1 T [°C]=50 pH [-]=3.2 Conductivity [mS/cm]=3.2 COD [mg/l]=1 860 BOD [mg/l]=<10 SST [mg/l]=<20 compartment 3: water flows in compartment 2 T [°C]=40 pH [-]=3.1 Conductivity [mS/cm]=2.71 COD [mg/l]=1 580 BOD [mg/l]=<10 SST [mg/l]=<20 |  |
| --- | --- | --- | --- | --- |

| Water NaOH (24°Baumé): dosed continuously water water formic acid (to get pH 4 on the fabric) | mercerising PES/CO (67/33) 50% of production on ML1 rinsing PES/CO (67/33) neutralising PES/CO (67/33) | Discharge: 5 m³/h This stream contains high concentrations of NaOH. A recuperation unit is present to recuperate both the water and the NaOH (in a more concentrated form) neutralising is done in counter current (fabric and water) and all the water is discharged in compartment 1 (ie 6.5 m³/h) compartment 1: discharge: 6.5 m³/h T [°C]= pH [-]=10 Conductivity [mS/cm]=3.75 COD [mg/l]=950 BOD [mg/l]=280 SST [mg/l]=<20 compartment 2: water flows in compartment 1 T [°C]= pH [-]=3.7 Conductivity [mS/cm]=3.19 COD [mg/l]=1 110 BOD [mg/l]=208 SST [mg/l]=<20 compartment 3: water flows in compartment 2 T [°C]= pH [-]=3.6 Conductivity [mS/cm]=2.47 COD [mg/l]=896 BOD [mg/l]=127 SST [mg/l]=<20 |
| --- | --- | --- |

An.5.b: Continuous process scheme

| Department | dyeing |
| --- | --- |
| Fabric | CO, CO/PES |
| Process | vat dyeing of CO vat/dispers dyeing of PES/CO |
| Equipment | hotflue and pad-steam |
| Item | HF1-2 and PS2 |
| Operating | continuous |
| Number of cycles/yr |  |
| Cycle time (h) |  |
| Processed fabric (kg/yr) | 4215540 |
| Processed fabric per hour (kg/h) | 710 |

Vat dyeing of cotton: 50% of production

| Water vat dyestuff: 40 g/l antifoam agent (diluted solution: 1/100): 8 ml/l anti-migration agent: 8 g/l pick-up = 60% (this means 60% of the dyestuff is picked up by the fabric) sodiumhydrosulphite (140 g/l): 370 ml/l NaOH (40°Bé): 100 ml/l water: 4.5 l/kg water: 3 l/kg water: 3 l/kg water: 3 l/kg water: 0.7 l/kg oxidising agent (only for deep shades): 17 ml/kg water: 0.7 l/kg oxidising agent (only for deep shades): 17 ml/kg water: 0.6 l/kg oxidising agent (only for deep shades): 17 ml/kg water: 3 l/kg water: 3 l/kg water: 1 l/kg acetic acid: to get pH 6 on the fabric | padding the dyestuff + drying on the HF1-2 treatment steps on PS2 padding water seal rinsing rinsing rinsing oxidising oxidising oxidising rinsing rinsing neutralising | Discharge type : discharge of the padder liquor: concentrated solution of auxiliaries and dyestuff T [°C]=25 T [°C]=32 pH [-]=7.7 Conductivity [mS/cm]=1.11 COD [mg/l]=22 SST [mg/l]=<20 T [°C]=37 pH [-]=12.3 Conductivity [mS/cm]=10.46 COD [mg/l]=1170 SST [mg/l]=<20 T [°C]=30 pH [-]=11.4 Conductivity [mS/cm]=3.88 COD [mg/l]=430 SST [mg/l]=<20 T [°C]=40 pH [-]=11.5 Conductivity [mS/cm]=3.82 COD [mg/l]=470 SST [mg/l]=<20 T [°C]=70 pH [-]=4.4 Conductivity [mS/cm]=7.64 COD [mg/l]=11980 SST [mg/l]=<20 T [°C]=70 pH [-]=3.6 Conductivity [mS/cm]=6.22 COD [mg/l]=28720 SST [mg/l]=<20 T [°C]=70 pH [-]=3.9 Conductivity [mS/cm]=4.05 COD [mg/l]=11970 SST [mg/l]=<20 T [°C]=75 pH [-]=6.0 Conductivity [mS/cm]=1.13 COD [mg/l]=460 SST [mg/l]=<20 T [°C]=75 pH [-]=7.3 Conductivity [mS/cm]=1.13 COD [mg/l]=42 SST [mg/l]=<20 T [°C]=43 pH [-]=3.8 Conductivity [mS/cm]=1.41 COD [mg/l]=4990 SST [mg/l]=<20 |
| --- | --- | --- |

Vat/dispers dyeing of polyester/cotton: 50% of production

| Water dispers dyestuff: 2.2 g/l vat dyestuff: 21 g/l antifoam agent (diluted solution: 1/100): 8 ml/l anti-migration agent: 8 g/l pick-up = 60% (this means 60% of the dyestuff is picked up by the fabric) dry air sodiumhydrosulphite (140 g/l): 313 ml/l NaOH (40°Bé): 85 ml/l water: 8 l/kg water: 4.5 l/kg water: 4.5 l/kg water: 1.3 l/kg H2O2 : 15 ml/kg water: 1.1 l/kg H2O2 : 15 ml/kg water: 0 l/kg water: 0 l/kg water: 1.6 l/kg water: 1.6 l/kg acetic acid to get pH 6 on the fabric water: 1.6 l/kg acetic acid to get pH 6 on the fabric | padding the dyestuff + drying on the HF1-2 fixation of dispers dyestuff treatment steps on PS2 padding water seal rinsing (comp 1) rinsing (comp 2) oxidising (comp 3) oxidising (comp 4) rinsing (comp 5) rinsing (comp 6) rinsing (comp 7) neutralising (comp 8) neutralising (comp 9) | Discharge type: discharge of the padder liquor: concentrated solution of auxiliaries and dyestuff light/medium shades: COD [mg/l]=41 000 dark shades: COD [mg/l]=83 500 T [°C]=30 pH [-]=10.9 Conductivity [mS/cm]=5.0 COD [mg/l]=880 SST [mg/l]=<20 T [°C]=30 pH [-]=11.1 Conductivity [mS/cm]=3.72 COD [mg/l]=370 SST [mg/l]=<20 T [°C]=30 pH [-]=10 Conductivity [mS/cm]=2.0 COD [mg/l]=140 SST [mg/l]=<20 T [°C]=60 pH [-]=8.8 Conductivity [mS/cm]=2.53 COD [mg/l]=1085 SST [mg/l]=<20 T [°C]=60 pH [-]=10.7 Conductivity [mS/cm]=2.66 COD [mg/l]=440 SST [mg/l]=<20 T [°C]=95 pH [-]=9.6 Conductivity [mS/cm]=1.36 COD [mg/l]=630 SST [mg/l]=<20 T [°C]=95 pH [-]=8.5 Conductivity [mS/cm]=1.1 COD [mg/l]=195 SST [mg/l]=<20 T [°C]=95 pH [-]=8.63 Conductivity [mS/cm]=1.0 COD [mg/l]=250 SST [mg/l]=<20 T [°C]=50 pH [-]=4.4 Conductivity [mS/cm]=1.2 COD [mg/l]=1700 SST [mg/l]=<20 T [°C]=20 pH [-]=4.4 Conductivity [mS/cm]=1.1 COD [mg/l]=1200 SST [mg/l]=<20 |
| --- | --- | --- |

- dosage of water in compartment 7 and via counter current stream, this water flows to compartment 6 and 5.

- dosage of acetic acid in compartment 9, which flows counter current to compartment 8

An.5.b: Continuous process scheme

| Department | dyeing |
| --- | --- |
| Fabric | CO |
| Process | reactive dyeing of cotton |
| Equipment | pad batch and pad-steam |
| Item | PB2 and PS1 |
| Operating | continuous |
| Number of cycles/yr |  |
| Cycle time (h) |  |
| Processed fabric (kg/yr) | 559440 |
| Processed fabric per hour (kg/h) | 712 |

| Water reactive dyestuff: 0-40 g/kg NaOH: 5 ml/kg sodiumsilicate: 20 ml/kg wetting agent: 0.6 g/kg technical ureum: 20 g/kg antifoam agent: 0.2 ml/kg water: 2 m³/h water: 4 m³/h water: 4 m³/h water: 3 m³/h water: 3 m³/h detergent: 2 g/l water: 3 m³/h detergent: 2 g/l water: 4 m³/h water: 4 m³/h water: 3 m³/h acetic acid: to get pH 6 on the fabric | padding the dyestuff dwelling the padded rolls to let the dyestuff react with the fabric treatment steps on PS1 water-seal cold rinsing hot rinsing hot rinsing soaping soaping hot rinsing hot rinsing neutralising | Discharge type (l) + (l/h): 2 mixed samples were taken: COD [mg/l]= 16 600 and COD [mg/l]= 53 790 pH [-]=10.9 Conductivity [mS/cm]=10.1 COD [mg/l]=1 400 SST [mg/l]= 75 T [°C]=45 pH [-]=11.2 Conductivity [mS/cm]=8.93 COD [mg/l]=1 980 SST [mg/l]=41 T [°C]=72 pH [-]=10.9 Conductivity [mS/cm]=5 870 COD [mg/l]=1 890 SST [mg/l]=28 T [°C]=86 pH [-]=10.7 Conductivity [mS/cm]=3.86 COD [mg/l]=1 480 SST [mg/l]=42 T [°C]=93 pH [-]= Conductivity [mS/cm]=2.55 COD [mg/l]=807 SST [mg/l]=26 T [°C]=94 pH [-]=9.9 Conductivity [mS/cm]=1.84 COD [mg/l]=925 SST [mg/l]=<20 T [°C]=94 pH [-]=9.2 Conductivity [mS/cm]=1.38 COD [mg/l]=911 SST [mg/l]=<20 T [°C]=80 pH [-]=8.3 Conductivity [mS/cm]=1.15 COD [mg/l]=237 SST [mg/l]=<20 T [°C]= cold pH [-]=5.5 Conductivity [mS/cm]=1.21 COD [mg/l]=955 SST [mg/l]=<20 |  |
| --- | --- | --- | --- |